## Slide 1: Update MBHA-001 2020-03-06
TE-MSC-TF
F. Mangiarotti, G. Willering,
G. Ninet, V. Desbiolles
M. Bajko
Acknowledgements to all involved.

## Slide 2: Tests done since last meeting
Reflectometry (Jaromir)
Impedance measurements (Jaromir)
6 kA discharge with standard protection
11.85 kA discharge with standard protection
HV tests: standard + special 200 V QH to QH
6 kA discharge with D1U QH delayed 100 ms

## Slide 3: Special HV test
Each QH to each other QH: 200 V
All QH to coil: 300, 640, 1850, 3200 V
Coil to ground: 300, 640, 1850, 3300 V
All QH to ground: 300, 640, 1850, 3300 V
All tests passed OK

## Slide 4: Summary of discharges so far
4.5 K
4.5 K
4.5 K
“Standard” 6 kA: no spikes
no DAQ
I include the “no DAQ” line to keep track of what was done
D1U QH delayed
D1U QH delayed
6 kA with delayed QH: no spikes

## Slide 5: Summary of discharges so far
4.5 K
4.5 K
4.5 K
no DAQ
D1U QH delayed
D1U QH delayed
Nominal current discharges:
Very little spikes ~150-200 ms

## Slide 6: Summary of discharges so far
4.5 K
4.5 K
4.5 K
no DAQ
D1U QH delayed
D1U QH delayed
At 8.5 kA we see many spikes before the “bump”

## Slide 7: Summary of discharges so far
Trying to see the “envelope” of the spikes:
Get maximum absolute value every 10 ms
4.5 K
4.5 K
4.5 K
no DAQ
D1U QH delayed
D1U QH delayed

## Slide 8: Summary of discharges so far
Trying to see the “envelope” of the spikes:
Get maximum absolute value every 10 ms
4.5 K
4.5 K
4.5 K
no DAQ
D1U QH delayed
D1U QH delayed

## Slide 9: Summary of discharges so far
Trying to see the “envelope” of the spikes:
Get maximum absolute value every 10 ms
4.5 K
4.5 K
4.5 K
no DAQ
D1U QH delayed
D1U QH delayed

## Slide 10: Summary of 9kA discharges so far
4.5 K
no DAQ
Same procedure for 9kA discharges
D1U QH delayed

## Slide 11: Summary of 9kA discharges so far
4.5 K
no DAQ
Same procedure for 9kA discharges
D1U QH delayed

## Slide 12: Suspected short voltage vs current
Plot idea: Emmanuele Ravaioli
No clear correlation of current level or voltage level for spikes appearance
D1U QH delayed

## Slide 13: uQDS and SM18 DAQ spikes
SM18 and uQDS data recorded for the 4.5 K discharge at 9 kA
SM18 data at 50 kSPS + low pass filter (~600 Hz ?)
uQDS data at 205 kSPS
Spikes are identical

## Slide 14: Bump in voltage and dI/dt
Discharges at nominal current (11.85 kA) for the three MBH magnets
Bump in voltage is visible in dI/dt as well
MBHA-002 has delayed bump and current decay due to external QH

## Slide 15: Trim leads spikes
“copper”
“splice”
We observe reaction to the spikes in the trim lead signals
Amplitude < ~1mV
We will continue to investigate

## Slide 16: Next steps
10.5 kA discharge, standard QH
9 kA discharge, QH with inverse polarity
9 kA discharge, standard QH
9 kA discharge, standard QH, artificial short
9 kA discharge, QH at lower current ?
Impedance measurements at high current ?
SPA (-120 A/s) ?
Magnetic measurements ?