## Slide 1: LGAD measurements from different producers
Alissa Howard, G. Kramberger, žan KljuN, Petja Skomina
Jožef STEFAN institute, ljubljana
A work performed in collaboration with CMs-ETL and ATLAS-hgtd groups:
INFN-Torino, USCS, IHEP-Bejing, CNM

## Slide 2: Motivation for the studies
ATLAS and CMS upgrades require sensors to withstand φeq=2.5e15 cm-2 and TID 200 Mrad -> significant decrease of gain
Gain decreases as boron substitutional atoms get deactivated (“acceptor removal”) –> reduction of the field
Ways to mitigate degradation of gain layer:
  Make the implant thinner (IW->”0”) and more doped NB (~1e17 cm-3), reduces the acceptor removal constant (c~2-7∙10-16 cm2)
  Increase the bias voltage -> after depletion increase of electric field in the GL is DE ~DVbias/thickness
  Make the implant deeper (increase of GL)
    Larger multiplication region
    Easier to recuperate the electric field DVgl/GL compensated by DVbias/thickness
  Replacement of gain layer implantation material or co-implantation of material that decreases the acceptor removal rate (carbon)
GL
iw
thickness
GL~1-2.5 mm
iw~1 mm
NB~1-10∙1016 cm-3
We want to compare the producers, which have choosen different approaches to achieve sufficient radiation hardness.

## Slide 3: Experimental Procedure
Irradiated with neutrons (at JSI Triga II reactor)
Annealed for 80 mins @ 60˚C and kept cold
CVIV:
  20˚C/500mV/10kHz
  Vgl/Vfd determined from CV
Timing/CC :
  -30˚C/90Sr source
  See Gregor’s talk for details
Example of Vgl/Vfd determination:

## Slide 4: HPK-P2 – Samples
HPK-Prototype 2
  4 different doping profile (“Splits”)
  50µm
7 fluences [1e14, 4e14, 8e14, 15e14, 25e14, 30e14, 40e14]
Sensors were irradiated together (W28,33) and (W37,43) and were packed close together to minimise fluence uncertainty.
Difference in sensors VGL was small and measured VBR was close to targeted
PHOTO?
Wafer | Wafer Layout | Split | Vgl | Target Vbr | Measured Vbr
28 | Small | 1 | 50.5V | 160V | 85-155V
33 | Small | 2 | 51.0V | 180V | 85-170V
37 | Small | 3 | 53.7V | 220V | 155-205V
43 | Small | 4 | 54.5V | 240V | 170-235V

## Slide 5: HPK-P2 – Vgl and Neff vs fluence
Dashed line is fit of Vgl(φ)=Vgl(t=0)exp(-c*φ)
HPK-P2 | W28 | W33 | W37 | W43
c [ 10-16 cm-2] | 4.3 | 4.5 | 4.6 | 5.0
D=Sensor thickness
xgl=gain layer thickness (assume 2 µm)
geff~0.01-0.015 cm-1

## Slide 6: HPK-P2 – Timing/CC (at 2.5e15 cm-2)
W28 is slightly better in CC , but all sensors are very close in performance.
Collected charge
noise
Jitter
Time resolution
S/N
Leakage current

## Slide 7: HPK-P2 – Timing/CC (W28)
W28 - highest gain layer doping
HPK-P2 run satisfies HGTD –TDR requirements (pre and post radiation!)
  4fC @ 720 V and st<50 ps after 2.5e15 cm-2
  Ileak<5 mm, Pdis<100 mW cm2 , S/N > 10
  safe operation voltage Vop~780 V for the highest fluence
Collected charge
Time Resolution
Leakage current
Noise

## Slide 8: HPK-P2 – 70 MeV proton irradiated
Wafer | c [10-16 cm-2]
28 | 6.51
33 | 6.53
37 | 6.87
43 | 6.96
cp/cn~1.5-1.6
similar to previous measurements
2 fluences [1e14, 15e14]
Ratio between neutron and proton damage cp/cn is nicely reflected in CC measurements – similar charge vs. voltage plot for 1.5e15 p and 2.5e15 n.

## Slide 9: FBK UFSD3.2 run
Purpose of the run to find optimum gain layer doping layer parameters
    Carbon dose
    Boron dose
    Depth of implantation
    Thermal budget during activation
Irradiated in two batches:
  Batch 1: Wafers 4, 7, 8, 10, 12, 14
  Batch 2 : Wafers 13, 18, 19
5 fluences [1e13(batch1)/1e14(batch2), 4e14, 8e14, 15e14, 25e14]

## Slide 10: FBK UFSD3.2 – Vgl vs fluence
Wafer | c [10-16 cm-2]
4 | 2.23
7 | 1.55
8 | 1.07
10 | 1.58
12 | 1.52
14 | 2.13
Wafer | c [10-16 cm-2]
13 | 1.87
18 | 2.06
19 | 1.87
1st batch
2nd batch
Large uncertainties in measured c – use them only as guidance!
preliminary

## Slide 11: FBK UFSD3.2 – Timing/CC
W10/12/14:
  Good results for 1.5e15cm-2(all perform similarly), but early breakdown at < 600V doesn’t allow exploitation of beneficial gain layer properties at 2.5e15 cm-2.
  DV(5fC)~200 V between 1.5&2.5e15, which corresponds roughly to DVGL ~8 V for GL depth of ~2 mm. Measured DVGL~6 V .
W19:
  much lower Vop – most radiation hard LGAD seen so far!
  DV(5fC)~130 V between W19 & W14(2.5e15), which corresponds roughly to DVGL ~5 V for GL depth of ~2 mm. Measured DVGL~4 V .
2x2 device

## Slide 12: FBK UFSD3.2 – Timing/CC (W19)
Excellent CC and time resolution
Satisfies HGTD requirements and possibly extends the fluence range beyond required – no need for inner ring replacements

## Slide 13: NDLv3 – CV
Non-irradiated
Vgl~29.4 V
Vfd~83 V
C~4.2 pF/pad
Leakage current very small – on the level of hundreds of pA – no break down up to 200 V.
Small resistivity of the wafer – Vfd ~ 83 V
50 mm thick
B58
B14
Blue/yellow/green overlap
CV PLOT
3 fluences [8e14, 15e14, 25e14]
c=7.3∙10-16 cm2
B58
B14

## Slide 14: NDLv3 – CC & timing
Non-irradiated: Good charge collection, S/N and noise – similar for both device types
Devices are functional
Gain layer degradation is too large
  devices can not be operated at 2.5e15 cm-2 , breakdown at 710 V

## Slide 15: CNM – AIDA2020v2 (R12916)
these two used in tests: irradiated to 2.5e15 cm-2
Narrow and highly doped implant, but also shallow

## Slide 16: CNM – Timing/CC
Both irradiated to 2.5e15

## Slide 17: Comparison of Vgl vs Fluence
Wafer | c [10-16 cm-2]
13 | 1.9
18 | 2
19 | 1.9
Wafer | c [10-16 cm-2]
28 | 4.3
33 | 4.5
37 | 4.6
43 | 5
Wafer | c [10-16 cm-2]
B58/14 | 7.3
B58
B14
NLDv3
HPK-P2
FBK-UFSD3.2
Shallow & narrow highly doped implant
Deep & highly doped C enriched implant
Deep & narrow highly doped implant
Much lower c for FBK – carbon enrichment of gain layer significantly improves the radiation hardness.

## Slide 18: Comparison at 2.5e15 cm-2
(1.5e15 cm-2)
(1.5e15 cm-2)
(1.5e15 cm-2)
The most radiation hard wafers (FBK/HPK) and both NDLv3 and CNM-AIDA2020v2 compared!
The performance of FBK seems to be comparable to HPK at voltages that are 300 V lower – significant improvement.
  DVbias=300 V for 50 mm thick detector means DE=6 V/mm. Assuming 2 mm thick gain layer that results in DVgl~12 V. Measured DVgl~12V.
FBK UFSD3.2 is clearly most radiation hard, but we see some problems with sensors breaking down at >600V.
Vgl~33V
Vgl~20V

## Slide 19: Conclusions and future work
HPK meets radiation hardness requirement needed for HGTD
  Behave well and have shown they can produce working full size sensors.
  This will be the best we get from HPK – they will not do any C implantation
FBK has also shown they can withstand high irradiation
  Excellent GL design; C implantation significantly improves radiation hardness
  Vop way below any other vendors
  But need to show can perform equally well with full size sensors
  Also need to fix breakdown problem
CNM just reaches required radiation hardness
  Future runs include C implantation
  Also need to show can maintain performance with full size sensors
NDL produced a sensor that works, but still in early phase of development
  Need to improve radiation hardness by modifying GL
All future runs will be qualified in the same way as those presented here

## Slide 20: Backup: cp/cn
In HGTD inner ring, neutron/charge hadron mix is ~50/50, goes to ~75/25 in outer ring.
Can use the cp/cn ratio during neutron irradiations, irradiating to higher fluence to take into account extra damage charged hadrons would cause.