## Slide 1: SciFi Tracker Upgrades
Prepared: Guido Haefeli, 30.March 2020

## Slide 2: Outline
Expected aging of the SciFi after Run 3 & 4
Replacement and upgrade
Upgrade the performance of the SciFi
  Micro-lens enhancement of SiPMs
  Thinner SciFi
  Cryo-cooling
Conclusion for Upgrade 1b, Upgrade II

## Slide 3: SiPM aging
SiPM nominal design:
Design luminosity 50fb-1
  Neutron radiation: 6*1011 neq/cm2
  Charged: 50Gy, responsible for 15-20% of SiPM DCR increase after neutron shielding
Fluka simulation with neutron shield yields the values for the most exposed regions in T1 and T3:
  T1: 8.1*1011 neq/cm2  3.3*1011 neq/cm2 (reduction of 2.5 after shielding )
  T3: 14*1011 neq/cm2  4.2*1011 neq/cm2 (reduction of 3.4 after shielding )
Fluka simulation uncertainty for the absolute values of the neutron fluence is a factor 2

## Slide 4: SiPM aging
SiPM after Run 3 of 40fb-1 :
  T1: 2.6*1011 neq/cm2 (worst case 5.2*1011 neq/cm2 )
  T3: 3.3*1011 neq/cm2 (worst case 6.6*1011 neq/cm2 )
SiPM after Run 3&4 of 80fb-1 :
  T1: 5.2*1011 neq/cm2 (worst case 10.4*1011 neq/cm2 )
  T3: 6.6*1011 neq/cm2 (worst case 13.2*1011 neq/cm2 )
In red, values beyond the design fluence which is the limit of acceptable dark count rate (DCR) and has a consequence the noise cluster rate (NCR).
To maintain NCR<10MHz, the noise threshold cut has to be increased and the efficiency is dropping rapidly.

## Slide 5: Neutron fluence is responsible for 80-85% of DCR increase of the SiPM after shielding
Neutron fluence with neutron shield.
3.3*1011 neq/cm2
4.2*1011 neq/cm2

## Slide 6: Dose due to charged tracks, makes up 15-20% of the DCR increase for the SiPMs
Radiation dose profile in the x-y plane
Decrease to the edge is slow

## Slide 7: Irradiated detector with 6*1011 neq/cm2
Reducing ΔV by 1V reduces DCR by a factor 1.58!
DCR as a function of temperature at 3 different possible operation points

## Slide 8: PDE as a function of over-voltage
Light emitted by the SciFi is centered around 475nm
Reducing ΔV by 1V reduces PDE by a factor 1.12!

## Slide 9: Noise cluster rate (NCR) expected for the current SciFi
Integration window (Pacific 25ns)
For “high” DCR only increasing the threshold can reduce NCR.

## Slide 10: Noise cluster rate for different seed thresholds
Integration window (Pacific 25ns)
~50x

## Slide 11: Noise cluster rate expected for the current SciFi
Irradiated detector to 3*1011 neq/cm2
Pacific integration time 25ns
Exponential behaviour of NCR

## Slide 12: Radiation damage of the fibre results in lower photon survival probability
Linear law model ratios:
Power law model ratios:

## Slide 13
Reduceing ΔV by 1V reduces DCR by a factor 1.58!
12PE
18PE
Radiation damage reduces the LY
The selection at the production allows to obtain LY>18PE before irradiation

## Slide 14: Cutting or “not using” 30cm of the inner-most part of the module
8.7PE
12PE
30cm from beampipe

## Slide 15: Inefficiency as a function of noise cut and LY
Chart: 
| 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12 | 12.5 | 13 | 13.5 | 14 | 14.5 | 15 | 15.5 | 16 | 16.5 | 17 | Mean number of detected photons in PE (LY)
Sum threshold cut in PE 0.5 | 0.049787 | 0.030197 | 0.018316 | 0.011109 | 0.0067379 | 0.0040868 | 0.0024788 | 0.0015034 | 0.00091188 | 0.00055308 | 0.00033546 | 0.00020347 | 0.00012341 | 7.4852e-05 | 4.54e-05 | 2.7536e-05 | 1.6702e-05 | 1.013e-05 | 6.1442e-06 | 3.7267e-06 | 2.2603e-06 | 1.371e-06 | 8.3153e-07 | 5.0435e-07 | 3.059e-07
Sum threshold cut in PE 1.5 | 0.19915 | 0.13589 | 0.091578 | 0.061099 | 0.040428 | 0.026564 | 0.017351 | 0.011276 | 0.0072951 | 0.0047012 | 0.0030192 | 0.0019329 | 0.0012341 | 0.00078594 | 0.0004994 | 0.00031667 | 0.00020042 | 0.00012663 | 7.9875e-05 | 5.031e-05 | 3.1645e-05 | 1.9879e-05 | 1.2473e-05 | 7.8174e-06 | 4.8944e-06
Sum threshold cut in PE 2.5 | 0.42319 | 0.32085 | 0.2381 | 0.17358 | 0.12465 | 0.088376 | 0.061969 | 0.043036 | 0.029636 | 0.020257 | 0.013754 | 0.0092832 | 0.0062322 | 0.0041636 | 0.0027694 | 0.0018346 | 0.0012109 | 0.00079648 | 0.00052226 | 0.00034145 | 0.00022264 | 0.00014481 | 9.3963e-05 | 6.0837e-05 | 3.9308e-05
Sum threshold cut in PE 3.5 | 0.64723 | 0.53663 | 0.43347 | 0.3423 | 0.26503 | 0.2017 | 0.1512 | 0.11185 | 0.081765 | 0.059145 | 0.04238 | 0.030109 | 0.021226 | 0.01486 | 0.010336 | 0.0071474 | 0.0049159 | 0.0033642 | 0.0022918 | 0.0015546 | 0.0010503 | 0.00070699 | 0.00047425 | 0.0003171 | 0.00021138
Sum threshold cut in PE 4.5 | 0.81526 | 0.72544 | 0.62884 | 0.5321 | 0.44049 | 0.35752 | 0.28506 | 0.22367 | 0.17299 | 0.13206 | 0.099632 | 0.074364 | 0.054964 | 0.040263 | 0.029253 | 0.021094 | 0.015105 | 0.010747 | 0.0076004 | 0.0053455 | 0.0037402 | 0.0026043 | 0.0018052 | 0.001246 | 0.00085664
End of Run4, >20%
End of Run 3, 2-3%

## Slide 16: Micro-lens enhanced SiPMs
Goal 1: Reduce pixel size without loosing light to reduce:
optical x-talk
gain and therefore bias current and self heating
recovery time (dead time) and after-pulsing
DCR for irradiated devices
Goal 2: Improve sensitivity (PDE)
use micro-lenses to focus light in the center of the pixel avoiding dead and low-field region
Expected improvement of the LY is larger than 20%
Same detector geometry and package size as current SiPM array
High cost for micro-lenses and through silicon via (TSV) package
No cleaning possible anymore
Pro:
Cons:

## Slide 17: Higher GFF technology between 2017 and now
GFF=70% for H2017 62x57.5μm2 vs GFF>80% for FBK 40x40μm2
GFF
Implementation example from FBK: High geometrical fill factor (GFF) due to thin trenches, NUV-HD has 20% higher GFF than the previous NUV design.
Comparison with H2017:

## Slide 18: Reducing occupancy
Typical cluster for an orthogonal track has a size of 3 channels.
Maximum occupancy depends not only on the number of tracks per linear distance but also on the cluster size.

## Slide 19: Reducing occupancy
3 ch
5 ch

## Slide 20: Reducing occupancy with thinner SciFi mats (less layers = less signal)
2 ch
4 ch
Less light, this can work with cryogenic cooling!

## Slide 21: Reducing occupancy with thinner SciFi mats and or segmenting channels in height
2 ch
2 ch
3 ch
2 ch
Requires 2x the number of channels, this will be simulated for evaluation.

## Slide 22: Reducing noise drastically with cryogenic cooling (LN2) in a vacuum chamber
SciFi mat
SciFi mat
mirror
SciFi mat
SciFi mat
Vacuum insulated cold box for LN2 cooling
Electronics
Note:
Flexible interface with clear fibre, expected light loss <15%
Total width of vacuum vessel allows space between modules. Sufficient space for services for the Si-pixel detector is available
Vacuum feedthrough with clear fibres
Vacuum
vessel

## Slide 23: Reducing noise drastically with cryogenic cooling (LN2) in a vacuum chamber
-40°C
120K -> 1/4000 DCR of the current level
2017
FBK cryo version of SiPMs

## Slide 24: Reducing noise drastically with cryogenic cooling (LN2) in a vacuum chamber
Noise reduction for FBK SiPMs optimized for cryogenic operation:
pessimistic assumption for noise reduction slope (10K instead of 8K for a factor 2)
Limited range of valid slope
Upgrade II conditions, 10 x radiation level 6*1012 neq/cm2 of current Upgrade
5x higher DCR than Hamamatsu for the same neutron fluence
Cryocooling allows to reduce DCR to a level of 5*107 Hz per SiPM array
Noise cut is as low as 1.5PE producing less NCR than for the current detector
Cryogenic cooling is currently the only solution to operate the SciFi tracker beyond Run 4! It can compensate for the reduction of LY due to the fibre irradiation.

## Slide 25: Conclusion
Large uncertainties for radiation level simulated by Fluka (Factor 2), neutron shield and neutron fluence.
Uncertainties for efficiency are large when the LY is close to 10 photons, steep rise
Uncertainties in LY from the fibre module at large irradiation level, annealing and aging of scintillator
We need to operate the detector to gain detailed knowledge
Upgrade 1b:
Optimistic scenario:
Replace the 12 0° central modules (6 layers) with Si-pixel + SciFi modules.
Keep fibre modules with 5° angles without exchange of fibres
Replace SiPMs for all 24 central modules after Run 3 (avoid 80fb-1 of radiation for central SiPMs)
Develop and produce advanced micro-lens enhanced SiPMs for this replacement
Pessimistic scenario:
All replacements needed for the optimistic case plus replacing also the 5° central fibre modules
Upgrade 2:
Replace all modules and SiPMs
Replace cooling with cryogenic LN2 cooling and develop a clear fibre interface

## Slide 26: EPFL and Upgrade 1b,2
Development of radiation optimized SiPMs
  Study optical focusing system on pixels with micro-lens to increase overall PDE.
  Study more radiation hard SiPM implementations (silicon structures) and the use of smaller pixels (Hamamatsu, Ketek, FBK, SensL, …).
Development of a clear fibre interface required for cryogenic cooling (vacuum feedthrough) and to reduce SciFi length for segmented readout.
Development of fast, high light yield, green fibres to reduce light transport loss (radiation) with possible application in LHCb SciFi Upgrade 1b or II.

## Slide 27: Backup S/N
27
Reduced hit detection efficiency is the “aging” effect of the SciFi and is directly coupled to the S/N ratio.
For 50 fb-1 a reduction of efficiency of 1-2% is expected. Precise numbers are difficult to obtain before a few years of operation.
S / N
Increase luminosity increases noise
Light loss of fibres decreases signal, green fibres help.
Increase PDE of SiPM increases signal
Decrease active surface of SiPM reduces noise
Reduce pixel size to improve x-talk, AP DCR, current induced self-heating
Decrease the number of fibre layers in mat to reduce occupancy!