## Slide 1: HEPDipo Status of the design and developments Baseline and 4 coils comparaison
MSC-MDT
April 1st, 2020

## Slide 2: Status of models and design
Model | Baseline | 4 coils option
2D Ansys magnetic |  | 
2D Opera magnetic |  | 
2D Roxie magnetic |  | 
2D Ansys mechanical |  | 
3D Ansys magnetic |  | 
3D Opera magnetic |  | 
3D Ansys mechanical |  | Updating for the new 4 coils solution
Magnet protection |  | Updating for the new 4 coils solution
Status of design | Addressing issues: pre-load criterium Ti pole deformation Stress on the wedge Rod (Al / SS) | Addressing issues: pre-load criterium Stress on the end plate etc..

## Slide 3: Status of cable trials
Magnet / option | Ramp angle (°) | Winding machine load 25 and 50 kg | Geometric measurements | Laser track
HEPDipo baseline | 10 |  |  | 
HEPDipo baseline | 17 (FRESCA2) |  |  | 
HEPDipo 4 coils Outer coil | 10 |  |  | 
HEPDipo 4 coils Outer coil | 17 (FRESCA2) |  |  | 
DEMO 16 T for FCC Inner layer | - |  |  | 
DEMO 16 T for FCC Outer layer | - |  |  | 
Status | finished | finished | finished | Data under analysis

## Slide 4: 4 coils option vs 6 coils (baseline)
Yoke
horizontal pad
vertical
pusher
iron pole
Aluminum Shell
titanium
pole
mid-plane
shim
inter-coil
shim
Coil1
Coil2
Coil3
Coil1
Coil2

## Slide 5: 4 coils option vs 6 coils (baseline)
 | Turns (1/4)
4 coils | 92
6 coils | 96
50 turns
50 turns
42 turns
42 turns
rails
boat
iron
pole
titanium
pole
mid-plane
shim
32 turns
32 turns
32 turns
32 turns
32 turns
32 turns

## Slide 6: Goal and cable data
 | Goal (SPC / LBNL)
B center | 15 / 16 T
% SS | 85% / 84%
temperature | 4.2 / 1.9 K
aperture | ‘rectangular’ 150x100
length | ~ 2 m
Cable data | 
number of strands | 44
thickness | 1.95 mm
width | 26.2 mm
turn insulation thickness | 0.20 mm
coil insulation thickness | 0.5 mm
Inter-layer insulation | 0.5 mm

## Slide 7: Wire specification
Parameter | Value
Wire technology | RRP 108/127
Wire diameter in mm | 1.1
Cu:non-Cu ratio | 1
RRR | >150
Critical current density at 15 T, 4.2 K in A/mm2 | 1640
Parameter | Value
Critical current density at 12 T, 4.2 K in A/mm2 | 3000
C0 in AT/mm2 | 255230
α | 0.96
TC0 in K | 16
BC20 in T | 28.8

## Slide 8: Magnetic results comparison (85 % of LL – 4.2 K)
Parameter | 4 Coils value | 6 Coils value
Bap - aperture field (T) | 14.84 | 14.82
Bpk - Coil peak field (T) | 15.17 | 15.31
Field quality b3, b5, b7, b9 (units) | - 5.86, - 4.01, 2.05, - 0.10 | 42.08, - 10.49, - 0.80, - 0.14
Energy per length (MJ/m) | 7.3 | 6.86
Horizontal Lorentz force (1/4) (MN/m) | 14.37 | 14.41
Vertical Lorentz force (1/4) (MN/m) | - 8.56 | - 7.11
Operational current (kA) | 14.67 | 14.28
(Bap/Bpk)/(SC_area) (1/mm2) | 8.09E-5 (+5.5%) | 7.68E-5

## Slide 9: Stress on coils comparison
High field
region
HF
region
HF
region
HF
region
HF
region
Inner
coil
Outer
coil
Inner
coil
Outer
coil
Inter
coil
15 T operation | 4 Coils von Mises stress | 6 Coils von Mises stress
Inner / inter / outer coils | 145 / / 120 MPa | 158 / 115 / 110

## Slide 10: Mechanical results comparison
Parameter | 4 Coils value (MPa) | 6 Coils value
 | Room temperature / cooling down / 15 T | Room temperature / cooling down / 15 T
Inner coil | 9 / 52 / 145 | 48 / 110 / 158
Inter coil | - | 74 / 154 / 145
Outer coil | 55 / 103 / 135 | 53 / 113 / 117
Iron pole (S1) | 1 / 13 / 280 | 1 / 15 / 246
Horizontal pad (S1) | 92 / 157 / 109 | 100 / 200 / 130
Vertical pad (S1) | 44 / 54 / 128 | 57 / 77 / 78
Yoke (S1) | 92 / 155 / 194 | 105 / 108 / 140
titanium pole (Von Mises) | 81 / 590 / 800 | 370 / 766 / 1225
Shell (Azimuthal) | 70 / 163 / 154 | 123 / 215 / 234

## Slide 11: Parametric analysis: horizontal tolerance
Fixed position
for the inner coil
Horizontal misalignment
Inner
coil
Outer
coil
Horizontal
misalignment
Horizontal misalignment
Fixed position
for the inner coil
Inner
coil
Outer
coil
Inter
coil

## Slide 12: Parametric analysis: horizontal tolerance
Chart: Von Mises Stress – High Field Region
| 0 mm | 0.25 | 0.5 | 0.75 | 1
4 coils | 145 | 146 | 147 | 148 | 147
6 coils | 158 | 163 | 174 | 181 | 185
4 Coils
6 Coils
For a mm of displacement
the peak of stress of the 4 coils
option remains the same.
The peak is stress of the 6 coils
option goes from 157 to 186 MPa

## Slide 13: Parametric analysis: horizontal tolerance (1 mm)
4 Coils
6 Coils
147 MPa
185 MPa

## Slide 14: Parametric analysis: vertical tolerance
Inner
coil
Outer
coil
Fixed position
for the inner coil
Inner
coil
Outer
coil
Inter
coil
Fixed position
for the inner
coil
The inner coil position is fixed. An interference, representing the dimension tolerance is introduced between coils ( )

## Slide 15: Parametric analysis: vertical tolerance - coils
Chart: Von Mises Stress – High Field Region
| 0 mm | 0.25 | 0.5 | 0.75 | 1
4 coils | 145 | 157 | 165 | 168 | 187
6 coils | 158 | 189 | 227 | 260 | 296
4 Coils
6 Coils
For a mm of interference between
Coils, the peak of stress of the
4 coils option goes from 145 to
187 MPa
The peak of stress of the 6 coils
option goes from 157 to 290 MPa

## Slide 16: Parametric analysis: vertical tolerance (1 mm)
4 Coils
6 Coils
188 MPa
297 MPa
220 MPa

## Slide 17: Parametric analysis: vertical tolerance – Ti pole
Chart: Von Mises Stress – Ti pole
| 0 mm | 0.25 | 0.5 | 0.75 | 1
4 coils | 800 | 940 | 1110 | 1268 | 1438
6 coils | 1225 | 1493 | 1762 | 2014 | 2262
4 Coils
6 Coils
For a mm of interference between
coils the peak of stress on the Ti
Pole of the 4 coils option goes from
800 to 1438 MPa
The peak is stress on the Ti pole
of the 6 coils option goes from
1225 to 2262 MPa

## Slide 18: Parametric analysis: vertical tolerance (1 mm)
4 Coils
6 Coils
Titanium Yield point = 1650 MPa
1440 MPa
2260 MPa

## Slide 19: Annex

## Slide 20: Magnetic 4.2 K - 85% of the load line
Bore field (B): 14.84 T
Max coil field (B): 15.17 T

## Slide 21: Magnetic 4.2 K - 85% of the load line
Bore field (B): 14.82 T
Max coil field (B): 15.31 T