## Slide 1
21.04.2020.
Status of laser polishing/treatment for QPR samples
Arturs Medvids, Pavels Onufrijevs, Aleksandrs Mychko, Liga Grase

## Slide 3
Fig.1. Optical image of Bulk Nb sample. Irradiated places are dark.
Sample diameter is 50 mm, irradiated areas are of size 5x5 mm2.
Imax
I min
I mid

## Slide 4: Fig. 2. Magnified image of the irradiated 5x5 mm2 area of the sample. The irradiated area is smoother.

## Slide 5: Fig. 3. Optical microscope images of the non-irradiated and irradiated with middle (irradiated 1) and maximal (irradiated 2) Nd:YAG laser intensity sample. The irradiated surface becomes smoother.
Non-irradiated
Irradiated 1
Irradiated 2
Laser: 1064 nm
Spot diameter: 1.5 mm
Scan speed: 1.0 mm/s
Span pitch: 0.3 mm
Irradiated 1
Energy: 34.1 ± 0.5 mJ
Filter: HC-1
Focus lens: 5.5 cm
Irradiated 2
Energy: 44.7 ± 0.6 mJ
Filter: Not used
Focus lens: 5.5 cm
Optical Microscope

## Slide 6: Fig. 4. XRD pattern of the non-irradiated and irradiated areas with minimal, middle and maximal laser intensity.

## Slide 7
Non-irradiated
white light interferometry

## Slide 8
Irradiated-4

## Slide 9
Thank you for your attention!