## Slide 1: EUROPEAN ORGANIZATION FOR NUCLEAR RESEARCH Proposal to the ISOLDE and Neutron Time-of-Flight Committee
D. Zyabkin1, I. Unzueta2, R. Mantovan3, H. P. Gunnlaugsson4, H. Masenda5, D. Naidoo6, K. Bharuth-Ram7, J. Schell7,8, P. B. Krastev9, S. Ólafsson10, B.Qi10, T. T. Dang7, K. Johnston8, D. C. Lupascu7 P. Schaaf1
1Department of Materials for Electronics, Institute of Materials Science and Engineering, TU Ilmenau, 98693, Germany
2Department of Applied Mathematics, University of the Basque Country UPV/EHU, 48013, Spain
3Laboratorio MDM, IMM-CNR, Via Olivetti 2, 20864, Agrate Brianza (MB), Italy
4Science Institute, University of Iceland, Dunhaga 3, IS-107 Reykjavík, Iceland
5School of Physics, University of the Witwatersrand, WITS 2050, South Africa
6University of KwaZulu-Natal, Durban 4001, South Africa
7Institute for Materials Science and Center for Nanointegration Duisburg-Essen (CENIDE), University of Duisburg-Essen, 45141, Germany
8European Organization for Nuclear Research (CERN), CH-1211 Geneva, Switzerland
9Institute for Nuclear Research and Nuclear Energy, Bulgarian Academy of Sciences, Sofia, 1784, Bulgaria
10Science Institute, University of Iceland, 107, Iceland
Development of new rare-earth-free hard magnetic materials
INTC-P-564
1

## Slide 2
New hard magnets?
2
INTC-P-564
Growing amount of autonomous vehicles, automatization
High demand of hard magnets
Depletion of rare-earth metals
(Nd, Dy, Tb etc)
MnX (X= Al, Bi & Ga)
Hard magnets without rare-earths?
Alternatives?

## Slide 3
Candidates
3
INTC-P-564
Segregation of Mn?
Doping theoretically may lead to high magnetization
hex.- MnBi
Metastable
L10- MnAl
Where is surplus of Mn? Which site?
Doping? Deteriorates magnetic properties!
Fe-doped is stable, what about dilute concentrations?
Not a single phase

## Slide 4
Candidates
4
INTC-P-564
L10- MnGa
Reveal the interplay between structure/strain and magnetism
Origin of the unexpected large hyperfine field at Ga sites
Expected:
negligible hyperfine fields with In at Ga sites
huge hyperfine fields with 119In
Observed:
LS2 did not allow to finalize the studies
In/Sn measured at angles of 60 and 0 under 0.6T during (a) and after (b) implantation.

## Slide 5
Feasibility
HOW?
As a function of
Sample stoichiometry
  MnxAl [x=49-60]
  MnxBi [x=49-60]
  MnxGa [x=0.7-1.9]
Annealing and measuring temperature
Magnetic field
Implantation depth [TRIM est. at 40 keV]:
19/13 nm [57Mn/ 119In] into MnAl
22/16 nm [57Mn/ 119In] into MnBi
15/10 nm [57Mn/ 119In] into MnGa
5
INTC-P-564
WHAT?
MnAl, MnBi & MnGa by electron beam and magnetron sputtering
[TU Ilmenau]
[ISOLDE/CERN]

## Slide 6
Feasibility
6
INTC-P-564
Emission Mössbauer spectroscopy
Probe-host & probe-defect interaction
  Valence, site symmetry, magnetic interactions, diffusion, spin relaxation, binding properties
Dilute concentration (~10-4 at.%)
Short spectra collection time

## Slide 7: eMIL
7
INTC-P-564
Zyabkin et al. Nucl. Instrum. Methods Phys. Res A.968 (2020)
Annealing up to 1100 K
Time-delayed measurements
Angular dependence
Solid Base for future modifications
Cryogenic measurements

## Slide 8: eMIL + eMMA
8
INTC-P-564
Magnetic field up 2.2 T
Off/On-line usage
Heating & possible cooling
Promising platform for investigation of magnetic materials

## Slide 9
BEAM TIME REQUEST
Isotope | Minimum intensity | Beam energy | Shifts | Target | Ion source
57Mn (1.5min) | (1-3) x 108 | ≥ 40 keV | 10 | UCx | Mn RILIS
119In (2.1min) | (2-3) x 108 | ≥ 40 keV | 5 | UCx | In RILIS
9
INTC-P-564

## Slide 10: FUNDING INVOLVED
BMBF
Bundesministerium für Bildung und Forschung
Erforschung kondensierter Materie mit Großgeräten
Ausbau und Unterhalt der Einrichtungen an ISOLDE/CERN
Germany, contract: 5K19SI1
10
INTC-P-564

## Slide 11
Thank you for your attention!
11
INTC-P-564

## Slide 12
57Mn/57Fe
Additional information eMS
12
INTC-P-564