## Slide 1: Perturbed angular correlation and x-ray diffraction studies on the α-β phase transition in multiferroic bismuth ferrite
DI Georg Marschick

## Slide 2: Bismuth Ferrite – BiFeO3
Quasi-cubic canted perovskite of LiNbO3 type
Curie Temperature: 820°C
Néel Temperature: 370°C
  Thus magnetoelectric at room temperature
Rhombohedral α-phase
Orthorhombic β-phase
α
β

## Slide 3: Structural studies – lattice and local properties
Perturbed angular correlation (local properties)
  Asymmetry and strength of Electric field gradient
  How are local properties influenced by the phase transition?
  Is the phase transition visible?
X-ray diffraction (lattice properties)
  Description of unit cell, lattice parameters and space group
  Atomic positions, bond lengths and angles
  Well known and understood method
Notes: PAC: determining the limits of pac, can we perform a structural analysis?
Xrd: validate the results of pac

## Slide 4: Perturbed Angular Correlation (PAC) Naive theory
We measure a frequency ω of angular γ-γ coincidences…
…due to force acting on the nucleus and thus „turning“ it…
…caused by electric or magnetic fields in the nucleus´ vicinity.
Observable
Actor / Consequence
Reason

## Slide 5: Perturbed Angular Correlation (PAC) Naive theory
Emission characteristic of γ-radiation – orientation of nuclei
Anisotropic emission of a γ- γ cascade
Conservation of angular momentum and selection rules
+
=
z
Channel
# of γ-γ coincidences

## Slide 6: Perturbed Angular Correlation (PAC) A method to probe hyperfine interactions in matter
z
intensity
Target
Molten Sn
Acceleration
Mass separation
Primary 1.4 GeV
proton beam
γ1
γ2

## Slide 7: Perturbed Angular Correlation (PAC) A method to probe hyperfine interactions in matter
90°
90°
z
intensity
Target
Molten Sn
Acceleration
Mass separation
Primary 1.4 GeV
proton beam
γ1
γ2
Cd @ Bi-site

## Slide 8: Perturbed Angular Correlation (PAC) A method to probe hyperfine interactions in matter
5/2+
245.395keV
84.5ns
ω1
ω3
ω2
ωL
2ωL
Electric Field Gradient (EFG)
Magnetic Hyperfine field
Nuclear level splitting
+ combined interactions
ω1
ω2
ω3
ωL
2ωL
ωn
Transition frequencies
Nuclear probing state in matter
Consequence
Observable
ω
ω

## Slide 9: Perturbed Angular Correlation (PAC) A method to probe hyperfine interactions in matter
5/2+
245.395keV
84.5ns
ω1
ω3
ω2
Electric Field Gradient (EFG)
Electric quadrupole interaction
Transition frequencies
Nuclear probing state in matter
Consequence
Observable
ω
interacts with core quadrupole moment Q
η
η=0
symmetric
ω1
ω2
ω3
η≠0
ω1
ω2
ω3
ω1=
ω2
ω3
η=1
unsymmetric
and Vzz (ω0)
describe the EFG

## Slide 10: DFT Simulations at University of Aveiro (PT)
(
Range of values follows the error
of the Q values of Cd of Q=0.641(25) b
Density functional theory simulations to calculate Vzz and η done for Cd @ Bi

## Slide 11: PAC Studies at CERN - ISOLDE (CH)
BiFeO3 samples were cut and 111mCd implanted at GLM
beamline at 30keV
6 detector fully digital spectrometer
High temperature measurements directly after implanting
One temperature per sample

## Slide 12: Temperature dependence of perturbation function R(t)

## Slide 13: Temperature dependence of error function R(t)
β
α

## Slide 14: X-ray diffraction studies at TU Wien (AT)
Samples were ground and placed on Pt-sample holder
Single temperature Bragg Brentano measurement (20°-70°)
Sweep measurements 30-33° (800-840-800°C)

## Slide 15: X-ray diffraction studies at TU Wien
Single temperature measurements
Sweep measurement 30°-33°
Both measurements show a phase transition at 818-820°C

## Slide 16: Results
The results of both experimental methods agree with a phase transition from rhombohedral α-BFO in R3c setting to orthorhombic β-BFO with its Pbnm space group at 820°C
PAC results suggest a forecast of the first order phase transition by the Cd probe ion as it senses the preceding symmetry change of the Bi(Cd) coordination environment
Phase transition is visible through a drop in quadrupole interaction frequency ω0
DFT results support the PAC results
XRD single temperature measurements suggest a phase transition temperature of 818°C, sweep measurements indicate a transition temperature of 820°C
The XRD results support the results gained with PAC

## Slide 17: Thank you!
J. Schell2, 3, B. Stöger1, J. N. Gonçalves4, M. O. Karabasov3, D. Zyabkin5, A. Welker2, M. Escobar C.3, D. Gärtner6, I. Efe7, R. A. Santos8, J. E. M. Laulainen9 and D. C. Lupascu3
1 X-Ray Center, Vienna University of Technology, 1040 Vienna, Austria
2 European Organization for Nuclear Research CERN, CH-1211 Geneva, Switzerland
3 Institute for Materials Science and Center for Nanointegration Duisburg-Essen (CENIDE), University of Duisburg-Essen, 45141 Essen, Germany
4 Departmento de Física and CICECO, Universidade de Aveiro, 3810-193 Aveiro, Portugal
5 Chair Materials for Electronics, Institute of Materials Science and Engineering and Institute of Micro and Nanotechnologies MacroNano, TU Ilmenau, 98693 Ilmenau, Germany
6 Institut für Materialphysik, AG Wilde, Universität Münster, 48149 Münster, Germany
7 Department of Materials, ETH Zürich, 8092 Zürich, Switzerland
8 Hyperfine Interactions Group - IPEN University of São Paulo, São Paulo, SP, Brazil
9 Department of Materials Science and Metallurgy, University of Cambridge, Cambridge, United Kingdom
Federal Ministry of Education and Research (BMBF) through grants 05K16PGA and 05K16SI1
European Union’s Horizon 2020 Framework research and innovation program 654002 (ENSAR2)
Thanks to the whole team of ISOLDE for the support and the high-quality beams

## Slide 19: DFT Details
VASP Code (Vienna Ab-Initio Simulation Package)
projector augmented wave method with a general gradient approximation
  5d106s26p3 for Bi
  2s22p4 for Fe
  3p63d64s2 for O
  4d105s2 for Cd
Alpha phase: 2x2x1 supercell with 4x4x3 k-point grid
Beta phase: 2x2x1 supercell with 5x5x4 k-point grid
Bi2Fe4O9: 2x1x2 supercell with 3x2x4 k-point grid
Energy cut-off 450eV
Self consistent stop @ values < 10e-5 eV

## Slide 20
DFT Results
PAC Results
Ion radii