## Slide 1: Research and development on SRF 6 GHZ cavities
Vanessa Garcia Diaz, E. Chyhyrynets, F. Stivanello, M. Zanierato, C. Pira
EASITrain – European Advanced Superconductivity Innovation and Training. This Marie Sklodowska-Curie Action (MSCA) Innovative Training Networks (ITN) has received funding from the European Union’s H2020 Framework Programme under Grant Agreement no. 764879

## Slide 2: Outline
Why 6 GHz?
State of art on 6 GHz cavities
Seamless motivation
Manufacturing process
Surface treatments
Coating process
RF Characterization
Magnetic flux trapped study
Nb on Cu coated QWR (LNL)

## Slide 3: Why 6 GHz cavities?
10 cm
~40 cm
6 GHz
1,3 GHz
400 MHz
~ 100 cm
S. Bauer et al., TEST RESULTS OF SUPERCONDUCTING CAVITIES PRODUCED AND PREPARED COMPLETELY IN INDUSTRY, Proceedings of EPAC 2004, Lucerne, Switzerland.

## Slide 4: Why 6 GHz cavities?
Low cost
Statistic
Easy to handle
Smaller equipments
10 cm
6 GHz

## Slide 5: State of Art Nb on Cu
ALPI (LNL-INFN)
ISOLDE (CERN)
LHC (CERN)
LEP2 (CERN)
High Q0
Thermal stability
Cost reduction
Bulk Nb
Nb on Cu
6GHz
6GHz

## Slide 6: 6GHz State of Art
Chart: Eacc (MV/m)
| 1.0744579999999999 | 1.2723845 | 1.5268614 | 1.8096136 | 2.0640904999999998 | 2.3751177999999999 | 2.7709708000000002 | 3.1668238999999998 | 3.5344014000000001 | 3.9302545000000002 | 4.3543824999999998 | 4.8067859999999998 | 5.3722899999999996 | 5.8812439999999997 | 6.4184732000000002 | 6.899152 | 7.4363809999999999 | 8.1432610000000007 | 8.6804904999999994 | 9.1328940000000003 | 9.8397740000000002 | 10.574928999999999 | 11.310085000000001 | 11.98869 | 12.63902 | 13.374174999999999 | 13.996230000000001 | 14.731385 | 15.579642 | 16.314796000000001 | 17.30443 | 18.011310000000002 | 18.803017000000001 | 19.453346 | 20.386429 | 21.291235 | 22.224318 | 23.270499999999998 | 24.316683000000001 | 24.967012 | 25.617342000000001 | 26.098020000000002 | 26.522148000000001
Nb_bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Thin film reference 1.8K | 711000000 | 696000000 | 743000000 | 744000000 | 740000000 | 736000000 | 732000000 | 726000000 | 715000000 | 712000000 | 700000000 | 697000000 | 688000000 | 680000000 | 670000000 | 659000000 | 651000000 | 647000000 | 639000000 | 629000000 | 629000000 | 622000000 | 614000000 | 604000000 | 601000000 | 594000000 | 585000000 | 582000000 | 574000000 | 562000000 | 559000000 | 546000000 | 530000000 | 512000000 | 491000000 | 476000000 | 459000000 | 429000000 | 402000000 | 377000000 | 376000000 | 348000000 | 322000000 | 293000000 | 265000000 | 243000000 | 225000000 | 199000000 | 179000000 | 156000000 | 133000000 | 115000000 | 102000000 | 87300000 | 69900000 | 57400000 | 49300000 | 46100000
Best 6GHz Nb bulk
Nb on Cu thin film
Increase performances!

## Slide 7
Manufacturing
Surface preparation
Chemical preparation
PVD process
Cleanroom assembly
RF characterization

## Slide 8: Seamless motivation
Imperfections
+
Roughness effect
JLAB
Defects in the equator!
Lower RF performances
See Sertore’s and Pira’s lecture (30/09)

## Slide 9: Seamless motivation
QPR ECR
400MHz
LHC DCMS 400MHz
1-cell HIPIMS
1.3GHz
HIE-ISOLDE QS16
100MHz
1-cell DCMS
1.5GHz
HIE-ISOLDE QSS2
100MHz
TESLA bulk Nb
1.3GHz (*)
L. Lilje “State of the art SRF cavity performance” Proceedings of LINAC 2004, Lübeck, Germany
W. Venturini “Thin film research: CERN experience and possible future applications” TTC meeting Milano 2018

## Slide 10: Manufacturing process @LNL
Spinning of a Brass Disc
https://www.manufacturingguide.com/en/spin-forming-discs
V. Palmieri «Seamless 1,5GHz cavities obtained by spinning a circular blank of Copper or Niobium» Proceedings of SRF 1993, Virginia, USA.

## Slide 11: Surface preparation
Cavity inner surface after grinding

## Slide 12: Surface preparation
Step 2
Al2O3
Coconut
4h
8h
0,3 g/h
3,6 µm/h
Step 1
0,01 g/h
0,1 µm/h
Vibrotumbling
Courtesy of Eduard Chyhyrynets
Initial surface

## Slide 13: Surface preparation
Vibration
Rotation
Vibrotumbling
Courtesy of Eduard Chyhyrynets

## Slide 14: Chemical preparation
Deoxidation
Electropolishing
Chemical polishing SUBU
HPR
Vertical electropolishing set up
HPR set up

## Slide 15: PVD process by DC Magnetron Sputtering
J. A. Thornton and D. W. Hoffman, “Stress-related effects in thin films,” Thin Solid Films, vol. 171, no. 1, pp. 5–31, 1989.
High substrate temperature
Copper @550°C
Niobium
See Pira’s lecture (30/09)

## Slide 16: PVD process by DC Magnetron Sputtering
Thick film
Nb bulk like properties
Decrease thermal boundary resistance
Thin film ~2-3 µm
Thick film ~70 µm
Copper
Niobium
High substrate temperature

## Slide 17: PVD process: thick films by long pulsed DCMS
Copper
Niobium
Thick film ~70 µm
Total time of process ~ 5 hours
DC ON
DC OFF
Single Layer thickness
100 - 500 nm
Chart: time (s)
| 0 | 50 | 50 | 230 | 230 | 270 | 270 | 450 | 450 | 490 | 490 | 670 | 670 | 710 | 710 | 890 | 890 | 910 | 900 | 1000
 | 0 | 0 | 1 | 1 | 0 | 0 | 1 | 1 | 0 | 0 | 1 | 1 | 0 | 0 | 1 | 1 | 0 | 0 | 0 | 0

## Slide 18: PVD process: thick films by long pulsed DCMS
Baking = 600°C for 48 hours
Temperature = 550 °C
Base pressure < 1 x 10-9 mbar
Magnetic Field = 830 Gauss
Current = 1 A
Grounded
Cu cavity
IR lamp
Nb cathode
Potential
Nb on Cu 6GHz cavity
Sputtering system for 6GHz cavities

## Slide 19: Thick Film morphology by EBSD
Cu
Courtesy of STFC (Reza Valizadeh)
Cav 21: 75 µm
500nm single layer thickness
Cu
Cav 16: 75 µm
500nm single layer thickness
Columnar growth
Larger grains

## Slide 20: RF characterization
Cavity inserted in cryostat in order to cool down
After cool down, Q vs Eacc is measured 4,2K and 1,8K.

## Slide 21: RF characterization
Chart: Cavity #23,0
Cav23 4.2 K | 23310000000 | 23500000 | 23500000 | 23600000 | 23100000 | 24200000 | 23000000 | 22900000 | 22400000 | 22300000 | 21700000 | 21400000 | 21400000 | 20300000 | 20200000 | 20000000 | 19700000 | 19400000 | 19000000 | 18600000 | 18500000 | 17800000 | 17600000 | 17400000 | 17100000 | 16900000 | 16800000 | 16900000 | 16600000 | 16800000 | 16600000 | 16600000 | 16400000 | 16400000 | 16100000 | 16100000
Nb_bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Nb_bulk 4.2K | 20745196 | 20272608 | 20117484 | 19659196 | 19508764 | 19359484 | 19211348 | 19064344 | 18918464 | 18630046 | 18487490 | 18487490 | 18066334 | 17928092 | 17790906 | 17519678 | 17385618 | 17385618
Nb Bulk @1,8K
Nb on Cu Thick film @1,8K
Nb on Cu Thick film @4,2K
Rres
Predominant @1,8K
Rbcs
Predominant @4,2K
See Vaglio’s lecture

## Slide 22: RF characterization @1,8K 6GHz
One shot mode:
Cav 9
Cav 3,1
Multilayer mode:
Cav 12
Cav 16
Cav 21

## Slide 23: RF characterization @1,8K 6GHz dependence of single pulse thickness
Chart: Eacc (MV/m)
Cav 8.1 100nm | 300000000 | 301000000 | 300000000 | 287000000 | 284000000 | 256000000 | 218000000 | 187000000 | 172000000 | 162000000 | 183000000 | 176000000 | 166000000 | 155000000 | 148000000 | 131000000 | 121000000 | 115000000 | 110000000 | 105000000 | 95900000 | 93100000 | 91000000 | 88100000 | 85000000 | 82000000 | 77700000 | 72500000 | 67900000 | 61200000 | 57700000 | 52100000 | 47900000 | 43800000 | 43600000
Cav 21 500nm | 768000000 | 773000000 | 774000000 | 778000000 | 780000000 | 782000000 | 782000000 | 784000000 | 785000000 | 785000000 | 781000000 | 780000000 | 780000000 | 781000000 | 782000000 | 781000000 | 784000000 | 780000000 | 774000000 | 773000000 | 769000000 | 764000000 | 769000000 | 767000000 | 768000000 | 771000000 | 772000000 | 773000000 | 776000000 | 779000000 | 779000000 | 781000000 | 781000000 | 783000000 | 786000000 | 725000000 | 727000000 | 728000000 | 729000000 | 729000000 | 148000000 | 140000000 | 130000000 | 126000000 | 122000000 | 115000000 | 106000000 | 101000000 | 92600000 | 84300000 | 76400000 | 69300000 | 45800000 | 30900000 | 23900000
Cav 16 500nm | 947000000 | 957000000 | 935000000 | 897000000 | 890000000 | 904000000 | 908000000 | 918000000 | 929000000 | 803000000 | 806000000 | 815000000 | 798000000 | 788000000 | 786000000 | 778000000 | 920000000 | 966000000 | 810000000 | 797000000 | 523000000 | 439000000 | 398000000 | 367000000 | 348000000 | 325000000 | 314000000 | 296000000 | 281000000 | 268000000 | 255000000 | 245000000 | 234000000 | 227000000 | 216000000 | 201000000 | 160000000 | 189000000 | 104000000 | 80900000
Nb Bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Nb Bulk

## Slide 24: RF characterization @1,8K 6GHz dependence of single pulse thickness
Chart: Eacc (MV/m)
Cav 8.1 100nm | 300000000 | 301000000 | 300000000 | 287000000 | 284000000 | 256000000 | 218000000 | 187000000 | 172000000 | 162000000 | 183000000 | 176000000 | 166000000 | 155000000 | 148000000 | 131000000 | 121000000 | 115000000 | 110000000 | 105000000 | 95900000 | 93100000 | 91000000 | 88100000 | 85000000 | 82000000 | 77700000 | 72500000 | 67900000 | 61200000 | 57700000 | 52100000 | 47900000 | 43800000 | 43600000
Cav 21 500nm | 768000000 | 773000000 | 774000000 | 778000000 | 780000000 | 782000000 | 782000000 | 784000000 | 785000000 | 785000000 | 781000000 | 780000000 | 780000000 | 781000000 | 782000000 | 781000000 | 784000000 | 780000000 | 774000000 | 773000000 | 769000000 | 764000000 | 769000000 | 767000000 | 768000000 | 771000000 | 772000000 | 773000000 | 776000000 | 779000000 | 779000000 | 781000000 | 781000000 | 783000000 | 786000000 | 725000000 | 727000000 | 728000000 | 729000000 | 729000000 | 148000000 | 140000000 | 130000000 | 126000000 | 122000000 | 115000000 | 106000000 | 101000000 | 92600000 | 84300000 | 76400000 | 69300000 | 45800000 | 30900000 | 23900000
Cav 16 500nm | 947000000 | 957000000 | 935000000 | 897000000 | 890000000 | 904000000 | 908000000 | 918000000 | 929000000 | 803000000 | 806000000 | 815000000 | 798000000 | 788000000 | 786000000 | 778000000 | 920000000 | 966000000 | 810000000 | 797000000 | 523000000 | 439000000 | 398000000 | 367000000 | 348000000 | 325000000 | 314000000 | 296000000 | 281000000 | 268000000 | 255000000 | 245000000 | 234000000 | 227000000 | 216000000 | 201000000 | 160000000 | 189000000 | 104000000 | 80900000
Nb Bulk 1.8K | 1567007620 | 1567007620 | 1579090820 | 1591267070 | 1603537280 | 1603537280 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1603537280 | 1603537280 | 1628362110 | 1640918270 | 1640918270 | 1640918270 | 1640918270 | 1653571330 | 1640918270 | 1640918270 | 1640918270 | 1628362110 | 1628362110 | 1628362110 | 1640918270 | 1628362110 | 1628362110 | 1615901950 | 1615901950 | 1591267070 | 1603537280 | 1591267070 | 1591267070 | 1591267070 | 1555016960 | 1531310340 | 1462336640 | 1293218050 | 1161363330 | 988354300 | 867363390 | 726898370
Nb Bulk
Systematically higher Q
and higher Eacc
Single pulse thickness 500nm

## Slide 25: Magnetic flux trapped study
Trapped magnetic flux
Increase Rres !!
)
instead of 1,8 (1,3GHz)
Martinello 2015, «Trapped flux surface resistance analysis for different surface treatments», Proceedings SRF2015, Whistler, Canada

## Slide 26: Magnetic flux trapped study
Chart: Eacc (MV/m)
| 1.613 | 1.6 | 1.74 | 1.99 | 2.2799999999999998 | 2.4700000000000002 | 3.22 | 3.41 | 3.42 | 3.73 | 4.0599999999999996 | 4.43 | 4.83 | 5.24 | 5.66 | 6.16 | 6.65 | 7.08 | 7.5 | 7.95 | 8.3800000000000008 | 8.82 | 9.2200000000000006 | 9.59 | 9.9700000000000006 | 10.4 | 10.8 | 11.2 | 11.5 | 11.8 | 12 | 12.2 | 12.3 | 12.4
0mG applied | 793900000 | 791000000 | 797000000 | 789000000 | 766000000 | 755000000 | 767000000 | 769000000 | 765000000 | 761000000 | 758000000 | 754000000 | 749000000 | 746000000 | 741000000 | 733000000 | 716000000 | 703000000 | 698000000 | 684000000 | 679000000 | 670000000 | 663000000 | 650000000 | 636000000 | 625000000 | 602000000 | 577000000 | 554000000 | 530000000 | 507000000 | 474000000 | 459000000 | 448000000
No Magnetic Field Applied | 526000000 | 526000000 | 535000000 | 544000000 | 548000000 | 561000000 | 574000000 | 589000000 | 590000000 | 595000000 | 600000000 | 599000000 | 605000000 | 647000000 | 615000000 | 608000000 | 605000000 | 599000000 | 592000000 | 586000000 | 595000000 | 587000000 | 562000000 | 538000000 | 540000000 | 534000000 | 507000000 | 490000000 | 509000000
50mG applied | 614900000 | 616000000 | 641000000 | 617000000 | 607000000 | 619000000 | 618000000 | 609000000 | 618000000 | 628000000 | 617000000 | 625000000 | 622000000 | 630000000 | 624000000 | 633000000 | 620000000 | 624000000 | 610000000 | 626000000 | 619000000 | 609000000 | 612000000 | 601000000 | 594000000 | 593000000 | 595000000 | 593000000 | 571000000 | 597000000 | 603000000 | 592000000 | 586000000 | 594000000 | 575000000 | 584000000 | 589000000 | 575000000 | 573000000 | 581000000 | 571000000 | 540000000 | 536000000 | 520000000 | 539000000 | 532000000 | 552000000 | 524000000 | 536000000 | 531000000 | 531000000 | 516000000 | 461000000 | 485000000
100mG applied | 626500000 | 622000000 | 606000000 | 608000000 | 597000000 | 586000000 | 582000000 | 583000000 | 582000000 | 578000000 | 564000000 | 571000000 | 561000000 | 553000000 | 543000000 | 533000000 | 517000000 | 508000000 | 500000000 | 475000000 | 440000000 | 405000000
180mG applied | 531200000 | 537000000 | 539000000 | 540000000 | 542000000 | 541000000 | 541000000 | 529000000 | 538000000 | 542000000 | 521000000 | 525000000 | 518000000 | 511000000 | 509000000 | 498000000 | 500000000 | 470000000 | 466000000 | 459000000 | 448000000 | 438000000 | 427000000 | 415000000 | 398000000 | 381000000 | 370000000 | 336000000 | 359000000 | 321000000
1.8K
6GHz
Niobium Bulk
180mG
100mG
50mG
No B applied
0mG (Compensation)
Nb04

## Slide 27: Magnetic flux trapped study
Nb on Cu
thin film
Chart: Eacc (MV/m)
Cav 39 0mG 02/07/2020 | 386400000 | 376000000 | 375000000 | 358000000 | 358000000 | 357000000 | 357000000 | 384000000 | 376000000 | 347000000 | 322000000 | 325000000 | 325000000 | 317000000 | 311000000 | 305000000 | 310000000 | 305000000 | 303000000 | 302000000 | 296000000 | 293000000 | 289000000 | 278000000 | 271000000 | 266000000 | 258000000 | 246000000 | 244000000 | 242000000 | 236000000 | 229000000 | 223000000 | 212000000 | 202000000 | 201000000 | 198000000 | 199000000 | 183000000 | 174000000 | 164000000 | 167000000 | 160000000 | 157000000 | 155000000 | 152000000 | 150000000
Cav 39 180mG 03/07/2020 | 362800000 | 361000000 | 358000000 | 355000000 | 345000000 | 346000000 | 341000000 | 338000000 | 335000000 | 331000000 | 335000000 | 325000000 | 318000000 | 312000000 | 306000000 | 296000000 | 289000000 | 278000000 | 266000000 | 258000000 | 250000000 | 244000000 | 238000000 | 228000000 | 215000000 | 207000000 | 199000000 | 189000000 | 172000000 | 159000000 | 154000000
Cav39 (No B applied) 17/07/2020 | 375600000 | 379000000 | 377000000 | 372000000 | 369000000 | 360000000 | 356000000 | 348000000 | 384000000 | 384000000 | 384000000 | 383000000 | 381000000 | 381000000 | 378000000 | 374000000 | 364000000 | 362000000 | 359000000 | 344000000 | 327000000 | 315000000 | 300000000 | 292000000 | 283000000 | 267000000 | 259000000 | 249000000 | 241000000 | 231000000 | 221000000 | 215000000 | 210000000 | 205000000 | 196000000 | 191000000 | 187000000 | 182000000 | 177000000 | 167000000 | 157000000 | 152000000
1.8K
6GHz
180mG
50mG
No B applied
0mG (Compensation)
Cu39

## Slide 28: Magnetic flux trapped study
Effect higher in Bulk Nb
Thick films effect?…
It is needed more statistic to confirm but this data indicates that Nb bulk cavities are more sensitive to magnetic field respect to thin film cavities, as expected
Chart: B applied (mG)
| 50 | 100 | 180
 | 1.4 | 0.95 | 0.92
 | 0.4 | 0.25

## Slide 29: Conclusions
Thick film is a promising approach in order to push the limits of the Nb on Cu cavities technology.
The effect of the surface preparation and single pulse thickness is fundamental for the cavity performance.
Magnetic flux trapped in 6GHz cavities study will include a thick film RF characterization.

## Slide 30
Thank you!