## Slide 1
EASITrain – European Advanced Superconductivity Innovation and Training. This Marie Sklodowska-Curie Action (MSCA) Innovative Training Networks (ITN) has received funding from the European Union’s H2020 Framework Programme under Grant Agreement no. 764879
Paola Mauceri
ASG Superconductors
Development of Superconducting MgB2 Wires
Student Workshop on Superconductivity and Applications

## Slide 2: Outline
Why MgB2?
MgB2 application matrix
ASG Superconductors company
Columbus MgB2 Unit
MgB2 production process
MgB2 wires production process
MgB2 wires quality control
MgB2 wire configurations
Conclusion

## Slide 3: Why MgB2?
Nagamatsu et al. 2001
Superconductivity at 39K in magnesium diboride
Nature 410 63-4
Simple composition and structure:
2 elements
Hexagonal crystal structure
Graphite type structure
Relatively high Tc
High critical field
Iwasa Y et al. 2006
A round table discussion on MgB2:
towards a wide market or a niche production?
IEEE Trans. Appl. Supercond 16 1457-64

## Slide 4: Why MgB2?
Zeng et al. 2003
Superconducting MgB2 thin film on silicon carbide substrate by HPCVD
APL 82 2097-9
Large critical current density
Compound | Mass density
Copper | 8,96 g/cm3
NbTi | 6 g/cm3
Nb3Sn | 5,4 g/cm3
YBCO | 6,35 g/cm3
BSCCO-2223 | 6,5 g/cm3
MgB2 | 2,6 g/cm3
Low density
Low material cost
PIT process for wire fabrication
MgB2-based systems could be cooled by modern cryocooling devices

## Slide 5: MgB2 Powder SEM Image
Hexagonal structure

## Slide 6: MgB2 application matrix
 | cables | Rotating machines (motors/ generators) | magnets | Fault current limiters | Energy storage devices
Medical |  |  |  |  | 
Electricity/ grid |  |  |  |  | 
Industrial |  |  |  |  | 
Aircraft/ aerospace |  |  |  |  | 
Energy generation |  |  |  |  | 
Naval |  |  |  |  | 
Notes: 2005
MRO - First MRI open space system , cryogen free , with MgB2conductor
2010 to date
The development of the second leg
IBA - one of two commercial systems for proton therapy utilizing a high field cryogen free system
MRO Rotating - first prototypes for Image Guided Therapy, SC magnets cryogen free that can be moved during operation
UHF MRI
We are also trying hard to introduce SC solutions in a very conservative industry :Energy transportation
SMES
FCL – we are close to install in UK the first induction system at 33 KV with MgB2 conductor

## Slide 8: Columbus MgB2 Unit
Round wires
MRO
MRI

## Slide 9: MgB2 Production Processes
B
Mg
B
Mg
IN-SITU
EX-SITU
MgB2

## Slide 10: MgB2 Production Processes
In-situ
Low cost
High speed process
Ex-situ
Easier process
Homogeneity over long length
Control of the powder granulometry and purity
Easier insertion of doping
Advantages

## Slide 11: MgB2 Production Processes
In-situ
Inhomogeneity over long length
Need of inert sheaths
Ex-situ
Need of hard sheath materials
Disadvantages
More flexible and reliable method!!!

## Slide 12: MgB2 Wires Production Process

## Slide 13: MgB2 Wires Production Process
4 meter furnace for annealing HT
20 m long in-line furnace
Powders clean synthesis
Multistep drawing machine
High power straigth drawing machine
Multistep rolling machine

## Slide 14: MgB2 Wires Quality Control (ISO 9001:2008)
Structure characterization
XRD
SEM and EDS

## Slide 15: MgB2 Wires Quality Control (ISO 9001:2008)
Chart: Temp. = 20 K Field = 0.50 T
Requirement | -2.9205e-07 | 1e-05
Tests parameters range
Field: 0 – 1.8 T
Temperature: 20 – 30 K
Current: 0 – 1000 A
Current transport measurement

## Slide 16: MgB2 Wires Quality Control (ISO 9001:2008)
Sample
Chart: Resistance vs Temperature
Chart: 
Residual-resistance ratio (RRR) and Tc Test

## Slide 17: MgB2 Wire Configurations
Dimension: 3,67 mm x 0,65 mm
12 filaments
Materials: Ni, Iron, Copper
FF: 11%
Diameter: d = 1.33mm
36 filaments
Materials: Monel, Ni
FF: 17%
Diameter: d = 1mm
37 filaments
Materials: Monel, Ni
FF: 14%
Dimension: 2mm x 1mm
6 filaments
Materials: Monel, Ni
FF: 29%
Round Wires
Tapes

## Slide 18: MgB2 Round Wires
Final configuration
Diameter: 0.93mm
37 filaments
Materials: Monel, Ni, Nb
FF: 11.5%
Copper-Tin electrodeposition

## Slide 19: MgB2 Tapes for MRI
Updated wire layout:
12 filaments
Improved fabrication process
Unit piece length 4.0 Km
Synthesis in controlled atmosphere
Wire layout in 2006:
14 filaments
Unit piece length 1.6 Km
MROpen

## Slide 20: Conclusion
MgB2 as a SC material, allow to produce high quality superconducting wires for the LHC.
Ex-situ PIT technique has been industrially implement in the new Columbus plant
Several wire configurations have been developed in the last years
MgB2 tapes are an optimal solution for the magnets development of MRI machines.
ASG Superconductors is working in innovative projects that are exploring the opportunity to implement MgB2 SC technology in many applications such as energy transmission, generation and storage