## Slide 1
Status of task 17.3 and publications on Shocks and Vibrations
Lorenzo Peroni (POLITO)
2nd Annual Meeting of Aries WP17

## Slide 2: Task 3 description
Task 3: Dynamic testing and online monitoring
  Testing of material samples in a broad range of environments:
  Mechanical testing in quasi-static and dynamic conditions, at various temperatures
  Tests under very high power laser and particle beams
  Irradiation tests with online monitoring of properties evolution
  Hydrodynamic simulations of experiments - constitutive models, spall strengths for new materials
  Participants: CERN, ELI-NP, GSI, POLIMI, POLITO

## Slide 3: Milestones



## Slide 4: Deliverables

## Slide 5: Task 17.3 – Material Testing: Irradiation at GSI UNILAC
Assessment of radiation damage to graphitic materials induced by 4.8 MeV/u Ca ions: electrical resistivity and coating microscopy analysis
Irradiation test (TNA) in March/April 2019 on coated and bare samples at DPA levels comparable to end-of-life HL-LHC. Examination started already ~2 months later thanks to low residual dose
Electrical Resistivity
  DC measurements with the 4-probe method and multi-layer model Bulk resistivity increasing faster in more ordered materials; MoGr with fibres more radiation resistant
  Coatings resistivity worsening significantly less in pulsed- mode (HIPIMS) compared to DC-mode (DCSM)
FIB-SEM investigation of Mo coating/bulk interface
  Columnar and dense structure kept after irradiation
  The coating-bulk interface is continuous, no evidence of coating detachment; no cracks
Pristine
Irradiated at max DPA

## Slide 6: Task 17.3 – Material Testing: Irradiation at GSI UNILAC
Assessment of hardening of graphitic materials (3 Graphites grades, 2 suppliers) induced by 4.8 MeV/u Au ions (early 2020) by quasi-static and dynamic techniques
Microindentation
  Young‘s modulus rises up to 300 %
Dynamic hardness test
  indenter accelerated towards sample surface with a constant force
  strain rates at the surface ~ 104 s-1
  observation of velocity and penetration on the surface; differences between grades detected
  calculation of dynamic hardness

## Slide 7: Task 17.3. Material Testing: FlexMat @ HiRadMat
Aim: Testing of dynamic response of target and beam dump materials to proton beam impact
Since last reporting: detailed analysis of response of different graphitic materials at high strain rates-using Ta core drivers
Short-pulse 440 GeV proton beam impact on Tantalum cores embedded in different graphitic shells
Identification of beam-induced radial & axial pressure waves
Extraction of material parameters in dynamic loading conditions with FE simulations
Identified load limits for failure of the graphitic shells by deviation from monotonic increase with increasing energy deposition density
Radial wave
Axial wave

## Slide 8: Task 17.3 – Material Testing: MultiMat @ HiRadMat
Post-processing of MultiMat acquired data and comparison to advanced simulations ongoing (CERN, POLITO, UOM):
In general good agreement, particularly for isotropic materials
Elastic constants of several materials updated (e.g. CFC, CuCD)
Role and extent of internal damping assessed
Some unexpected failures (SiC and TZM) analyzed and (partly) explained

## Slide 9: Task 17.2 and 17.3 – Highlights
X-ray tomography
Nanoimpact with varying Strain Rate depending on impact parameters
Raman spectroscopy
Nanoindentation, nanoimpact
Fatigue testing
Creep
Poisson ratio measurements
Laser Flash analysis
Thermomechanical analysis
X Ray Diffraction
GSI
2D CFC
POCO Foam
Isotropic graphite
8 µm grains -SGL
Isotropic graphite
1 µm grains-POCO

## Slide 10: Special Issue

## Slide 11: Only 3 submitted papers…
Shockwave propagation in particle accelerator scenarios
Martina Scapin
Submitted 2019/12/09
Editor assigned, reviewers invited
Dynamic Response of Graphitic Targets with Tantalum Cores Impacted by Pulsed 440-GeV Proton Beams
Pascal Simon, Philipp Drechse, Peter Katrik, Kay-Obbe Voss, Philipp Bolz, Fiona J. Harden, Michael Guinchard, Yacine Kadi, Christina Trautmann, Marilena Tomut
Submitted 2020/06/14
Editor assigned, reviewers invited
Thermomechanical Characterisation of Copper Diamond and Benchmarking with the MultiMat experiment
Nicholas J. Sammut, Pierluigi Mollicone, Michele Pasquali, Federico Carra, Alessandro Bertarelli, Jorge Guardia Valenzuela, Oscar Sacristan De Frutos, Marcus Portelli,
Submitted 2020/07/08
All the submitted papers have at least one of the authors which is also a guest editor for the SI