## Slide 1: Updates on BLIP irradiation tests and RaDIATE activities
N. Solieri
Under the supervision of M. Calviani
On behalf of the RaDIATE collaboration

## Slide 2: Outline
Radiation damage in Beam Impacted Devices (BIDs)
    Material R&D approaches for BIDs at different time-scales
    The RaDIATE collaboration
BLIP Irradiations
    BNL’s BLIP facility
    Organization of an irradiation at BLIP and subsequent PIE
    An overview of the irradiations that we have launched
    The CERN2 capsule
An overview of some of the other RaDIATE activities
    BeGrid2 (HRMT43) organization and subsequent PIE (K. Ammigan, FNAL)
    Fatigue testing of Ti alloys for FNAL beam windows (S. Bidhar, FNAL)
    Ti-base alloy tensile testing and microscopy (D. Senor, PNNL)
    Radiation damage effects in Be (S. Kuksenko, UKAEA)
    Development of ANSYS scripts for the implementation of radiation damage data (N. Solieri, CERN)

## Slide 3: Material R&D studies for BIDs
Data from material studies for nuclear reactors poorly translate to BID scenarios  Need own material R&D
TIMESCALE
ns / µs
months / years
HiRadMat
2 Courtesy E. Fornasiere, in collaboration with Framatome GmbH
Characterization of the dynamic response of the materials/prototypes under proton beam impact. No relevant radiation damage produced
1Courtesy C. Torregrosa
1

## Slide 4: Material R&D studies for BIDs
Data from material studies for nuclear reactors poorly translate to BID scenarios  Need own material R&D
TIMESCALE
ns / µs
months / years
HiRadMat
Post-mortem irradiation examination
BLIP Irradiations
2 Courtesy E. Fornasiere, in collaboration with Framatome GmbH
Characterization of the dynamic response of the materials/prototypes under proton beam impact. No relevant radiation damage produced
Opening of a spent AD-Target after 7 years of irradiation
1Courtesy C. Torregrosa
1
2
Several small samples for material testing enclosed in welded stainless steel capsules (Ø70 mm, 5 mm thick)

## Slide 5: Material R&D studies for BIDs
Data from material studies for nuclear reactors poorly translate to BID scenarios  Need own material R&D
TIMESCALE
ns / µs
months / years
HiRadMat
Post-mortem irradiation examination
BLIP Irradiations
2 Courtesy E. Fornasiere, in collaboration with Framatome GmbH
Characterization of the dynamic response of the materials/prototypes under proton beam impact. No relevant radiation damage produced
Opening of a spent AD-Target after 7 years of irradiation
1Courtesy C. Torregrosa
1
2
Several small samples for material testing enclosed in welded stainless steel capsules (Ø70 mm, 5 mm thick)
WE CAN ALSO COMBINE THE TWO APPROACHES (BeGrid2)

## Slide 6
Broad aims are threefold:
to generate materials data for accelerator and fission/fusion communities
Bring together HEP and nuclear fusion/fission materials research communities
to initiate a continuing synergy between research in these communities, benefitting both proton accelerator applications in science and industry and carbon-free energy technologies
5th in-person collaboration meeting held at CERN in Dec. 2018

## Slide 7: Irradiations at BLIP
BLIP – Brookhaven Linear Isotope Producer at BNL
1Courtesy K. Ammigan
Material irradiation in tandem and upstream of isotope targets:
  Primary proton energy: up to 200 MeV
  RaDIATE Target array needs to be optimized for each run to deliver a beam that is appropriate for isotope production
  POT ~ 1E21
  Peak DPA: 0.88 (Ta2.5W, CERN2 capsule), 1.2 (Ir, HighZ capsule)
  Rastered beam profile to achieve more constant irradiation profile
  Irradiation length O(months)
1
RaDIATE Targets
Isotope Targets
2
2Courtesy J. Canhoto
Objectives:
  Evaluate radiation damage effects from high-energy protons in various accelerator materials:
      Beam windows, Secondary particle production targets, Beam dumps
  Perform PIE activities to characterize property changes due to proton irradiation damage
      Strength (tensile, bend, fatigue)
      Thermal (CTE,conductivity)
      Annealing effects and microstructure (SEM, TEM, EBSD)

## Slide 8: Organization of an irradiation at BLIP and subsequent PIE
Definition of irradiation run aims and target assembly
FLUKA Studies
ANSYS Studies
Comparison with the conditions achieved in the BID and BNL proton energy budget
1Courtesy K. Ammigan

## Slide 9: Organization of an irradiation at BLIP and subsequent PIE
Definition of irradiation run aims and target assembly
Capsule and material specimens fabrication
FLUKA Studies
ANSYS Studies
Comparison with the conditions achieved in the BID and BNL proton energy budget
EBW
Capsule Cover
Filling with specimens
1Courtesy K. Ammigan

## Slide 10: Organization of an irradiation at BLIP and subsequent PIE
Shipment of capsule to BNL and installation in the beamline
Definition of irradiation run aims and target assembly
Capsule and material specimens fabrication
FLUKA Studies
ANSYS Studies
Comparison with the conditions achieved in the BID and BNL proton energy budget
EBW
Capsule Cover
Filling with specimens
Capsule fitted in
capsule holder
Basket assembly
(2.5 mm water gap)
Target box assembly
1
1Courtesy K. Ammigan

## Slide 11: Organization of an irradiation at BLIP and subsequent PIE
Shipment of capsule to BNL and installation in the beamline
Irradiation and subsequent cooldown – O(year)
Definition of irradiation run aims and target assembly
Capsule and material specimens fabrication
FLUKA Studies
ANSYS Studies
Comparison with the conditions achieved in the BID and BNL proton energy budget
EBW
Capsule Cover
Filling with specimens
Capsule fitted in
capsule holder
Basket assembly
(2.5 mm water gap)
Target box assembly
CERN2 Capsule: Computed dose sum @ 1m after 18 months cooldown ~4 mSv/h
1
1Courtesy K. Ammigan

## Slide 12: Organization of an irradiation at BLIP and subsequent PIE
Shipment of capsule to BNL and installation in the beamline
Irradiation and subsequent cooldown – O(year)
Definition of irradiation run aims and target assembly
Capsule and material specimens fabrication
FLUKA Studies
ANSYS Studies
Comparison with the conditions achieved in the BID and BNL proton energy budget
EBW
Capsule Cover
Filling with specimens
Capsule fitted in
capsule holder
Basket assembly
(2.5 mm water gap)
Target box assembly
CERN2 Capsule: Computed dose sum @ 1m after 18 months cooldown ~4 mSv/h
PIE ACTIVITIES
1
1Courtesy K. Ammigan

## Slide 13: Organization of an irradiation at BLIP and subsequent PIE
Shipment of capsule to BNL and installation in the beamline
Irradiation and subsequent cooldown – O(year)
Definition of irradiation run aims and target assembly
Capsule and material specimens fabrication
FLUKA Studies
ANSYS Studies
Comparison with the conditions achieved in the BID and BNL proton energy budget
EBW
Capsule Cover
Filling with specimens
Capsule fitted in
capsule holder
Basket assembly
(2.5 mm water gap)
Target box assembly
CERN2 Capsule: Computed dose sum @ 1m after 18 months cooldown ~4 mSv/h
PIE ACTIVITIES
CERN2 Capsule  Design started in second half of 2017
PIE on some of the specimens will take place during 2020
1
1Courtesy K. Ammigan

## Slide 14: An overview of the BLIP irradiation runs we launched
POT: 1.03E21
Peak DPA: 2.75 (Ir)
Max Tirr: ~850 °C
CuCrZr, TZM  SPS Int. Dump
Ir  AD-Target
Capsule currently at PNNL
Opening will take place in the coming weeks
PIE  4-point bending test
A previous capsule suffered catastrophic damage and all the specimens were destroyed
High-Z Capsule

## Slide 15: An overview of the BLIP irradiation runs we launched
CERN2 Capsule
POT: 1.03E21
Peak DPA: 2.75 (Ir)
Max Tirr: ~850 °C
CuCrZr, TZM  SPS Int. Dump
Ir  AD-Target
Capsule currently at PNNL
Opening will take place in the coming weeks
PIE  4-point bending test
A previous capsule suffered catastrophic damage and all the specimens were destroyed
POT: 2.8E21
Peak DPA: 4.77 (Ta)
Max Tirr: ~230 °C
Capsule currently at BNL
Opening was scheduled for end of Mar-Apr. 2020 @ Framatome
Restart of activities being planned in collaboration with BNL
PIE  Coating visual inspection, adhesion test, 4-point bend test
Mo-Coated MoGr and CFC  HiLumi Collimators
Monocr. Si  SPS Dump
High-Z Capsule

## Slide 16: An overview of the BLIP irradiation runs we launched
CERN2 Capsule
POT: 1.03E21
Peak DPA: 2.75 (Ir)
Max Tirr: ~850 °C
CuCrZr, TZM  SPS Int. Dump
Ir  AD-Target
Capsule currently at PNNL
Opening will take place in the coming weeks
PIE  4-point bending test
A previous capsule suffered catastrophic damage and all the specimens were destroyed
POT: 2.8E21
Peak DPA: 4.77 (Ta)
Max Tirr: ~230 °C
Mo-coated MoGr and Gr7550  HiLumi Collimators
Capsule construction under way at CERN
Irradiation was scheduled to take place in May 2020, now scheduled for second half of 2020
Capsule currently at BNL
Opening was scheduled for end of Mar-Apr. 2020 @ Framatome
Restart of activities being planned in collaboration with BNL
PIE  Coating visual inspection, adhesion test, 4-point bend test
Mo-Coated MoGr and CFC  HiLumi Collimators
Monocr. Si  SPS Dump
High-Z Capsule
CERN3 Capsule (CERN/FNAL)
POT: 7.5E21 (expected)
Max Tirr: ~170 °C (CERN specimens)

## Slide 17: An overview of some of the other RaDIATE activities

## Slide 18: BeGrid2 (HRMt43) - Organization
Objectives 
Very complex coordination between BNL, FNAL, PNNL and CERN for handling of highly radioactive samples
Real-time measurement of dynamic thermo-mechanical response of graphite specimens in an effort to benchmark numerical simulations
Completed in Oct. 2018
Identify thermal shock response differences between non-irradiated and previously
proton-irradiated specimens from BNL BLIP:
        (Be, C, Ti-alloys, Si, SiC-coated C)
Explore novel materials such as:
      Metal foams (C, SiC)
      Electrospun fiber mats (Al2O3, ZrO2)
First and unique tests with
pre-activated materials at HiRadMat
K. Ammigan (FNAL)

## Slide 19: BeGrid2 (HRMt43) - Organization
Objectives 
Very complex coordination between BNL, FNAL, PNNL and CERN for handling of highly radioactive samples
Real-time measurement of dynamic thermo-mechanical response of graphite specimens in an effort to benchmark numerical simulations
Completed in Oct. 2018
Identify thermal shock response differences between non-irradiated and previously
proton-irradiated specimens from BNL BLIP:
        (Be, C, Ti-alloys, Si, SiC-coated C)
Explore novel materials such as:
      Metal foams (C, SiC)
      Electrospun fiber mats (Al2O3, ZrO2)
First and unique tests with
pre-activated materials at HiRadMat
K. Ammigan (FNAL)

## Slide 20: Fatigue testing of Ti alloys for FNAL T2K beam window (1/2)
FNAL custom-made Bending Fatigue tester
Cyclic load frequency of 15 Hz
Stress range of 375MPa - 1250 Mpa
Automatically stops when sample cracks
Ti Grade 5 and 23 tested
Testing completed in Feb 2020
Ti specimens in BLIP capsule
BLIP capsule in capsule holder
BLIP irradiation – dose map (DPA) on Ti specimens
T2K’s Ti beam window subjected to thermal shock-induced load cycles AND long-term proton beam irradiation damage
Ti bend specimens for fatigue testing
S. Bidhar (FNAL)

## Slide 21: Fatigue testing of Ti alloys for FNAL T2K beam window (2/2)
Similar slope between irradiated and
un-irradiated specimens but decrease in the fatigue life for a given stress amplitude

## Slide 22: Ti-base alloys tensile testing and microscopy
Distinct radiation hardening observed for each of the analyzed Ti grades
D. Senor (PNNL)

## Slide 23: Radiation damage effects in Be
S. Kuksenko (UKAEA)
NuMI beam window:
  120 GeV proton beam
  1.57×1021 protons during its lifetime
  Up to 0.5 dpa
  T ≈ 50ºC
Significant hardening is observed in the p-irradiated beryllium even at 0.1 dpa
Hardening increases with irradiation to higher doses (at least up to 0.5 dpa)
Hardness of the irradiated beryllium is less anisotropic

## Slide 24: Development of ANSYS scripts for the implementation of radiation damage data
We need a way to easily implement the radiation damage to material properties data accumulated through the BLIP irradiations into ANSYS Workbench for the assessment of our devices
Importation of FLUKA-generated DPA map into ANSYS and its scaling to integrated intensity
Discretization into N DPA levels and generation of N corresponding materials
Implementation of law of degradation of material property with respect to DPA:
        Thermal conductivity/expansion
        Hardening
        …
Assignment of material to element depending on DPA value at element centroid coordinates
Only adds a couple of minutes of computation time for typical size-models
Already available for XYZ and RPZ binning
N. Solieri (CERN)

## Slide 25: Example – Th. Conductivity Degradation in first block of K12 TAX
What would happen to the thermal conductivity of the C10300 in the first TAX block after 4 years of 4x intensity BD mode (integrated intensity 2.4E19)?
1Courtesy A. Ciccotelli
2M. Eldrup, N. Singh, Influence of composition, heat treatment and neutron irradiation on the electrical conductivity of copper alloys
1
2
APDL Script
24% peak reduction in Th. Cond!

## Slide 26: Conclusions & future outlook
Proton-beam-induced radiation damage to materials is one of the main challenges in the design, operation of current and future BIDs
BLIP Irradiations: assessing long-term radiation damage on materials that we employ in BIDs
Two capsules will be opened during 2020:
    High-Z Capsule  CuCrZr, TZM (SPS Internal Dump), Ir (AD-Target)
    CERN2 Capsule  Mo-coated MoGr and CFC (HiLumi collimators)
A new irradiation is scheduled for 2020:
    CERN3 Capsule  Mo-coated MoGr and Gr7550 (HiLumi collimators)
Plenty of results coming from RaDIATE work packages in the coming months

## Slide 27: BACKUP SLIDES

## Slide 28: Microscopic radiation damage effects
Three main effects of irradiation on the microstructure of structural materials:
  Structural changes from displacement and rearrangement of atoms
      Creation of vacancies and self-interstitials (and their recombination or clustering)
      Growth of cavities (swelling), climb of dislocations (creep), microvoids
      …
  Kinetic effects  Radiation Enhanced Diffusion, Segregation and Precipitation (RED, RIS, REP)
  Transmutation  Production of new atomic species. Production cross sections are highest for light transmutants (H, He)
      Displacement cross section σdpa Above 20 MeV (for Fe) only very slightly increases with energy
      H and Helium production cross section σα  Continuously increasing with energy
Irradiation Source | DPA rate (DPA/s) | He gas production (appm/DPA) | Irradiation Temp (˚C)
Mixed spectrum fission reactor | 3 x 10-7 | 1 x 10-1 | 200-600
Fusion reactor | 1 x 10-6 | 1 x 101 | 400-1000
High energy proton beam | 6 x 10-3 | 1 x 103 | 100-800
1
1P. Hurh
Notes:       Radiation Enhanced Diffusion (RED)  Caused by the increased concentration of vacancies and the additional presence of self-interstitials
      Radiation Induced Segregation (RIS)  Due to flux of defects to sinks
      Radiation Enhanced Precipitation (REP) 

## Slide 29: Microscopic radiation damage effects
Three main effects of irradiation on the microstructure of structural materials:
  Structural changes from displacement and rearrangement of atoms
      Creation of vacancies and self-interstitials (and their recombination or clustering)
      Growth of cavities (swelling), climb of dislocations (creep), microvoids
      …
  Kinetic effects  Radiation Enhanced Diffusion, Segregation and Precipitation (RED, RIS, REP)
  Transmutation  Production of new atomic species. Production cross sections are highest for light transmutants (H, He)
      Displacement cross section σdpa Above 20 MeV (for Fe) only very slightly increases with energy
      H and Helium production cross section σα  Continuously increasing with energy
Irradiation Source | DPA rate (DPA/s) | He gas production (appm/DPA) | Irradiation Temp (˚C)
Mixed spectrum fission reactor | 3 x 10-7 | 1 x 10-1 | 200-600
Fusion reactor | 1 x 10-6 | 1 x 101 | 400-1000
High energy proton beam | 6 x 10-3 | 1 x 103 | 100-800
1
1P. Hurh
Effects from low energy neutron irradiations do not equal effects from high energy proton irradiations (transmutation)
Notes:       Radiation Enhanced Diffusion (RED)  Caused by the increased concentration of vacancies and the additional presence of self-interstitials
      Radiation Induced Segregation (RIS)  Due to flux of defects to sinks
      Radiation Enhanced Precipitation (REP) 

## Slide 30: Radiation damage effects on macroscopic material properties
Dimensional Change and associated reduction of density
Reduction of thermal/electrical conductivity and thermal expansion
Hardening and embrittlement
                Loss of ductility
                Hardening
                Reduction of fracture toughness, change of fracture mode from ductile to brittle
                Irradiation embrittlement  Mostly due to pinning of dislocations by irradiation induced dislocation loops, precipitates, cavities or bubbles
                H and He embrittlement
                Accelerated corrosion
1
1K. Whittle, Radiation Damage, Ch.2
2M. Li, S. J. Zinkle, Physical and Mechanical Properties of Copper and Copper Alloys, Comprehensive Nuclear Materials, vol.4 (2012)
2
E.g. SS316

## Slide 31: Radiation damage effects on macroscopic material properties
Dimensional Change and associated reduction of density
Reduction of thermal/electrical conductivity and thermal expansion
Hardening and embrittlement
                Loss of ductility
                Hardening
                Reduction of fracture toughness, change of fracture mode from ductile to brittle
                Irradiation embrittlement  Mostly due to pinning of dislocations by irradiation induced dislocation loops, precipitates, cavities or bubbles
                H and He embrittlement
                Accelerated corrosion
1
1K. Whittle, Radiation Damage, Ch.2
2M. Li, S. J. Zinkle, Physical and Mechanical Properties of Copper and Copper Alloys, Comprehensive Nuclear Materials, vol.4 (2012)
2
E.g. SS316
Thermo-mechanical response of BIDs heavily depend on material properties, but material properties heavily dependent upon Radiation Damage

## Slide 32: The CERN2 capsule
Stainless steel welded capsule containing:
  40x Ta2.5W specimens (BDF Target)
  20x Monocrystalline Si specimens (SPS Int. Dump)
  4x Mo-coated CFC specimens (HiLumi Collimators)
  4x Mo-coated MoGr specimens
  Panasonic graphite foils
  Graphite fillers
Capsule Ø70 mm, 5 mm thick
1
1Courtesy I. Lamas
2A. Waets, FLUKA simulations on residual gas production in IR7 collimators, ColUSM 20/09/2019
2
TCSPM Prototype

## Slide 33: Scope of the Contract – Baseline activities
        Shipment of the capsule to the contractor’s facility (Capsule currently at BNL, USA)
        Opening of the capsule:
          Preparation of opening procedure. Evaluation of applicability of opening procedure when the CERN2 irradiated capsule is unloaded in the hot cell
          Validation of opening procedure on spare CERN2 capsule supplied by CERN
          Extraction of the specimens by means of vacuum tweezers
          Sorting and storage of the specimens
        PIE activities:
          Visual inspection on 4 Mo-coated MoGr and 4 Mo-coated CFC specimens
          Test adhesion of the coating on 2 Mo-coated MoGr specimens
        Transport of all the specimens from contractor’s facilities to CERN
CERN rules 
Technical specification for the activities
    Tendering procedure for companies who have experience in the field
        Awarding of contract: Framatome GmbH (DE)

## Slide 34: Scope of the Contract – Baseline activities
        Shipment of the capsule to the contractor’s facility (Capsule currently at BNL, USA)
        Opening of the capsule:
          Preparation of opening procedure. Evaluation of applicability of opening procedure when the CERN2 irradiated capsule is unloaded in the hot cell
          Validation of opening procedure on spare CERN2 capsule supplied by CERN
          Extraction of the specimens by means of vacuum tweezers
          Sorting and storage of the specimens
        PIE activities:
          Visual inspection on 4 Mo-coated MoGr and 4 Mo-coated CFC specimens
          Test adhesion of the coating on 2 Mo-coated MoGr specimens
        Transport of all the specimens from contractor’s facilities to CERN
CERN rules 
Technical specification for the activities
    Tendering procedure for companies who have experience in the field
        Awarding of contract: Framatome GmbH (DE)
Project delayed due to COVID but now on track to completion during 2020