## Slide 1
New results on beam-induced color centers in nitrogen containing diamonds
P. Simon, M. Tomut (GSI) D. Grech, M. Kitzmantel (RHP)
2nd Annual Meeting of ARIES WP17

## Slide 2: Recap of 1st Annual Meeting in Malta
Measured first iono-luminescence (IL) spectra in 2018 on Diamond/Titanium-matrix composites:
Raman/PL measurements on composites is not straight forward:
NV-
NV0
N-clusters
pristine
1E11
1E12
1E13

## Slide 3: Recap of 1st Annual Meeting in Malta
NV-
NV0
N-clusters
Measured first iono-luminescence (IL) spectra in 2018 on Diamond/Titanium-matrix composites:
Raman/PL measurements on composites is not straight forward:
New IL measurements with improved SNR during 2019 & 2020 beamtimes
pristine
1E11
1E12
1E13
Measurements on irradiated monocrystals with the same characteristics

## Slide 4: Irradiation campaigns 2019 & 2020
Irradiation with 4.8 MeV/n 48Ca and 197Au
Beamtime 2019 (composites & yellow diamonds):
  Improved IL measurements with peltier-cooled moving-grating CCD spectrometer (up to 5⋅1013 i/cm2)
    Sensitivity beyond beam diagnostic cameras
  In-situ FT-IR measurements (up to 5⋅1013 i/cm2)
  First irradiation of monocrystalline diamonds (irregular geometry)
Beamtime 2020 (composites, CVD diamonds & yellow diamonds):
  IL with fast CCD spectrometer and on-line flux measurement
  In-situ UV/c absorption spectroscopy at 50 K and RT
  Irradiation of monocrystalline diamonds with regular geometry

## Slide 5: Irradiation campaigns 2019 & 2020
Irradiation with 4.8 MeV/n 48Ca and 197Au
Beamtime 2019 (composites & yellow diamonds):
  Improved IL measurements with peltier-cooled moving-grating CCD spectrometer (up to 5⋅1013 i/cm2)
    Sensitivity beyond beam diagnostic cameras
  In-situ FT-IR measurements (up to 5⋅1013 i/cm2)
  First irradiation of monocrystalline diamonds (irregular geometry)
Beamtime 2020 (composites, CVD diamonds & yellow diamonds):
  IL with fast CCD spectrometer and on-line flux measurement
  In-situ UV/c absorption spectroscopy at 50 K and RT
  Irradiation of monocrystalline diamonds with regular geometry

## Slide 6: IL + FT-IR measurements 2019
In-situ FT-IR:
  Thermo Fisher Nicolet 6700
  2 cm-1 resolution
On-line iono-luminescence:
  Horiba iHR320
  Integration time: 5-120 s
spectrometer
optical
camera

## Slide 7: Iono-luminescence

## Slide 8: Iono-luminescence Spectrum
No nitrogen-related ZPLs!
  [N-V-N]: 502 nm
  NV0: 575 nm
  NV-: 638 nm
NV- ZPL
1×1011 ions/cm2
NV0 ZPL
N-V-N ZPL
ZPL: zero-phonon line
PSB: phonon sideband
HPHT: High pressure / high temperature

## Slide 9: Iono-luminescence Spectrum
No nitrogen-related ZPLs!
Broad bands:
  500 – 650 nm
    [N-V-N] PSB?
    Intrinsic „A“ radiation band?
  650 – 800 nm
    NV- PSB?
NV- PSB
NV- ZPL
1×1011 ions/cm2
NV0 ZPL
H3 [N-V-N] PSB?
„A“ rad. Band?
NV0 ZPL
N-V-N ZPL
ZPL: zero-phonon line
PSB: phonon sideband
HPHT: High pressure / high temperature

## Slide 10: Iono-luminescence Spectrum
No nitrogen-related ZPLs!
Broad bands:
  500 – 650 nm
    [N-V-N] PSB?
    Intrinsic „A“ radiation band?
  650 – 800 nm
    NV- PSB?
ZPLs:
  ~690 nm
    Al2O3 (nat. oxide layer on sample holder)
  ~884 nm
    Nickel-related (precursor during HPHT)
NV- PSB
NV- ZPL
1×1011 ions/cm2
NV0 ZPL
ZPL: zero-phonon line
PSB: phonon sideband
HPHT: High pressure / high temperature
H3 [N-V-N] PSB?
„A“ rad. Band?
NV0 ZPL
N-V-N ZPL

## Slide 11: Iono-luminescence Spectra Evolution
Evolution of ZPL at ~500 nm
  H3 [N-V-N]: 503.2 nm
  3H (intrinsic): 503.4 nm
Strong decrease of integrated IL signal
Possible ZPLs at ~590, ~660 & 760 nm → No clear identification possible
1×1011 ions/cm2 1x
1×1012 5x
5×1012 20x
3×1013 15x
H3 ZPL?
NV- PSB
Al2O3

## Slide 12: Integrated IL signal
Exponential decay of IL sigal with increasing fluence
Only 5% of initial signal preserved at final fluence
  Close to detection limit of spectrometer
No significant contribution of beam-induced defects
beam off (2 h)
H3 / 3H

## Slide 13: Integrated IL signal
Exponential decay of IL sigal with increasing fluence
Only 5% of initial signal preserved at final fluence
  Close to detection limit of spectrometer
No significant contribution of beam-induced defects
... And what about transmission?
beam off (2 h)
H3 / 3H
1×1011
1×1012
5×1012
1×1013 ions/cm2
5 mm
After irradiation with 4.8 MeV/n 197Au:

## Slide 14: IL signal / composite vs. monocrystal
TiCD / 4.8 MeV/n 197Au
1×1011 ions/cm2
Commercially available (10-100 €/pc., up to 3x3x1 mm) HPHT diamonds with ~200 ppm Ns
Measurements with new (fast) CCD spectrometer set-up
Good agreement between old & new IL set-up!
Monocrystals behave virtually identical to composites!

## Slide 15: IL signal / composite vs. monocrystal
beam off (2 h)
H3 / 3H
Commercially available (10-100 €/pc., up to 3x3x1 mm) HPHT diamonds with ~200 ppm Ns
Measurements with new (fast) CCD spectrometer set-up
Good agreement between old & new IL set-up!
Monocrystals behave virtually identical to composites!

## Slide 16: FT-IR spectroscopy of irr. diamond
pristine
1344 cm-1: C-center (Ns)
1282 cm-1: A-center (N=N)
1280 cm-1: B-center (4N=V)
Tracking of radiation-induced defect dynamics

## Slide 17: FT-IR spectroscopy of irr. diamond
1344 cm-1: C-center (Ns)
1282 cm-1: A-center (N=N)
1280 cm-1: B-center (4N=V)
Tracking of radiation-induced defect dynamics
Non-luminescent defects that act as sinks for nitrogen:
N + V → N-V + N → N-V-N → N=N + V
ΔEb = 6.3 eV
ΔEb = 4.5 eV
ΔEb = 2.3 eV
C
A
B

## Slide 18: FT-IR spectroscopy of irr. diamond
1344 cm-1: C-center (Ns)
1282 cm-1: A-center (N=N)
1280 cm-1: B-center (4N=V)
Tracking of radiation-induced defect dynamics
C-center signal almost constant
  Dominated by non-irradiated volume
A&B center signal increases with fluence
  Damage cross-section:
  (8.5±0.4) nm2/ion

## Slide 19: FT-IR spectroscopy of irr. diamond
1344 cm-1: C-center (Ns)
1282 cm-1: A-center (N=N)
1280 cm-1: B-center (4N=V)
Tracking of radiation-induced defect dynamics
C-center signal almost constant
  Dominated by non-irradiated volume
A&B center signal increases with fluence
  Damage cross-section:
  (8.5±0.4) nm2/ion
No effect of beam-induced macroscopic temperature!
Similar effect as annealing >1600°C & >5 GPa for several hours!

## Slide 20: In-situ UV/c absorption spectroscopy
Irradiation and measurement at both RT and 50 K
Dramatic decrease in transmission
  Already 30-40% loss of transmission at 1×1012 (>450 nm)
Several absorption lines of color centers can be identified, mostly intrinsic
ND1 (V-)
3H / H3 (N-V-N)

## Slide 21: Summary
IL signal drops down to 5% of initial signal with irradiation
Optical camera shows change of main emission from „green“ to „blue“
  Beam diagnostic cameras operate with a narrow filter
FT-IR shows that complex non-luminescent nitrogen defects are forming
Intrinsic degradation of transmission by irradiation
  Additional process that degrades IL signal
IL signal of diamond excited by swift heavy-ions might be an intrinsic process
  Implications for potential optimization of the diamonds?