## Slide 1
PIT 192
RRP 108/127
No recover of Ic after unload
Ic0(B=19T) = 135 A
Irreversible stress limit at ~ 70 MPa
A flavour of HTS: transverse stress sensitivity of Bi2212 wires