## Slide 1: Results from test 23
EASITrain – European Advanced Superconductivity Innovation and Training. This Marie Sklodowska-Curie Action (MSCA) Innovative Training Networks (ITN) has received funding from the European Union’s H2020 Framework Programme under Grant Agreement no. 764879
15th WP15 Meeting
Presenter
Dmitry Tikhonov
Early stage researcher
Helmholtz-Zentrum Berlin
dmitry.tikhonov@helmholtz-berlin.de
+49-30-8062-12922

## Slide 2: Testing sample
B-4.9 | B-3.7
Full HiPMS | DCMS
Chemical ‘polishing’ before coating | (BCP), exposed to air before SIS
Nb-AlN-NbN 4um-8nm-180nm | Nb-AlN-NbN 4um-35nm-200nm

## Slide 3: Last SIS results
Low Rres ~40 nOhm
No non-monotonic
Good Rs vs B quality

## Slide 4: Last SIS results
Low Rres ~40 nOhm
No non-monotonic
Good Rs vs B quality

## Slide 5: BCS part
Low Rres ~40 nOhm
No non-monotonic
Good Rs vs B quality
BCS is lower

## Slide 6: Last SIS results

## Slide 7: Last SIS results
Nb-AlN-NbN
4um-35nm-200nm
Nb-AlN-NbN
4um-8nm-200nm
Nb-AlN-NbTiN
bulk-15nm-75nm
J-Lab

## Slide 8: Second test of 3.7
Second test of B-3.7:
Peaks appear but changed
Reheating cavity up to 20 K and sample did not help
1st cooldown
2nd cooldown

## Slide 9: IDEAS and explanations
Ideas:
Peaks appear due to thermal properties of the insulator layer
Flux trapping effects?
Effects bc. exposed to air?
Effects of the sample edges quality?

## Slide 10: Last SIS results
Nb ~ 9.3 K
NbN >20K???
Reference
Tc NbN <17.2

## Slide 11: Difference
Full EP sample:
No “Q-switches”
Lower Rres
Better performance at 1.3 GHz
B 4.9 SIS with EP
“Other samples”

## Slide 12: Last SIS results
Low Rres ~40 nOhm
No non-monotonic
Good Rs vs B quality

## Slide 13: Last SIS results
Still high losses at Q3

## Slide 14
Conclusions?
Non-monotonic effect
        Effect of thickness, make the thickness 20-25 nm?
        No exposure to air after each layer is the reason?
        Flux trapping?
        2. Chemical ‘polishing’ of the whole sample should be implemented in the procedure
 | Rres | Mx field | Tc
400 MHz | ~40 nOhm | ~35 mT | ??
800 MHz | ~140 nOhm | ~35 mT | ??

## Slide 15
Conclusions?
 | Location, film
B-2 | CERN, Nb thick film
B-3 | HZB, SIS (siegen 35 nm)
B-4 | HZB, SIS (Siegen)
B-5 | RTU, Nb

## Slide 16: Last SIS results

## Slide 17: Last SIS results

## Slide 18: Last SIS results