## Slide 1: Task 5: High-Tc Superconducting Link Status Report Eucard - WP7 – WP7 Collaboration Meeting, Geneva
Aubele (BHTS), A. Ballarino (CERN),
S. Berta and G. Grasso (Columbus), Y. Yang and C. Beduz (Soton)
8th June 2010

## Slide 2: Advancement of activities
Definition and procurement of tooling and material for the assembly of short length of cables (CERN)
Preparation of test station for the test of the 20 m multi-circuit superconducting link (CERN). The installation is planned to be available by end 2011
Design of a cryogenic test station for the electrical characterization of short length of cables (~2 m) cooled by supercritical helium in the temperature range 5 to 30 K (University of Southampton). The test station is planned to be available in October 2010.
Definition of functional specification for the multi-circuit superconducting link (CERN)
Creation of a database on superconductors properties (CERN, with data supplied by Columbus and BHTS)

## Slide 3: Advancement of activities
Optimization of electrical splices between MgB2 tapes and development of appropriate procedures (Columbus)
Optimization of electrical splices between Bi-2223 and Y-123 tapes an development of appropriate procedures (BHTS)
Definition of procedures for the measurement of the critical current of long lengths of MgB2 conductor (Columbus)
Preparation of conductors for the assembly of superconducting cables (Columbus, BHTS)
The next working of Task 7.5 meeting will take place at Columbus in Genova on the 30-31st August 2010

## Slide 4: Progress with MgB2: optimization of electrical splices -1-
In MgB2 wires, a rection layer typically occurs between the sheath material and the MgB2 filaments
The reaction layer, although thin, behaves as a resistive barrier, and it provides a significant resistance to the current transfer to the filaments
A procedure to reduce/eliminate the reaction layer is preferable in order to reduce the dissipation at the cable termninations

## Slide 5: Progress with MgB2: optimization of electrical splices -2-
Optimizing the final heat treatment of the MgB2 wires can reduce the reaction layer significantly
Chart: Reaction layers thickness
| B | C | D | E | F | G | H | I | L | M | N | O
strato totale di reazione | 10.73 | 9.14 | 8.57 | 6.92 | 6.43 | 5.76 | 7.11 | 4.96 | 5.33 | 4.36 | 4.14 | 3.72
strato primario di reazione | 6.22 | 4.74 | 4.37 | 3.8 | 3.42 | 2.8 | 3 | 2.47 | 2.7 | 1.9 | 2.06 | 1.9
strato secondario di reazione | 4.51 | 4.4 | 4.2 | 3.12 | 3.01 | 2.96 | 4.11 | 2.49 | 2.63 | 2.46 | 2.08 | 1.82
B 960°C 200s C 960°C 150s D 960°C 100s
E 920°C 200s F 920°C 150s G 920°C 100s
H 880°C 200s I 880°C 150s L 880°C 100s
M 840°C 200s N 840°C 150s O 840°C 100s
Total thickness
Mg-Ni alloy
Mg-B-Ni alloy

## Slide 6: Progress with MgB2: optimization of electrical splices -3-
Addition of a 10 micron–thick Niobium layer in between MgB2 filaments and the Nickel sheath: optimal way to eliminate any reaction of the superconducting phase
The wires with optimized interface between MgB2 and sheath material will be now used to study the influence on the electrical splice resistance