## Slide 1: 2021 Joint Universities Accelerator School Superconducting Magnets Section I
Paolo Ferracin
  (pferracin@lbl.gov)
Lawrence Berkeley National Laboratory (LBNL)

## Slide 2: Introduction Goal of the course
Overview of superconducting magnets for particle accelerators (dipoles and quadrupoles)
  Description of the components and their function
From the superconducting material to the full magnet
Superconducting material
Superconducting strand
Superconducting cable
Superconducting coil
Superconducting magnet

## Slide 3: Introduction Superconducting magnet technology
Multidisciplinary field: mixture of
  Chemistry and material science: superconducting materials
  Quantum physics: the key mechanisms of superconductivity
  Classical electrodynamics: magnet design
  Mechanical engineering: support structures
  Electrical engineering: powering of the magnets
  Cryogenics: keep them cold…
Very different order of magnitudes

## Slide 4: Outline
Section I
  Particle accelerators and magnets
  Superconductivity and practical superconductors
Section II
  Magnetic design
Section III
  Coil fabrication
  Forces, stress, pre-stress
  Support structures
Section IV
  Quench, protection, training

## Slide 5: References
Particle accelerators and magnets
Superconductivity and practical superconductors
  K.-H. Mess, P. Schmuser, S. Wolff, “Superconducting accelerator magnets”, Singapore: World Scientific, 1996.
  Martin N. Wilson, "Superconducting Magnets", 1983.
  Fred M. Asner, "High Field Superconducting Magnets", 1999.
  P. Ferracin, E. Todesco, S. Prestemon, “Superconducting accelerator magnets”, US Particle Accelerator School, www.uspas.fnal.gov.
  E. Todesco, “Masterclass - Design of superconducting magnets for particle accelerators”, https://indico.cern.ch/category/12408/
  A. Devred, “Practical low-temperature superconductors for electromagnets”, CERN-2004-006, 2006.
  Presentations from Luca Bottura and Martin Wilson

## Slide 6: Particle accelerators and magnets
Principle of synchrotrons
  Driving particles in the same accelerating structure several times
Electro-magnetic field accelerates particles
Magnetic field steers the particles in a circular orbit
Particle accelerated  energy increased  magnetic field increased (“synchro”) to keep the particles on the same orbit of curvature r
Constant
by E. Todesco

## Slide 7: Particle accelerators and magnets Dipoles
Main field components is By
  Perpendicular to the axis of the magnet z
Electro-magnets: field produced by a current (or current density)
Magnetic field steers (bends) the particles in a circular orbit
by E. Todesco



## Slide 8: Particle accelerators and magnets Quadrupoles
The force necessary to stabilize linear motion is provided by the quadrupoles
  They provide a field
    equal to zero in the center
    increasing linearly with the radius
They act as a spring: focus the beam
Prevent protons from falling to the bottom of the aperture due to the gravitational force
  it would happen in less than 60 ms
by E. Todesco



## Slide 9: Particle accelerators and magnets Quadrupoles
A typical accelerator structure is the FODO cell
  Alternating quadrupoles spaced by length L of similar gradient
One can prove that this gives positive focusing in both transverse planes




by E. Todesco

## Slide 10: Particle accelerators and magnets
Dipoles: the larger B, the larger the energy
Quadrupoles: the larger B, the larger the focusing strength
For an electro-magnet, the larger B, the larger must be J
In normal conducting magnets, J ~ 5 A/mm2
In superconducting magnets, Je ~ 600-700 A/mm2

## Slide 11: Superconductivity The discovery
Superconductivity was discovered in 1911 by Kammerling-Onnes who observed that the resistance of a mercury wire disappeared (immeasurably small value) at 4.2 K
  Not just “little” resistance - truly ZERO resistance

## Slide 12: Superconductivity Critical temperature
The temperature at which the transition takes place: critical temperature Tc
Below Tc,  no resistance
Observed in may materials
  but not in the typical best normal conductors (copper, silver, gold…)
At a temperature > Tc , a superconductor is a very poor conductor
2 kinds of superconductors
  Type I and Type II
    Different behaviour with magnetic field

## Slide 13: Superconductivity Type I superconductors
Meissner-Ochsenfeld effect (1933)
Perfect diamagnetism
  With T<Tc magnetic field is expelled
But, the B must be < critical field Bc
  Otherwise superconductivity is lost
by L. Bottura
B
B
Increase of field
Cool-down
Superconducting state
Normal state
Unfortunately, first discovered superconductors (Type I) with very low Bc ( 0.1 T)
  not practical for electro-magnets

## Slide 14: Superconductivity Type II superconductors
So, for 40-50 years, superconductivity was a research activity
Then, in the 50’s, type II superconductors
  Between Bc1 and Bc2 : mixed phase
    B penetrates as flux tubes: fluxoids
      with a flux of o = h/2e = 2 · 10-15 Wb
Much higher fields and link between Tc and Bc2
by L. Bottura
B<Bc1
Bc1<B<Bc2
Tc (K)

## Slide 15: Superconductivity Type II superconductors
Field penetrated in the form of flux tubes (fluxoids), each with a flux of
  o = h/2e = 2· 10-15 Wb
Observed both in a photo by Essmann & Träuble (1967) and with magneto-optical imaging technique by Oslo Univerisity
http://www.mn.uio.no/fysikk/english/research/groups/amks/superconductivity/

## Slide 16: Superconductivity Hard superconductors
…but, if a current is passed through the type II superconductor under a field >Bc1
  Lorentz force on the fluxoids
    F = J x B
The force causes a motion of tubes
  Flux motion (dB/dt)→ voltage (V)→ dissipation (V· I)
The fluxoids are therefore locked in pinning centers
  Defects or impurities in the structure: precipitates or grain boundaries
    Produced during fabrication

## Slide 17: Superconductivity Hard superconductors
The pinning centres exert a pinning force Fp
As long as Fp  J x B
  No flux motions (flux tubes pinned)  no dissipation
The critical current density of the superconductor Jc is the current density at which, for a given B and at a given T the pinning force is exceeded by the Lorentz force
So, there is a mutual link between maximum J, B, and T
by M. Wilson

## Slide 18: Superconductivity Critical surface
A type II material is supercond. below the critical surface defined by
  Critical temperature Tc
    Property of the material
  Upper critical field Bc2
    Property of the material
  Critical current density Jc
    Hard work by the producer

## Slide 19: Superconductivity Materials
Nb3Sn and Nb-Ti, discovered in 1954 and 1961, are the most commonly used type II superconductors (80-90% of all devices).
Since their critical temperature Tc is 9 K (for Nb-Ti) and 18 K (for Nb3Sn), they are defined as low T superconductors.
  High temperature superconductors (HTS) have a Tc up to 80-120 K.
Nb-Ti
Nb3Sn

## Slide 20: Superconductivity Nb-Ti
Nb and Ti combine in a ductile alloy (called  phase)
  Easy to process by extrusion and drawing techniques.
Tc and BC2 depend on Ti content: the optimal is 46.5-47 in weight %.
  Tc is ~9.2 K at 0 T.
  BC2 is ~14.5 T at 0 K.
The critical current Jc depends on microstructure
  Cold works and heat treatments form -Ti phase for flux pinning

## Slide 21: Superconductivity Nb-Ti
Most widely used superconductor
Implemented on large scale for the first time in the the Tevatron accelerator, built at Fermilab in the early 80s
In High Energy Physics, used also for all the post-Tevatron accelerators
Other important applications
  MRI /NMR magnets
  Fusion magnets (Tore Supra, France).
The cost is ~ 200 US $ per kg of wire (about 1 euro per m of strand)

## Slide 22: Superconductivity Nb3Sn
Nb and Sn can form an intermetallic compound from the A15 family (like Nb3Al).
TC and BC2 depend on Sn content: the optimal is 20-25 in weight%.
  TC is ~18 K at 0 T
  BC2 is ~28 T at 0 K
The critical current Jc depends on the micro (grain) structure
  High Jc obtained with grains from 30 to 300 nm

## Slide 23: Superconductivity Nb3Sn
Nb3Sn is brittle
  Cannot be extruded as Nb-Ti.
  Its formation must occur only at the end of the cable and/or coil fabrication process.
In addition, it is strain sensitive
  critical parameters   applied strain
Used in
  NMR, with field of about 20 T
  Model coils for ITER
  High energy physics (R&D)
The cost is approximately ~1500 US $ per kg of wire.
  ~5 euro per m of strand
by A. Godeke

## Slide 24: Superconductivity Nb-Ti vs. Nb3Sn
Nb-Ti
Nb3Sn

## Slide 25: Superconductivity Nb-Ti vs. Nb3Sn
Nb-Ti
Nb3Sn

## Slide 26: Superconductivity from Cu to Nb3Sn
Typical operational conditions (0.85 mm diameter strand)
Cu
Nb3Sn
Nb-Ti
Je ~ 5 A/mm2
I ~ 3 A
B = 2 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 8-9 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 12-13 T

## Slide 27: Practical superconductors
Typical operational conditions (0.85 mm diameter strand)
Cu
Nb3Sn
Nb-Ti
Je ~ 5 A/mm2
I ~ 3 A
B = 2 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 8-9 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 12-13 T

## Slide 28: Practical superconductors Introduction
Superconducting materials are produced in small filaments and surrounded by a stabilizer (typically copper) to form a multi-filament wire or strand.
A superconducting cable is composed by several wires: multi-strand cable.

## Slide 29: Practical superconductors Multi-filament wires motivations
The superconducting materials used in accelerator magnets are
  subdivided in filaments of small diameters
    to reduce magnetic instabilities called flux jumps
    to minimize field distortions due to superconductor magnetization
  twisted together
    to reduce interfilament coupling and AC losses
  embedded in a copper matrix
    to protect the superconductor after a quench
    to reduce magnetic instabilities called flux jumps

## Slide 30: Practical superconductors Multi-filament wires motivations
Fluxoid distribution depends on the applied B and on Jc.
Thermal disturbance  the local change in Jc  motion or “flux jump”  power dissipation
Stability criteria for a slab (adiabatic condition)
  a is the half-thickness of the slab
  jc is the critical current density [A m-2]
   is the density [kg m-3]
  C is the specific heat [J kg-1]
  c is the critical temperature.
Nb-Ti filament diameters usually < 50 µm
by L. Bottura
B<Bc1
Bc1<B<Bc2

## Slide 31: Practical superconductors Multi-filament wires motivations
Superconductor magnetization
  When a filament is in a varying Bext, its inner part is shielded by currents distribution in the filament periphery
    They do not decay when Bexis held constant  persistent currents
  These currents produce field errors and ac losses proportional to Jcrf
    LHC filament diameter 6-7 µm.
    HERA filament diameter 14 µm.
by K.-H. Mess, et al.
Bext
M
Field distorsion/errors

## Slide 32: Practical superconductors Multi-filament wires motivations
Inter-filament coupling
  When a multi-filamentary wire is subjected to a time varying magnetic field, current loops are generated between filaments.
  If filaments are straight, large loops with large currents  ac losses
  If the strands are magnetically coupled the effective filament size is larger  flux jumps
To reduce these effects, filaments are twisted
  twist pitch of the order of 20-30 times of the wire diameter.
by M. Wilson
by L. Bottura

## Slide 33: Practical superconductors Multi-filament wires motivations
Quench protection
  Superconductors have a very high normal state resistivity
    If quenched, could reach very high temperatures in few ms.
  If embedded in a copper matrix, when a quench occurs, current redistributes in the low-resisitivity matrix  lower peak temperature
  The copper matrix provides time to act on the power circuit
  In the case of a small volume of superconductor heated beyond the critical temperature the current can flow in the copper for a short moment, allowing the filament to cool-down and recover supercond.
  The matrix also helps stabilizing the conductor against flux jumps
by L. Bottura

## Slide 34: Practical superconductors Multi-filament wires motivations
Flux jumps
Persistent currents
AC losses
Quench protection

## Slide 35: Practical superconductors Fabrication of Nb-Ti multifilament wires
Nb-Ti ingots
  200 mm ∅, 750 mm long
Monofilament rods are stacked to form a multifilament billet
  then extruded and drawn down
  can be re-stacked: double-stacking process

## Slide 36: Practical superconductors Fabrication of Nb-Ti multifilament wires
Copper to superconductor ratio
  ensure quench protection without compromising the overall critical current of wire.
Filament diameter
  Minimize flux jumps and persistent currents
  Minimizing the wire processing cost
The inter-filament spacing
  small so that the filaments, harder then Cu, support each other during drawing operation
  large enough to prevent filament couplings
Cu core and sheath to reduce cable degradation
Main manufacturing issue: piece length
  It is preferable to wind coils with single-piece wire (to avoid welding)
    LHC required piece length longer than 1 km

## Slide 37: Practical superconductors Fabrication of Nb3Sn multifilament wires
Internal tin process
  A tin core is surrounded by Nb rods embedded in Cu (Rod Restack Process, RRP) or by layers of Nb and Cu (Modify Jelly Roll, MJR).
  Each sub-element has a diffusion barrier.
  Advantage: no annealing steps and not limited amount of Sn
  Disadvantage: small filament spacing results in large effective filament size (100 µm) and large magnetization effect and instability.
  Non-Cu JC up to 3000 A/mm2 at 4.2 K and 12 T.
by A. Godeke

## Slide 38: Practical superconductors Fabrication of Nb3Sn multifilament wires
Powder in tube (PIT) process
  NbSn2 powder is inserted in a Nb tube, put into a copper tube.
  The un-reacted external part of the Nb tube is the barrier.
  Advantage: small filament size (30 µm) and short heat treatment (proximity of tin to Nb).
  Disadvantage: fabrication cost.
  Non-Cu JC up to 2300 A/mm2 at 4.2 K and 12 T.
A. Godeke, [2].
by A. Godeke

## Slide 39: Practical superconductors Fabrication of Nb3Sn multifilament wires
Reaction of a PIT wire
by A. Godeke

## Slide 40: Practical superconductors Multi-strand cables motivations
Most of the superconducting coils for particle accelerators wound from a multi-strand cable (Rutherford cable)
  Reduction of strand piece length
  reduction of number of turns
    easy winding
    smaller coil inductance
      less V for power supply during ramp-up;
      after a quench, faster discharge and V
  current redistribution in case of a defect or a quench in one strand
The strands are twisted to
  Reduce inter-strand coupling currents
    Losses and field distortions
  Provide more mechanical stability
by M. Wilson

## Slide 41: Practical superconductors Multi-strand cables motivations
Rutherford cables fabricated by cabling machine
  Strands wound on spools mounted on a rotating drum
  Strands twisted around a conical mandrel into rolls (Turk’s head)
  The rolls compact the cable and provide the final shape
by M. Wilson

## Slide 42: Practical superconductors Multi-strand cables
A Rutherford cable can be rectangular or trapezoidal
  To stacking cables in an arc-shaped coil around the beam pipe
Cable compaction
  Ratio of the sum of the cross-sectional area of the strands (direction parallel to the cable axis) to the cross-sectional area of the cable
    88% (Tevatron) to 92.3% (HERA).
  Chosen to provide good mechanical stability + high current capability + enough space for helium cooling or epoxy impregnation.
Cables degradation
  Critical current density of a virgin wire before cabling is higher then the one of a wire after cabling

## Slide 43: Practical superconductors Multi-strand cables
Edge deformation may cause
  reduction of the filament cross-sectional area (Nb-Ti)
  breakage of reaction barrier with incomplete tin reaction (Nb3Sn)
In order to avoid degradation
  strand cross-section investigated
  Edge facets are measured
    General rule: no overlapping of facets
Keystone angle is usually of ~ 1° to 2°

## Slide 44: Practical superconductors Cable insulation
The cable insulation must feature
  Good electrical properties to withstand turn-to-turn V after a quench
  Good mechanical properties to withstand high pressure conditions
  Porosity to allow penetration of helium (or epoxy)
  Radiation hardness
In Nb-Ti magnets overlapped layers of polyimide
In Nb3Sn magnets, fiber-glass braided or as tape/sleeve.
Typically the insulation thickness: 100 and 200 µm.

## Slide 45: Practical superconductors Superconducting cables
Filling ratio: 0.25-0.3