## Slide 2
Vacuum Systems
Lecture 4
V. Baglin
CERN TE-VSC, Geneva

## Slide 3
Outline
Synchrotron radiation and photodesorption
Vacuum instability and ion stimulated desorption
Particle losses and ion stimulated desorption
Electron cloud and related surface parameters

## Slide 4
1. Synchrotron radiation
and
photodesorption

## Slide 5
1.1 Synchrotron radiation

## Slide 6
In synchrotron, particles can radiate light by synchrotron radiation
Can be used for diagnostics purposes :
CERN Control Centre LHC beams SR displays
But particles loose energy by synchrotron radiation  should be compensated by RF system
Beam emittance shrink by synchrotron radiation
Power is dissipated on the machine elements
Molecules are desorbed from the vacuum chamber wall due to synchrotron radiation
Synchrotron radiation: visible light

## Slide 7
Synchrotron Radiation
A charged particle which is accelerated produce radiation
The power of the centripetal radiation is larger than the longitudinal radiation (factor )
For a relativistic particle, the radiation is highly peaked (opening angle ~ 1/ )
The radiation energy range from infra-red to gamma rays: from meV to MeV
K. Hübner, CAS 1984, CERN 85-19
R.P. Walker, CAS 1992, CERN 94-01
A. Hofmann, CAS 1996, CERN 98-04
L. Rivkin, CAS 2008
References :

## Slide 8
Magnetic rigidity:
Critical energy
The critical energy split the power spectrum in two equals parts
90 % of the emitted photons have an energy lower than the critical energy

## Slide 9
The energy emitted by the synchrotron radiation per turn and per particle is:
The average power emitted per turn by the beam is:
So, the average power emitted by the beam per unit of length is:
Dissipated power

## Slide 10
Dissipated power
The average power emitted by the beam per unit of length is
Electrons :
Protons:

## Slide 11
The SR power emitted by a particle is a function of the vertical angle and the wavelength.
Integrating over the vertical angle, one obtains the spectral power density per unit of length :
Power spectrum

## Slide 12
Since the photon flux is linked to the power by :
The photon flux per unit length in a relative energy band is written:
So, the total photon flux per unit of length is:
Photon flux

## Slide 13
The photon flux per unit of length is given by :
Electrons :
Protons:
Linear photon flux

## Slide 14
LHC SR Spectrum : from IR to UV
With nominal parameters : 7 TeV and 585 mA
2010, 2011, 2012 and 2015 spectra
450 GeV
7 TeV
Key parameter: photodesorption yield

## Slide 15
7 TeV
εc= 44 eV
0.2 W/m
1017 photons/m/s
1/gamma = 0.13 mrad
E3
E4
E
LHC SR properties
1/gamma opening angle

## Slide 16
LEP SR spectrum: X-rays & gamma rays

## Slide 17
 |  | Soleil | KEK-B |  | LEP |  |  | LHC | 
 |  |  | LER | HER | Inj. | 1 | 2 | Inj. | Col.
Particle |  | e- | e+ | e- | e- | e- | e- | p | p
Beam current | mA | 500 | 2600 | 1100 | 3 | 3 | 7 | 584 | 584
Energy | GeV | 2.75 | 3.5 | 8 | 20 | 50 | 96 | 450 | 7000
Bending radius | m | 5.36 | 16.31 | 104.46 | 2962.96 |  |  | 2784.302 | 
Power | W/m | 14 030 | 20 675 | 5 820 | 0.8 | 30 | 955 | 0 | 0.2
Critical energy | eV | 8 600 | 5 800 | 11 000 | 6 000 | 94 000 | 660 000 | 0 | 44
Photon flux | photons/m/s | 3 1019 | 7 1019 | 1 1019 | 3 1015 | 7 1015 | 3 1016 | 7 1015 | 1 1017
Dose at 3000 h | photons/m | 4 1026 | 8 1026 | 1 1026 | 3 1022 | 7 1022 | 3 1023 | 7 1022 | 1 1024
In LEP, and all synchrotron light sources, the evacuation of the power is an issue
The LHC operates at 7 TeV with ~ .6 A. Power evacuation is an issue for the cryogenic system (1 kW/arc !!)
The critical energy varies from a few 10 eV to 660 keV. Strongly bound molecules can be desorbed
The photon flux is large, so large gas load. Adequate dimensioning of the effective pumping speed is required
The annual photon dose is large. Implications on gas reduction and radiation
SR impact on different type of machines …

## Slide 18
(C. Herbeaux et al.)
… heavy consequences on design
A complex vacuum chamber design with a light extraction path, pumping and instrumentation ports and power absorbers (crotch)
Stainless steel
NEG coated, in-situ baked to 180ºC

## Slide 19
Soleil « crotch » power absorber: Water cooled copper Glidcop (256 W/mm2)
SOLEIL Design
(C. Herbeaux et al.)
… heavy consequences on design

## Slide 20
(E. Al-Dmour, EPAC 2006)
(E. Huttel et al.)
ALBA Design
ANKA Design
… heavy consequences on design
Antechamber design to absorb the SR power externally to the beam path with the integration of a distributed pumping
NSLS-2 Design

## Slide 21
LEP Design
(CERN LEP Vacuum group)
… heavy consequences on design
Antechamber and distributed NEG pumping, water cooling and lead shielding

## Slide 22
LHC Design
(CERN LHC Vacuum group)
Courtesy N. Kos CERN TE/VSC
Courtesy N. Kos CERN TE/VSC
… heavy consequences on design
Perforated Cu colaminated beam screen to intercept the SR power protecting the 1.9 K cold bore and to allow a distributed pumping

## Slide 23
1.2 Photodesorption

## Slide 24
The interaction of photons (light) with matters produce the desorption of neutral gases inside the vacuum system
The photon stimulated desorption (PSD) of physisorbed (meV) or chemisorbed (eV) molecules can be direct or non-direct
The identified transmitters are photoelectrons, secondary electrons and phonons
The photon stimulated molecular desorption is a function of the nature of the material, its temperature, its surface state, of the photon energy and the irradiation angle.
No model exists, therefore in-situ qualification of material is required for the design of a future machine.
Photodesorption

## Slide 25
The photodesorption process is linked to the production of photoelectrons and secondary electrons
Photoelectrons contribute to the gas load by ESD
The oxide and carbon layers are believed to be the source of gas
The diffusion of atoms into the solid and their recombination at the surface plays a role
O. Gröbner et. al. EPAC 1992
J. Gómez-Goñi et al. JVSTA 12(4) Jul/Aug 1994, 1714
T. Kobari et al Proc .of Vacuum Design of Synch Light Sources Conference, Argonne, 1990
Photodesorption: present understanding

## Slide 26
Beam cleaning during the first period of LEP
O. Gröbner. Vacuum 43 (1992) 27-30
C. Herbeaux, Journée thématiques RTVide, décembre 2014
SOLEIL
Dynamic pressure due to PSD
The dynamic pressure decreases by several orders of magnitude with photon dose: “photon conditioning”
The photon desorption yield is characterised by ηphoton
With beam P ~ 10-10 Torr
With beam P ~ 2 10-9 mbar

## Slide 27: Photo-desorption yield measurement
V. Baglin et al. EPAC 1998, Stockholm, Sweden.
SR light is extracted from a dipole magnet to irradiate the chamber at ~ 11 mrad
SR fan is vertically collimated therefore photon flux < 4 eV are attenuated
The gas load is measured by the throughput method via a conductance (72.5 ℓ/s for N2)
A wire and a collector are biased for current measurement to estimate the photon reflectivity and photoelectron yield
J. Gómez-Goni et al. J. Vac. Sci. Technol. A 12(4), Jul/Aug 1994, 1714
With G = 4.3 1019 molecules/mbar.ℓ at RT

## Slide 28: CERN EPA Synchrotron Light Facility 42 - 1999
The LEP Pre-Injector as a multipurpose facility, J-P. Potier, L. Rinolfi, EPAC 1998, Stockholm, Sweden, 1998

## Slide 29
C. Herbeaux et. al. EPAC 2008, Gênes, Italie
O. Gröbner et al.
J.Vac.Sci. 12(3), May/Jun 1994, 846-853
Cu baked at 150°C
The hydrogen desorption is characterised by a diffusion process: a = 0,5
M. Andritschky et al., Vacuum 38 (8-10), 933, (1988)
a ~ 0.9-1.3
Conditioning under photon irradiation
Typical desorption yield range: from 10-3 molecule/photon to 10-6 when conditioned
NEG coated SS activated at 180°C

## Slide 30
C. Herbeaux et al. JVSTA 17(2) Mar/Apr 1999, 635
Unbaked stainless-steel
3.75 keV
Gas | H2 | CH4 | H2O | CO | CO2 | Total
molecules/cm2 x 1015 | 8.1 | 0.2 | 1.1 | 2.8 | 2.2 | 14.4
Gas load
The total desorbed quantity amounts to 15 monolayers for an unbaked system
Unbaked stainless-steel
3.75 keV

## Slide 31
At low energy, the photoelectric effect dominates
Above a few 100 keV, Compton diffusion dominates and produce a cascade of energetic recoil electrons with a diffusion of secondary photons
J. Gómez-Goñi et al. JVSTA 12(4) Jul/Aug 1994, 1714
150°C bake-out
O. Gröbner. CAS 99-15
Evolution with critical energy

## Slide 32: Photodesorption of NEG films
Very low desorption yields: “ultra” clean surface
Be aware of the difference between effective and intrinsic yields
TiZrV film on stainless-steel
4.5 keV
V. Anashin et al. EPAC 2002, Paris, France.
Baked at
80°C
Activated at
190°C
V. Baglin et al. CERN VTN 98-04, 1998.
Activated
Non- Activated

## Slide 33
Photodesorption at Cryogenic Temperature
Initial yield, η0, are smaller than at room temperature
V. Baglin et al., Vacuum 67 (2002) 421-428

## Slide 34
Desorption of physisorbed molecules
V. Anashin et al., Vacuum 53 (1-2), 269, (1999)
Stainless steel
250-300 eV
Perpendicular incidence
V. Baglin et al. EPAC 2002, Paris, France.
Photo-cracking of molecules
What about physisorbed molecules?

## Slide 35
Photo-desorption in LHC
Let’s consider a nominal beam circulating in the LHC which beam screen operates at 15 K, what is the initial pressure increase?
Sholes = 316 l/s/m
LHC photon flux = 1017 ph/m/s
Desorption yield, = 2 10-4 H2/ph
Pressure increase at 15 K:
What is the corresponding gas density?
In 2018, the measured gas density was n = 2.5 1012 H2/m3, the corresponding molecular photo-desorption yield is then 10-5 H2/ph

## Slide 36
2. Vacuum instability and ion
stimulated desorption

## Slide 37
High current machines: ISR, LHC …
First documented pressure bump in the ISR E. Fischer/O. Gröbner/E. Jones 18/11/1970
current
pressure
Beam current increases to 1 A
Pressure increases up to 10-6 Torr (x 50 in a minute)
Beam loss
The phenomenon

## Slide 38
The mechanism of vacuum instability
When the beam current approach the critical current, the pressure increases to infinity
Quasi stationary long tube (C=0)
Origin are ions produced by beam gas ionisation

## Slide 39
O. Gröbner, CERN 99-05
LHC beam current (A)
Varies with the material, the ion energy and ion species
Several units of molecules can be desorbed by ions  Sputtering
Baked
stainless steel
A.G. Mathewson, CERN ISR-VA/76-5
N2+
A.G. Mathewson, CERN ISR-VA/76-5
Unbaked
stainless steel
N2+
5 keV, Baked
G. Hulla, PhD Thesis, Vienna Tech. U, 2009
He+, Ne+, Ar+, Kr+, Xe+
H2+, CH4+,C2H4+, C2H6+
CO+,N2+,CO2+
0.2-0.5 keV
Ion desorption yield

## Slide 40
A conditioning is observed but at high dose, some ions can be implanted !
G. Hulla, PhD Thesis, Vienna Tech. U, 2009
7 keV, Cu Baked, Ar+
G. Hulla, PhD Thesis, Vienna Tech. U, 2009
7 keV, Cu Baked, CO+
In the LHC : the maximum flux is about 3 108 ions/(cm2.s) i.e. a dose of 3 1015 ions/(cm2.year)
In the LHC, there is no “beam” conditioning under ion bombardment
Conditioning and implantation

## Slide 41
Beam conditioning being negligible, one must decrease the desorption yield and optimise the pumping speed
ISR : Argon glow discharge (Ar, 10 % O2,~ 400 V, 1018 Ar/cm2)) with in-situ bakeout :
A.G. Mathewson, CERN ISR-VA/76-5
How to ensure vacuum stability ?

## Slide 42
3. Particle losses
and
ion stimulated desorption

## Slide 43
Loss of ions from a beam leads to large pressure increases: 10-8 …10-5 mbar!
W. Fischer et. al. EPAC 2002, Paris, France
110 bunches, Au79+,
9.9 GeV/u
W. Fischer et. al. EPAC 2006, Edinburgh, Scotland
3 109, Au79+, 9.9 GeV/u
1, 2 & 3 mrad
RHIC

## Slide 44
E. Mahner et al. ,
Phys. Rev. ST Accel. Beams 6, 013201 (2003)
Desorption yields range from 20 – 20 000 molecules per ion
The desorption is determined by the energy given to the electrons (electronic stopping force)
Pb53+, 4. 2 MeV/u, 14 mrad
The desorption induced by the electrons is the responsible mechanism
L. Prost et al. , PRL 98, 064801 (2007)
High energy ions

## Slide 45
Located in the LHC arcs around IP2 to intercept lead beams with modified charge produced at the interaction point: Pb81+ instead of PB82+
W jaws
HL-LHC ions collimator
TCLD
TCLD & LEN Bypass
Courtesy S. Redaelli, F. Savary

## Slide 46
4. Electron cloud
and related surface parameters

## Slide 47
4.1 Introduction

## Slide 48
F. Ruggiero et al., LHC Project Report 188 1998, EPAC 98
Key parameters:
- beam structure
- bunch current
- vacuum chamber dimension
- secondary electron yield
- photoelectron yield
- electron and photon reflectivities
…
LHC mechanism

## Slide 49
Once again, play with the key parameters :
  - Reduce the photoelectron yield (grazing incidence has larger yield than perpendicular incidence)
  - Reduce the secondary electron yield (scrubbing, NEG or amorphous carbon films, geometry)
  - Reduce the amount of electrons in the system (solenoid magnetic field, clearing electrodes, material reflectivity)
  Adapt the beam structure or the vacuum chamber dimensions to reduce the multiplication
  …
How to mitigate the electron cloud?

## Slide 50
4.2 Photons from SR

## Slide 51
Photoelectric effect : when a photons irradiates a surface with enough energy, it produces electrons
The energy of emitted electrons varies from :
0 eV to (hν – Wf) eV
Most of the electrons are secondaries
A few 0.1 % to 1 % have high energy
R. Cimino et al. , Phys. Rev. ST Accel. Beams 2, 063201 (1999)
Gold
Photoelectrons

## Slide 52: EDC under SR irradiation
EDC: Electron distribution curve
SR dose reduce the amount of low energy photoelectrons
The total yield is decreased by 40 % after 1 day of nominal LHC operation
R. Cimino et al. Phys. Rev. AB-ST 2 063201 (1999)

## Slide 53
V. Baglin et al., Trieste, 1998
From 1 to 80% forward reflectivity
Low reflectivity at perpendicular incidence
High reflectivity at grazing incidence i.e. this is the case of SR in accelerators
In LHC, 5 mrad gives more than 95% reflection
Copper adsorption at 920 eV
Henke databook
DCI, Ec=3 keV
O. Gröbner et al., 24-4-1988
Photon reflectivity
In complex geometries, ray tracing is done with e.g. Synrad

## Slide 54
4.3 Electrons from the electron cloud

## Slide 55
Electron Distribution Curve (EDC)
The Electron Distribution Curve shows :
  - A component at reflected electron energy
  - Secondary electrons with low energy
Most of the emitted electrons have low energy
Courtesy R. Cimino
CASINO code
Penetration depth: 1 – 10 nm
N. Balcon et al,
IEE Trans. On Plasma Sci. 40, 2012, 282
Escape depth: <10 nm

## Slide 56
Secondary Electrons Yield
N. Hilleret et al., LHC Project Report 433 2000, EPAC 00
312 eV
Technical material
Maximum around 200-300 eV
δmax ~ 2 to 3.5

## Slide 57
M. Taborelli et al., ECM workshop, 2008
TiZrV film
LHC RT beam pipes
C. Scheuerlein et al. Appl.Surf.Sci 172(2001)
Amorphous carbon
HL-LHC Cryogenic Triplets
The origin of the low SEY is different in both case :
- nature of the surface
- smooth versus rough surfaces
Very low SEY

## Slide 58
LHC : Scrubbing of the surface
dmax
V. Baglin et al., Chamonix, 2001
Photoelectrons produced by SR are accelerated towards the test sample
Reduction of SEY under electron irradiation is observed
1 to 10 mC/mm2 is required to scrub the surface
Growth of a carbon layer (AES, XPS)
dmaxini
dmaxfinal
LHC design:
δmax ~ 1.3

## Slide 59
Beam scrubbing at 10 K but SEY increases with gas condensation
R. Cimino , I.R. Collins, App. Surf. Sci. 235, 231-235, (2004)
N. Hilleret et. al. Chamonix 2000
N. Hilleret. LHC MAC December 2004
0.0
0.20
0.40
0.60
0.80
1.0
1.2
0
50
100
150
200
250
300
350
d
Primary Energy (eV)
d
total
Contribution
of secondaries
to
d
Contribution of reflected
electrons to
d
Fully scrubbed Cu
SEY at cryogenic temperature
The control of the surface coverage in a cryogenic machine is a must

## Slide 60
G. Vorlaufer et al., CERN VTN, 2000
Unbaked copper
Threshold around 10 eV
Electron desorption yield

## Slide 61
Reduction of the electron desorption yield with the electron dose: ~ 40 monolayers of gas desorbed from the surface during beam scrubbing
G. Vorlaufer et al., CERN VTN, 2000
 | H2 | CH4 | H2O | CO | CO2
η0 | 2 10-1 | 2.5 10-2 | 1 10-1 | 3.5 10-2 | 5 10-2
D0 x 1014 | 3 | 1 | 6 | 2 | 4
a | 0.47 | 0.62 | 0.66 | 0.49 | 0.54
Electron dose
 | H2 | CH4 | H2O | CO | CO2
x 1e15 | 28 | 0.5 | 4.6 | 3.4 | 4.6
Molecules/cm2 desorbed after 1019 e/cm2 i.e 16 mC/mm2

## Slide 62
For a monolayer (1015 molecules/cm2)
 | H2 | CH4 | CO | CO2
η | 500 | 5 | 10 | 0.5
H. Tratnik et al., Vacuum 81, 731,(2007)
Studied for 300 eV electrons with :
Pure gas
Equimolecular mixture of 4 gases
Standard LHC gas composition
Electron desorption at cryogenic temperature: Cu
The yields are very large
   physisorbed molecules under e- bombardment are strongly recycled in the gas phase

## Slide 63
ESD in LHC
In 2015, about 1W/m was dissipated on the LHC beam screen due to electron cloud heat load, what is the corresponding ESD yield?
Sholes = 0,316 m3/s/m, n=2.25 1013 H2/m3
Mean electron energy 100 eV
Electron flux = 6 1016 e/m/s
Electron Stimulated Desorption yield:
What is the corresponding electron dose, D ?
  D= 2 1021 e/cm2 or 3 C/mm2
In 2018, heat load drops to 0.3 W/m and n=2.5 1012 H2/m3
  D= 2 1022 e/cm2 or 32 C/mm2

## Slide 64: Lecture 4 summary
In accelerators, the circulating beam can contribute to stimulate molecular desorption
Those phenomenon can lead to much larger gas load than the thermal outgassing rate
Photon stimulated desorption originates from SR
Ion stimulated desorption originates from beam gas ionisation and can lead to vacuum instability
Particle losses
Electron stimulated desorption originates from an electron cloud

## Slide 65
Some References
Cern Accelerator School, Vacuum technology, CERN 99-05
Cern Accelerator School, Vacuum in accelerators, CERN 2007-03
Cern Accelerator School, Vacuum for particle accelerators, Glumslov, June 2017
The physical basis of ultra-high vacuum, P.A. Redhead, J.P. Hobson, E.V. Kornelsen. AVS.
Scientific foundations of vacuum technique, S. Dushman, J.M Lafferty. J. Wiley & sons.
Les calculs de la technique du vide, J. Delafosse, G. Mongodin, G.A. Boutry. Le vide.
Vacuum Technology, A. Roth. Elsevier Science
Foundations of vacuum science and technology, Ed by J.M. Lafferty. J. Wiley & sons.
Vacuum in Particle Accelerators: Modelling, Design and Operation of Beam Vacuum Systems, O. Malyshev. Wiley VCH.
Some Journals
Journal of Vacuum Science and Technology
Vacuum
Applied Surface Science
Nuclear Instruments and Methods
Physical Review Accelerator and Beams

## Slide 66
Thank you for your attention !!!

## Slide 68
Complementary
information

## Slide 69
1.1 Synchrotron radiation

## Slide 70
G.Y Hsiung et al.
… heavy consequences on design
A complex vacuum chamber design with a light extraction path, pumping and instrumentation ports and power absorbers (crotch)
Extruded Aluminum
Ex-situ baked to 150ºC
TPS Design
Complementary information

## Slide 71
1.2 Photodesorption

## Slide 72: Desorption yield vs gas load
The quantity removed during the cleaning process is a useful information to estimate intervals between getter reactivation or surface coverage on a cryogenic surface
Unbaked stainless-steel
3.75 keV
Baked OFHC Cu
3.75 keV
O. Gröbner et al.
J.Vac.Sci. 12(3), May/Jun 1994, 846-853
C. Herbeaux et al. JVSTA 17(2) Mar/Apr 1999, 635
 | H2 | CH4 | CO | CO2 |  | H2 | CH4 | CO | CO2
η0 (molecules/ph) | 9.2 10-4 | 2.3 10-4 | 3.7 10-4 | 5.5 10-4 |  | 8.8 10-3 | 4.4 10-4 | 5.7 10-3 | 8.4 10-3
Qo (Torr l /m) | 3.0 10-2 | 4.5 10-4 | 8.4 10-3 | 1.1 10-2 |  | 1.9 10-1 | 3.9 10-3 | 5.7 10-2 | 4.0 10-2
Q0 (molecules/cm2) | 2.3 1014 | 3.5 1012 | 6.5 1013 | 8.5 1013 |  | 1.5 1015 | 3.1 1013 | 4.5 1014 | 3.2 1014
Complementary information

## Slide 73
2. Vacuum instability and ion
stimulated desorption

## Slide 74
In the case of a machine with distributed pumping (C≠0) :
When the denominator approach zero, the pressure diverge
so
therefore
In the case of more complex geometry, numerical tools are used
Description of the mechanism
Complementary information

## Slide 75
It is a function of the speed & the charge of the projectile and of the nature of the residual gas.
 | Ionisation cross-section (in 10-18 cm2) |  | 
Gas | 26 GeV | 450 GeV | 7000 GeV
H2 | 0.27 | 0.36 | 0.45
He | 0.27 | 0.36 | 0.45
CH4 | 1.9 | 2.5 | 3.2
H2O | 1.4 | 1.9 | 2.4
N2 | 1.6 | 2.2 | 2.7
CO | 1.6 | 2.2 | 2.7
O2 | 1.8 | 2.4 | 3.1
Ar | 1.7 | 2.4 | 3.1
CO2 | 2.5 | 3.4 | 4.3
Chart: Ionisation cross section for proton beam
| 1 | 1.2 | 1.4 | 1.6 | 1.8 | 2 | 2.2000000000000002 | 2.4 | 2.6 | 10 | 26 | 100 | 200 | 450 | 600 | 1000 | 7000
H2 | 1.2494e-22 | 4.3575e-23 | 3.2147e-23 | 2.7791e-23 | 2.5611e-23 | 2.4372e-23 | 2.3616e-23 | 2.3138e-23 | 2.2831e-23 | 2.4297e-23 | 2.7105e-23 | 3.1283e-23 | 3.3448e-23 | 3.5982e-23 | 3.6881e-23 | 3.8478e-23 | 4.456e-23
He | 1.1244e-22 | 4.0149e-23 | 2.9845e-23 | 2.5924e-23 | 2.3976e-23 | 2.2883e-23 | 2.2228e-23 | 2.1825e-23 | 2.1576e-23 | 2.3545e-23 | 2.6604e-23 | 3.1128e-23 | 3.3471e-23 | 3.6213e-23 | 3.7186e-23 | 3.8913e-23 | 4.5495e-23
CH4 | 7.733e-22 | 2.7697e-22 | 2.0609e-22 | 1.7912e-22 | 1.6574e-22 | 1.5824e-22 | 1.5376e-22 | 1.5101e-22 | 1.4932e-22 | 1.6346e-22 | 1.8499e-22 | 2.168e-22 | 2.3327e-22 | 2.5255e-22 | 2.5939e-22 | 2.7154e-22 | 3.1781e-22
H2O | 6.0006e-22 | 2.1416e-22 | 1.5917e-22 | 1.3825e-22 | 1.2785e-22 | 1.2202e-22 | 1.1852e-22 | 1.1636e-22 | 1.1503e-22 | 1.2547e-22 | 1.4174e-22 | 1.6581e-22 | 1.7827e-22 | 1.9285e-22 | 1.9803e-22 | 2.0722e-22 | 2.4223e-22
CO | 6.4194e-22 | 2.3166e-22 | 1.7278e-22 | 1.5039e-22 | 1.3931e-22 | 1.3313e-22 | 1.2946e-22 | 1.2722e-22 | 1.2588e-22 | 1.3882e-22 | 1.5768e-22 | 1.8551e-22 | 1.9992e-22 | 2.1678e-22 | 2.2277e-22 | 2.3339e-22 | 2.7387e-22
O2 | 7.031e-22 | 2.5509e-22 | 1.9058e-22 | 1.6605e-22 | 1.5394e-22 | 1.4719e-22 | 1.4321e-22 | 1.408e-22 | 1.3937e-22 | 1.5449e-22 | 1.7592e-22 | 2.0752e-22 | 2.2388e-22 | 2.4302e-22 | 2.4981e-22 | 2.6187e-22 | 3.0782e-22
CO2 | 1.0284e-21 | 3.6949e-22 | 2.752e-22 | 2.3934e-22 | 2.2156e-22 | 2.1161e-22 | 2.0568e-22 | 2.0206e-22 | 1.9985e-22 | 2.1945e-22 | 2.4873e-22 | 2.9198e-22 | 3.1437e-22 | 3.4058e-22 | 3.4988e-22 | 3.6639e-22 | 4.2929e-22
F.F. Rieke, W. Prepejchal , Phys. Rev. A5, 1507 (1972)
Heavy gas must be avoided
Ionisation cross section
Complementary information

## Slide 76
Described by the nuclear and electronic stopping force (stopping power)
Low masses (H2) are desorbed by the electronic energy transfer to the lattice
High masses are desorbed by the direct nuclear momentum transfer between two particles
S(E)
Ion desorption
G. Hulla, PhD Thesis, Vienna Tech. U, 2009
Complementary information

## Slide 77
Desorption of physisorbed gas
Critical current is changed to
’H2 ~ 2000
’CO2 ~ 2
@ 5 keV and 1 monolayer
(N. Hilleret, R. Calder, IVC, 1977)
It is a function of the geometry, the gas specie, the sticking coefficient and of the 2 desorption yields
H2+, 3.2 K
J. Barnard et al., Vacuum 47 (4), 347, (1996)
At cryogenic temperature
Complementary information

## Slide 78
LHC beam screen stability
A minimum pumping speed is provided beam the beam screen’s holes
Beam screen’s holes provide room for LHC upgrades …..
Courtesy N. Kos CERN TE/VSC
 | H2 | CH4 | CO | CO2
(ηI)crit [A] | 1300 | 80 | 70 | 35
NB : In the long straight sections, vacuum stability is provided by TiZrV films and ion pumps which are less than 28 m apart
Complementary information

## Slide 79
The ion flux is a function of the pressure and the beam current
For nominal parameters, P~ 10-8 mbar and I ~ 600 mA
Ion energy will be about 100 eV, so the desorption yield about 2 molecules/ion
Beam screen pumping speed, S
Pressure increase due to ion:
No visible pressure increase in LHC
Pressure increase in LHC due to ions ?
Complementary information

## Slide 80
3. Particle losses
and
ion stimulated desorption

## Slide 81
Surface effect (except diffusion H2) due to a thermal activation
M. Bender et al. , NIM B 267 (2007) 885-890
Xe29+, 1.4 MeV/u, Perpendicular
Temperature of atomic Cu subsystem after Xe impact
300° C
Desorbed particles per Xe per dt
« Inelastic thermal spike model » : a temperature map coupled to the thermal desorption model
Mecanism
Complementary information

## Slide 82
Use of NEG films (LEIR, RHIC, GSI)
Use of beam conditioning
Intercept ion loss on dedicated collimators:
  - LEIR : 30 μm gold film on SS 316 LN, perpendicular incidence
C. Omet et. al. EPAC 2008, Genoa, Italy
- GSI : 0.1 μm gold film, perpendicular incidence. Absorbeur inserted in a secondary vacuum chamber. NEG film
Remedies: collimation!
- HL-LHC : movable collimator – 150 W of 7 ZxTeV ions coming from BPFP
. J. Jowett
BFPP:
208Pb82+ + 208Pb82+ → 208Pb82+ + 208Pb81+ + e+
Complementary information

## Slide 83
4. Electron cloud
and related surface parameters

## Slide 84
4.1 Introduction

## Slide 85
Vacuum stability test of a baked aluminium chamber 200°C, diam 160 mm (1976-1977)
Observation of pressure spikes, particularly during transverse displacement of a proton bunch
The existence of the spike varies with :
- bunch length
- number of proton bunch
Existence of a current threshold (120 mA for 20 bunches)
Different gas composition (dominated by H2 instead of CO)
Measurement of a significant electron current on the clearing electrodes
Gas desorption is stimulated by electrons
Electrons are accelerated by the proton bunch: multipactor effect
O. Gröbner, ISR-VA/77-38
History: observed at the ISR
Complementary information

## Slide 86: PEP-II
J. Seeman et al., EPAC 2000, Vienna, Austria
Electron cloud in the positron ring was foreseen during the design phase: TiN coating on Aluminium
Emittance blow up above 800 mA (SR light)
Observation of non linear pressure rise
Winding of solenoids in the straight section
Luminosity increase
Complementary information

## Slide 87
Cu OFHC vacuum chamber, unbaked, NEG pumping
Emittance blow up in the vertical plane of the positron beam
Positron bunch instability due to the cloud of photoelectrons
Observed in multibunch mode
Installation of permanent magnets then solenoids
Y. Funakoshi et al., EPAC 2000, Vienna, Austria
Observation at IP
K. Ohmi, F. Zimmermann, PRL 85, 3821 (2000)
KEKB LER Solenoids
KEKB
Luminosity increase
Complementary information

## Slide 88
Stainless steel vacuum chamber baked at 250°C in the straight sections
Stainless steel vacuum chamber cooled at 4 K in the arcs
Pressure increase with protons and ions beams
NEG, bakeout, solenoids, beam structure …..
H. Hseuh et al., EPAC 2002, Paris, France
RHIC
Luminosity increase
Complementary information

## Slide 89
Unbaked stainless steel vacuum chamber
Pressure increase observed with LHC type beams
Measurement of electron current on a pick up
Ok for LHC beam injection
J.M. Jimenez et al., EPAC 2000, Vienna, Austria
7.7 1010 protons/bunch
J.M. Jimenez et al., EPAC 2000, Vienna, Austria
60 h of beam conditioning
SPS
Complementary information

## Slide 90
Synchronism condition:
O. Gröbner. PAC 97, Vancouver, Canada
Speed increment due to the kick
Intensity threshold:
Enough energy gain due to the kick to produce secondaries:
Electrons in the vacuum chamber wall vicinity receive a kick of 190 eV, those in the beam vicinity receive 15 keV.
Simple model
Complementary information

## Slide 91
4.2 Photons from SR

## Slide 92: Behaviour with critical energy
SR irradiation at EPA
Grazing incidence, 11 mrad
The photoyield increases when increasing critical energy.
Photon reflectivity slightly decreases when increasing critical energy
PY*: photoelectrons per absorbed photons
I.R. Collins et al. EPAC 1998,Stockholm, Sweden
NB : molecular desorption yields are linear in the range, 10 – 300 eV. So the photoelectron yield should be also proportional to critical energy
Complementary information

## Slide 93: Photoelectrons for a LHC type beam screen
The Photoyield decrease with beam conditioning
It varies from 1 to 4 % under perpendicular incidence
V. Baglin et al., Chamonix, 2001
Sawteeth, Ec=194 eV
~ 40 mm
~ 500 mm
Complementary information

## Slide 94
Flat Cu
Saw tooth
N. Mahne et al. App. Surf. Sci. 235, 221-226, (2004)
Photon reflectivity of LHC type material
The saw tooth structure reduces the reflectivity
Complementary information

## Slide 95
4.3 Electrons from the electron cloud

## Slide 96: Geometrical effect
A fancy effect or a real application ?
After a coffee discussion, a drilled sampled by the VAC workshop (H. Kos)
Ø ~1 mm , 92 holes/cm2
Measurement courtesy A. Kuzucan
SEY max < 1.3 for Cu unbaked !!
Original idea with groove only:
Complementary information

## Slide 97: Laser Engineered Structure Surface
Still under development by STFC and Dundee university, so it came too late for the LHC construction !
Principle: laser treatment of a tube at atmospheric pressure
Production of a micrometric structure
Appl. Phys. Lett. 101, 2319021 (2012). Physics Highlights – Physics Today (February 2013). Opt. Mater. Exp. 1,1425 (2011).
Applied Physics Letters 12/2014; 105(23): 231605
δmax< 0.8 !
CERN data, 2015
Complementary information

## Slide 98
Origin of the SEY reduction at 300 K
R. Cimino et al. PRL 109, 064801(2012)
Graphitization of the carbon contamination layer
under electron irradiation
Modification of C1s core level
Conversion sp3 => sp2
High energy electrons increase the number of graphitic like C-C bounds
HOPG : highly oriented pyrolity graphite
δmax
2.2
1.35
1.1
1.05
Complementary information

## Slide 99
Conditioning and electron energy
At 300 K, the scrubbing efficiency of low energy electron is less than high energy electrons
Electron energy distribution at the LHC vacuum chamber wall
~ half of the electrons have E < 20 eV
R. Cimino , I.R. Collins, App. Surf. Sci. 235, 231-235, (2004)
R. Cimino et al. PRL 109, 064801(2012)
Knowing the energy distribution of electrons is of paramount importance
Complementary information

## Slide 100: Electron scrubbing
After a dose of ~ 5 1018 e/cm2 i.e. 8 mC/mm2, the maximum of SEY equals ~ 1.3
The scrubbing process desorbs several monolayers of gas from the surface
Potential impact on:
  frequency of NEG activation
  increase of SEY due to gas condensation
 | H2 | CH4 | H2O | CO | CO2
Q x 1015 | 19 | 0.4 | 4 | 2 | 3
several monolayer of gas are desorbed when a surface is conditioned
Complementary information

## Slide 101
Hydrogen desorption
H2 electron desorption can be explained by a diffusion model with a non-uniform concentration i.e. H is produced by dissociation of hydroxydes under electron bombardement
However, the diffusion coefficients taken for RT and 200ºC were the same
J. Gómez-Goñi, A.G. Mathewson. J. Vac. Sci. Technol. A 15(6) (1997) 3093
No obvious correlation between the surface composition determined by AES and desorption yields as a function of temperature : No changes in AES spectra vs 1 to 3 orders of magnitude decrease for the yields.
The thickness of the oxide layer is more than 3 monolayers (AES scanning depth).
A porous surface oxide layer provide the reservoir of gas
M.H. Achard et al., Vacuum 29-2, 53,(1978)
Electron desorption studies at different temperature
Complementary information

## Slide 102
4.5 Beam structure

## Slide 103: Multipacting: Influence of Beam Structure
VGI.134.7L1.B
VGPB.237.7R1.B
Time separation:
Non-linearity
Bunch intensity:
a threshold effect
Beam intensity:
pressure linearity
G. Bregliozzi et al., IPAC San Sebastian, 2011
Complementary information