## Slide 2: Materials fabrication in SRF cavities: beyond niobium
Sergio Calatroni – CERN
With the contribution of: Cornell U., FNAL, ICMAB, INFN-LNL, JLAB, STFC, Temple U.

## Slide 3: Outline
Motivation (one of several): the FCC-ee study
State of the art of bulk Nb
Techniques for Nb3Sn SRF cavities:
  Thermal diffusion of Sn vapours
  Liquid Sn diffusion
  Magnetron sputtering
Techniques for NbN / NbTiN SRF cavities
  Thermal diffusion of N
  Magnetron sputtering
Techniques for other materials
  MgB2
  REBCO

## Slide 4
4
The history of accelerators
Exponential development for more than 80 years
In many cases accelerator needs have been the driving force behind new technologies
Superconductivity, key technology of high-energy and high intensity machines since the 1980s (SC magnets and/or SRF)
!! Not up to date !!
Courtesy O. Brunner - CERN
Notes: US Electron-Ion Collider Project –
In US, two electron-ion colliders, eRHIC and JLEIC, have been proposed in BNL and JLab respectively

## Slide 5
The next step

## Slide 6
6
Notes: US Electron-Ion Collider Project –
In US, two electron-ion colliders, eRHIC and JLEIC, have been proposed in BNL and JLab respectively

## Slide 7: The International Linear Collider (ILC) – 500 GeV CM
Eacc 31.5 MV/m @ Q0 > 1010

## Slide 8: State of the art: bulk niobium + nitrogen doping
Courtesy A. Grassellino - FNAL

## Slide 9: What kind of doping?

## Slide 10: Results

## Slide 11: Inverse slope
Courtesy A. Grassellino - FNAL

## Slide 13: The FCC-ee parameter list

## Slide 14: The challenge of the FCC-ee
Machine | E (GeV) | ec (keV) | I (mA) | F (ph/s) | P per beam (MW) | F’(ph/s/m) | P’(kW/m)
Z | 45.6 | 19.6 | 1390 | 4.85·1022 | 50 | 6.25·1017 | 0.65
W | 80 | 105.7 | 147 | 9.30·1021 | 50 | 1.20·1017 | 0.65
H | 120 | 356.6 | 29 | 2.79·1021 | 50 | 3.59·1016 | 0.65
tt | 182.5 | 1254.5 | 5.4 | 7.88·1020 | 50 | 1.02·1016 | 0.65
Courtesy Roberto Kersevan - CERN
Z
W
H
tt2
tt1
High intensity (Z, FCC-hh): 400 MHz Nb/Cu 1-cell cavities
Higher energy (W, H): 400 MHz 4-cell Nb/Cu cavities
tt machine complement: 800 MHz 5-cell cavities (4/CM.), based on bulk Nb
~1 MW per cavity
~> 20 MV/m
Courtesy O. Brunner - CERN

## Slide 15
A promising future!
(S. Aull et al.)
Nb/Cu R&D program
Strong efforts to overcome the 'Q-slope‘ problem:
QPR studies
Innovative techniques (HIPIMS, ECR)
Cu substrate Quality & Substrate Preparation
R&D on seamless cavities
Electrodeposition of copper
A15 R&D program
New material such as NB3Sn/MgB2 could drastically improve performance
Example FCC-ee (𝑡𝑡 ̅ ): orders of magnitude
Bulk Nb
Well mature technology !
High-Q (> 3E10), high-G (>45 MV/m)
New treatments: Low-T or/and N-infusion
Cost need to be reduced !
Cryomodule design:
Active shielding
Active compensation of microphonics
Courtesy S. Aull - CERN

## Slide 16: Power losses in SRF – for a given total voltage
Length of accelerating section
Cryogenic power
Static cryogenic losses
Dissipated power

## Slide 17: Power losses
(S. Aull et al.)
A small accelerating field is favorable in circular accelerators,
in terms of overall energy consumption
Example FCC-ee (𝑡𝑡 ̅ ): orders of magnitude

## Slide 18: Surface resistance
Surface resistance
: defects, impurities, inhomogeneities, grain boundaries, hydrogen, welds, contamination, …
: “Intrinsic”
: “Extrinsic”
(500 MHz)
RBCS (4.5 K) of these A15 and B1 materials is comparable to RBCS (1.9 K) of Nb
Provided Rres is also kept similar, operation at 4.5 K could allow great power savings

## Slide 19: Outline
Motivation (one of several): the FCC-ee study
State of the art of bulk Nb
Techniques for Nb3Sn SRF cavities:
  Thermal diffusion of Sn vapours
  Liquid Sn diffusion
  Magnetron sputtering
Techniques for NbN / NbTiN SRF cavities
  Thermal diffusion of N
  Magnetron sputtering
Techniques for other materials
  MgB2
  REBCO

## Slide 20: Nb3Sn
Two main routes:
Using a bulk Nb cavity, and forming Nb3Sn on its surface , reacting either Sn vapours or Sn liquid
Using a Cu cavity, and sputter a thin Nb3Sn film on its surface, either by co- or sequential sputtering or from an alloyed target
Image by Charlie Sanabria - CC BY 4.0

## Slide 21: Furnace configurations
1970 1990 2010 2015 today
(Coordinated development work)
Image courtesy S. Posen, D. Hall - Supercond. Sci. Technol. 30 (2017) 033004

## Slide 22: Nb3Sn from vapours
Set-up of a 9-cell ILC cavity in Fermilab coating furnace (two tin sources, independent heating)
Courtesy S. Posen – FNAL (SRF 2019 talk)

## Slide 23: Thermal cycles, vapour pressures
Excess of Sn to uniformly cover all the surface is needed, before Nb natural oxide is reduced.
By means of controlled-temperature Sn source
By means of added SnCl2 source (larger Sn vapour pressure)
  (still unclear the role of Cl, might promote nucleation sites)
By means of thicker Nb oxide (anodization)
  (thicker oxide detrimental to RRR, leading to quenches)
Plots courtesy S. Posen, D. Hall - Supercond. Sci. Technol. 30 (2017) 033004

## Slide 24: Layer evolution with and without SnCl2
Slide courtesy of Uttar Pudasaini, Jefferson Lab - Thin Films 2018 Talk
With SnCl2

## Slide 25: Growth process
Sn arrives at Nb surface from Sn source
Sn reacts with Nb until full coverage of Nb3Sn is obtained.
Nb3Sn progresses by Sn diffusion through Nb3Sn grain boundaries, reaching and reacting with the Nb substrate.
Images courtesy of Uttar Pudasaini, Jefferson Lab - Thin Films 2018 Talk
Nb3Sn film grain orientation is independent from Nb grain orientation

## Slide 26: Nb3Sn layer
Slide courtesy of Ryan Porter, Cornell U.

## Slide 27: Coating (doesn’t look that much different…)
Before
After
Images courtesy of Ryan Porter, Cornell University - TTC 2018 Talk

## Slide 28: RF results: Nb bulk reference
Bulk Nb at 2 K

## Slide 29: Nb3Sn results (1.3 GHz cavities)
Plot courtesy of Uttar Pudasaini, Jefferson Lab - Thin Films 2018 Talk
Nb3Sn from JLAB
Very high Q0
Bulk Nb at 2 K

## Slide 30: Nb3Sn results (1.3 GHz cavities)
Nb3Sn from FNAL
Plot Courtesy S. Posen – FNAL (TTC 2019 talk)
Largest achieved Eacc
Bulk Nb at 2 K
Very high Q0

## Slide 31: Nb3Sn results (1.3 GHz cavities)
Plot Courtesy R. Porter – Cornell U.
Bulk Nb at 2 K
Nb3Sn from Cornell U.
4.2 K
Very good performance at 4.2 K

## Slide 32: Cryogenic efficiency: operation at 4.2 K
Plot from S. Posen, D. Hall - Supercond. Sci. Technol. 30 (2017) 033004
Potential for 1.3 GHz cavities, ILC / LCLS-II type
Plot Courtesy R. Porter – Cornell U.
@16 MV/m
Single cell cavity

## Slide 33: Nb3Sn via liquid diffusion: setup

## Slide 34: Nb3Sn via liquid diffusion: samples

## Slide 35: Nb3Sn via liquid diffusion: RF performance

## Slide 37: Nb3Sn thin films on copper
CERN: sputtering from alloyed target
STFC: co-sputtering from
Nb and Sn targets
JLAB, INFN-LNL:
multilayer sequential sputtering
Images courtesy of G. Rosaz – CERN, R. Valizadeh – STFC, N. Sayeed - JLAB

## Slide 38: Thermal treatment
Annealing temperatures | 600 - 800oC
Annealing time | 24 h… 72 h
Coating temperatures | 600 - 735oC
Additional Annealing | 24 h… 72 h
Annealing temperatures must be compatible with copper, brazed SS flanges
Cu-Sn diffusion problem
Images courtesy of G. Rosaz – CERN. [1] A. Godeke. Supercond. Sci. Technol., 19 (2006) R68-R80
Phase diagrams by C. Sanabria - CC BY 4.0

## Slide 39: Intermixing – Cu diffusion
SEM
EDS
E. A. Ilynia, G. Rosaz, et al., Supercond. Sci. Technol. 32 (2019)

## Slide 40: Barrier Layer of Ta
The Ta barrier layer is the solution in order to avoid any Cu diffusion into the Nb3Sn layer.
Courtesy of G. Rosaz – CERN. [1] A. Godeke. Supercond. Sci. Technol., 19 (2006) R68-R80

## Slide 41: RF characterization with quadrupole resonator
Calorimetric technique
Courtesy of M. Arzeo – CERN

## Slide 42: RF performance
f≈400 MHz
The slope increases with both temperature and frequency
It requires further investigation
Large sensitivity to thermal cycling
Courtesy M. Arzeo, A. Miyazaki, W. Venturini-Delsolaro – CERN

## Slide 43: Nb3Sn by sputtering: QPR results
Comparing to Nb/Cu LHC cavities
Courtesy M. Arzeo, A. Miyazaki, W. Venturini-Delsolaro – CERN

## Slide 44: Multilayer coating @ LNL (on bulk Nb)
Courtesy C. Pira – INFN-LNL

## Slide 45: RF performance at 6 GHz
Courtesy C. Pira – INFN-LNL

## Slide 46: Outline
Motivation (one of several): the FCC-ee study
State of the art of bulk Nb
Techniques for Nb3Sn SRF cavities:
  Thermal diffusion of Sn vapours
  Liquid Sn diffusion
  Magnetron sputtering
Techniques for NbN / NbTiN SRF cavities
  Thermal diffusion of N
  Magnetron sputtering
Techniques for other materials
  MgB2
  REBCO

## Slide 47: The NbN phase diagram
SC fcc phase
TC = 17.3 K
SC tetragonal phase
TC = 12÷15 K
Courtesy R. Musenich – Genova U.

## Slide 48: NbN Thermal diffusion
Reaction at 1700 K for 3 hours in 130 mbar N2

## Slide 49: The NbTiN phase diagram at 1200 °C
Equilibrium nitride phase for any Nb,Ti ratio
Segregation of other phases for non optimal composition range
Stabilization of -phase at low temperature (from Musenich)

## Slide 50: NbTiN by thermal diffusion
From R. Musenich – Genova U.
(NbTi cavities were tested as well, but NbTi is not a good candidate material)

## Slide 51: Sputter coating of cavities

## Slide 52: Nb1-xTixN by sputtering
SC NbTi magnets
Optimum for SRF

## Slide 53: Thin film coatings: reactive sputtering
Formation of nitrides
Sputtering yield: YNb > YNbN
Ar + N2
Problem understood and techniques devised to control instability and film composition: larger pumping speed, target to substrate surface ratio…
Sputtering rate [a.u.]
Substrate
Nb target

## Slide 54: Characterization by simple resonators (examples)
TE011 demountable cavity at 6.5 GHz, NbN
Microstrip resonator at 3.5 GHz, NbTiN
Very promising RBCS
High Rres
Little effect of external DC magnetic field
(Lot of work done for SC-RF devices in many labs)

## Slide 55: Cavity coatings: CEA-Saclay (TE011 plates at 4 GHz)
Tc = 16.0 K
Tc = 16.31 K
Tc = 16.17 K
Proc. SRF 1991
Proc. SRF 1993
Development towards 1.5 GHz stopped

## Slide 56: Sputtering of 500 MHz at CERN
Tcoating ≈ 200 °C
Proc. SRF 1991
Formation of nitrides
Sputtering yield: YNb > YNbN
Ar + N2
Substrate
Nb target

## Slide 57: Sputtering of 500 MHz at CERN
Proc. SRF 1991
Measured Tc ≈ 14.5 K
RBCS = 9 n
Rres = 18 n
Scaled LEP specs for bulk Nb @ 4.5 K

## Slide 58: Grain-boundary model
Phys.Rev.B 43 (1991) 6128

## Slide 59: Grain boundaries fit
Grain-Boundaries [µcm]
S.C. – Thesis 1990
intragrain ≈ 40÷50 µcm
G.B. ≈ 20÷30 µcm
30÷40% of total

## Slide 60: Sputtering of 1.5 GHz at CERN at 350 °C
M. Marino - Proc. SRF 1997
Analysis: G.B. < 20 % of the total resistivity

## Slide 61: Further developments: optimise coating temperature
Massimo Marino PhD Thesis 1999
1.5 GHz
Nb/Cu
1÷3 n
150 °C
400 n

## Slide 62: Known limitations
Limit of pumping speed
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb

## Slide 63: Known limitations
Limit of pumping speed and cathode surface
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb
Control of instabilities problematic
New techniques: pulsed sputtering (loss of efficiency)

## Slide 64: Known limitations
Limit of pumping speed and cathode surface
Cathode temperature
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb
Evolution of cathode composition during sputtering through N2 absorption.
Cooling of cathode

## Slide 65: Known limitations
Limit of pumping speed
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb
N2 to NbTi ratio depends on position, can be problematic close to sputtering threshold.
Better designs are possible

## Slide 66: Known limitations
Limit of pumping speed
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb

## Slide 67: Known limitations
Limit of pumping speed
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb
Non homogenous composition along cavity meridian
(Can be troublesome for Nb3Sn)
Better cathode design

## Slide 68: NbN and NbTiN by PE-ALD @ Cornell
Slide courtesy T. Oseroff – Cornell U.
Plasma-Enhanced Atomic Layer Deposition

## Slide 69: Outline
Motivation (one of several): the FCC-ee study
State of the art of bulk Nb
Techniques for Nb3Sn SRF cavities:
  Thermal diffusion of Sn vapours
  Liquid Sn diffusion
  Magnetron sputtering
Techniques for NbN / NbTiN SRF cavities
  Thermal diffusion of N
  Magnetron sputtering
Techniques for other materials
  MgB2
  REBCO

## Slide 70: Motivation

## Slide 71: MgB2 by HPCVD at Temple University
Courtesy Xiaoxing Xi – Temple U.

## Slide 73: RF results on samples
Courtesy Xiaoxing Xi – Temple U.
Mg-Cu eutectic liquid promote growth aty low temperature process, <500°C.
MgCu2 alloy layer grows on top of Cu substrate

## Slide 74
Courtesy Xiaoxing Xi – Temple U.

## Slide 75
Courtesy Xiaoxing Xi – Temple U.

## Slide 76
Courtesy Xiaoxing Xi – Temple U.

## Slide 77
Courtesy Xiaoxing Xi – Temple U.

## Slide 78
Poor RF properties due to poor connectivity of MgB2 coating caused by incomplete reaction of B with Mg-Cu alloy.
Longer time deposition can achieve more complete reaction.
Courtesy Xiaoxing Xi – Temple U.
Copper

## Slide 79: High-Temperature Superconductors
By PJRay - Own work, CC BY-SA 4.0, https://commons.wikimedia.org/w/index.php?curid=46193149
Y-123
YBCO
REBCO
Tl-1223

## Slide 80: REBCO: old idea, new materials and technologies
Collaboration within CERN FCC-hh study to apply HTS for beam impedance reduction
  Operation at 50 K, 16 T, needed Jc of 25 kA/cm2
S. Calatroni, E. Bellingeri, C. Ferdeghini, M. Putti, R. Vaglio, T. Baumgartner and M. Eisterer, “Thallium-based high-temperature superconductors for beam impedance mitigation in the Future Circular Collider”, Supercond. Sci. Technol. 30 (2017) 075002
T. Puig, P. Krkotić, A. Romanov, J. O’Callaghan, D. A. Zanin, H. Neupert, P. C. Pinto, P. Demolon, A. Granadeiro Costa, M. Taborelli, F. Perez, M. Pont, J. Gutierrez and S. Calatroni, “Coated conductor technology for the beamscreen chamber of future high energy circular colliders”, Supercond. Sci. Technol. 32 (2019) 094006
Important results on RF behavior of HTS in presence of strong magnetic field
  Potential use for muon collider capture cavities, SRF cavities for axion detection,
  Potential operation at 77 K

## Slide 81: REBCO: how to make cavities?

## Slide 82: Technique and results
Bonding technology under active development (first results very encouraging)
3x improvement at 8 GHz at 50 K compared to copper
expected 20x improvement at 1 GHz (f3/2)
no degradation from stacking
Courtesy J. Gutierrez - ICMAB

## Slide 83: Spin-off: axion detection
Axions as solution for strong-CP problem
Axions as dark matter candidates:
  Dark matter axions (low mass) converting to photons in B-Field
  By means of microwave cavities in solenoid magnet
  Sensitivity goes as B2 V Qcav where B is the applied field, V the total volume, Q is the quality factor of the cavity
ADMX type experiment: using tunable cavities in the ~1 GHz range

## Slide 84: ADMX
From Gianpaolo Carosi LLNL

## Slide 85: Checking other frequencies
Theoretical predictions (plot from Gray Rybka 2017)
HTS can have much better Q at lower frequencies
There is a crossover with copper at high frequencies: to be verified with our data

## Slide 86: Pictures from CAPP
Twelve sectors, with glued HTS tapes, 5.7 GHz
RADES at CERN will explore ~8 GHz

## Slide 87: Conclusions
Promising candidate new materials for SRF: A15 (Nb3Sn, V3Si, …) and B1 (NbN, NbTiN, …)
Very successful results for Nb3Sn from Sn vapour diffusion
  Technological evolution over >30 years, great leap in the past 10 years
Fast-pace evolution for Nb3Sn films on Cu
  Mastering Sn-Cu diffusion is the key for success… as in magnets!
NbN being pursued in several places
  Probably intrinsically limited by metastable -phase
NbTiN remains the best B1 candidate
  Composition accuracy and grain size need to be solved
Other innovative materials will require further developments
  MgB2 being pursued only at Temple University
  REBCO might be a viable alternative, for some niche applications. New-generation coated-conductors have very peculiar performance

## Slide 88: Acknowledgements
Cornell University: Matthias Liepe, Thomas Oseroff, Ryan Porter
Fermilab: Anna Grassellino, Sam Posen
ICMAB: Joffre Gutierrez
INFN-LNL: Cristian Pira
Jefferson Lab: Anne-Marie Valente-Feliciano
STFC: Reza Valizadeh
Temple University: Xiaoxing Xi