## Slide 2
2007:
Committee: “Proton Accelerators for the future”
Upgrade in luminosity is limited by electron cloud formation
Amorphous Carbon coatings
M. Taborelli et al: Nine years of carbon coating development for the SPS upgrade: achievements and heritage; CERN-ACC-2016-0010
Start development of amorphous Carbon coatings to mitigate electron cloud in SPS*
* NEG coating can’t be used as SPS is unbaked vacuum system

## Slide 3
The formation of electron clouds in particle accelerators.
+
+
+
+
Proton bunch (charge +)
Electron (charge -)
Gas molecule
Accelerator beam pipe
Secondary electron Yield (SEY) =
Number of emitted electrons
Number of impinging electrons

## Slide 4
Why is electron cloud formation bad?
Pressure rises.
Heat load to the cryogenic beam pipes (superconducting magnets, not for SPS).
Beam instabilities.
With upgrade of injectors LIU for HL-LHC: higher intensity => more e-cloud.

## Slide 5
Development of carbon coatings (from 2007)
Why carbon?
Graphite has a low SEY (secondary electron yield)
Threshold
for e-cloud
Threshold for e-cloud

## Slide 6
Difficulty: Coat narrow elliptical beam-pipes in Magnets
QF with elliptical beam pipe
New technique: DC Hollow Cathode Sputtering
Development of coating process

## Slide 7
Coat beam-pipes in Magnets by DC Hollow Cathode Sputtering (DCHCS)
Based on electrical confinement of electrons in plasma
Cathode:
graphite targets
(cells)
82
82

## Slide 8
Cathode:
graphite targets
(cells)
82
82
Coat beam-pipes in Magnets by DC Hollow Cathode Sputtering (DCHCS)
Based on electrical confinement of electrons in plasma

## Slide 9
SSS
1 cell = 63.995 m
Coating lab in surface building
MBB
MBB
MBA
MBA
MBA
MBB
MBB
MBA
MBA
QF
SSS
SSS
QD
QF
How to imply this in existing vacuum chambers
drifts to 181
Coating in SPS
2 units in 867
2 mobile units in SPS
SPS ARC:
Repetition of identical cells

## Slide 10
Coating in surface building ; similar for SPS mobile system
Carbon cathode in constant move
Pumping group
Gas injection system
Coating process:
20 hours
C thickness: 400 nm
Sample for SEY measurement in extension
Q..C. during process: Residual Gas Analysis & Optical emission spectroscopy (OES)
How does it look like?
Hydrogen Monitoring
Q.C. after process: - Visual inspection for short vacuum chambers
- Endoscopy for QF vacuum chambers
- SEY measurement of sample of each run: threshold: 1.1 – 1.25

## Slide 11
QC during coating run
OES
RGA
Hydrogen decrease over time
Chart: 
Time [h]
5
10
15
20
Intensity [AU]
Ar
H
substrate
aC coating

## Slide 12
88 QF magnets coated in SPS during LS2
In lab:
  96 coating runs: 110 QF type elements coated
  Round chambers: 14 runs; 29 chambers (up to 5.7 m)
During LS2
  SEY threshold: 1.25