## Slide 1: Benchmarking of Surface Conditioning – Problems of current technology & possible future development routes for electron cloud mitigation
Marcel Himmerlich on behalf of TE-VSC

## Slide 2
Motivation
Laboratory solutions for a-C coatings and CuLESS for E-cloud
mitigation have proven efficiency
Some technical constraints require rethinking of the development strategy
Definition and agreement of target thresholds for initial SEY maximum
and required conditioning dose is required

## Slide 3
Lab-based analysis of electron-conditioning
T = 293 K
SEY E-gun
COND E-gun
Analysis of SEY changes vs. Electron dose at room temperature as input
parameters for E-cloud and conditioning in the machine
Real conditioning dynamics depend on SE generation, magnetic field and
geometric aspects and have to be simulated
V. Petit et al. Phys. Rev. Acc. Beams 22, 083101 (2019)
Sample

## Slide 4
Two approaches for e-cloud mitigation
a-C film coating CuLESS
100 µm

## Slide 5
LESS – nanoparticles at the surface
ablated region
redeposited dendritic
surface layer
Surface patterning and redeposited nanoparticles define the SEY
Ablation depth, trench distance and SEY can be tuned via laser parameter adjustment
Surface is fragile and scratching, contact (i.e. RF Ball) should be avoided
Risk of particle release during a quench are currently evaluated

## Slide 6
LESS beam screen characteristics
100 µm
Ablation depth too high (< 25 μm)
Reduction of groove depth beneficial for
surface Impedance
SEY higher compared to lab LESS samples
surface conditions to SEY<1 for
electron doses <10-4 C/mm2
max.
For machine-acceptance, the laser treatment has to be developed further.

## Slide 7
Low-Particle-density laser structuring
Low-power treatment reduces particle
coverage and ablation/undulation depth
 Better for machine acceptance in terms
of impedance aspects and risk of UFOs
SEY maximum is in this case higher and
can be tuned up to Cu OFE characteristics
Courtesy of J. JJ Nivas (Univ. Naples), submitted to Appl. Surf. Sci.

## Slide 8
a-C coating with residual H2
Unintentional outgassing of
hydrogen during deposition or
intentional H2 injection leads to an
increased SEY maximum
Coating setups, especially for
magnets, do not always allow
bakeout of the system prior film
deposition
If only hydrogen is incorporated,
conditioning requires a reasonable
amount of electron dose

## Slide 9
a-C coating with H2 and Cryosorbers
Warm-up of cryosorbers induced desorption of species that affect the coating
(not only H2, also hydrocarbons)  R&D ongoing to mitigate the effect.
unconventional
conditioning behavior

## Slide 10
Discussion
Optimization of laser treatment for lower particle generation and low trench depth
+
a-C coatings in the presence of Cryosorbers
Initial SEY maximum of the surface will be > 1
Conditioning at reasonable doses will enable SEY < 1
The future development strategies requires consensus on parameters
and conditioning benchmarks
Proposal:
initial SEY maximum of the processes surfaces ≤ 1.5
Conditioning allows to reduce SEY max. to < 1 for a dose ≤ 5×10-4 C/mm2
The higher the values, the more flexibility for the treatment.