## Slide 1: Special Technical Meeting on the 11T Dipole QH-Trace to Wire Jointing Proposal to move forward
F. Savary
CERN – Virtual room https://indico.cern.ch/event/978144/ – 2020.11.27

## Slide 2: Statements, 1
Pin connector concept
  “General good quality, both connector and QH copper surfaces are in contact with the solder” [M.D. Crouvizier, M.D. Jedrychowski, M.S. Meyer]
  Can meet requirements, but two failure cases
  Caveat: the execution of the work requires great care
  The procedure is sensitive, relies too much on workmanship
Direct connection between the QH-trace and the wire
  “General good quality, wires and QH copper surfaces are in contact with the solder”
  Meet requirements
  Used in models (both QXF and 11T) and in full-length QXF, so far w/o a single failure

## Slide 3: Statements, 2
Flat connector concept
  “General good quality, both connector and QH copper surfaces are in contact with the solder”
  Can meet requirements, however internal defects have been observed
Flat connector concept, with Omega
  Does not meet the requirements
    “Majority of the connector is soldered but significant imperfections are noticed”
    “Poor bonding with the presence of large bonding imperfections”
  The execution of the work requires also great care

## Slide 4: Proposal
Based on the results of the work presented today, it is proposed to implement the solution relying on a direct connection between the QH-trace and the wire

## Slide 5: Thank you for your attention! Questions?