## Slide 1: WP4 : High Field Magnet Materials and Technology
1- Dimensional changes of Nb3Sn cables (QXF PIT) :
  Measurement of the longitudinal contraction in coil configuration: 4 tests completed.
  Still pending: Measurement of the cable thickness under 5 Mpa.
3- Measurement of the thermal conductivity on impregnated stacks of cables.
  Adaptation for the transverse configuration done and qualification of the entire facility with instrumentation almost ready.
  Measurements on 2 cables : 11T (twist pitch = 100) + QXF (twist pitch = 109).
  Samples :
    4 stacks 11T already reacted and impregnated / 2 samples Lmeasurement = 100 mm ready.
    4 stacks QXF reacted.
  3 types of tests, according to the direction of the heat flow:
New program: to be validated