## Slide 1
Status of R2D2
the Research Racetrack
Dipole Demonstrator
ADDENDUM FCC-GOV-CC-0121 - KE 3782
CEA: E. Rochepault, V. Calvelli, M. Durante, H. Felice, P. Mallon, P. Manil, G. Minier, G. Maitre, F. Rondeaux
CERN: S. Izquierdo Bermudez, J.C. Perez, D. Tommasini, J. Fleiter
27/11/2020
TM & © Lucasfilm Ltd.
All Rights Reserved

## Slide 2: Conceptual design RD 2.1 – Conductor
Expected Parameters | HF | LF
# strands | 21 | 34
strands | 1.1 mm | 0.7 mm
Pitch angle | 16.5 deg | 16.5 deg
Transposition pitch | 85.0 mm | 85.0 mm
Cu/Sc ratio | 0.8 | 2
Insulation | 0.15 mm | 0.15 mm
Expected Dimensions (reacted & insulated) | 2.36 x 13.04 mm | 1.61 x 13.04 mm
Expected Parameters | HF | LF
# strands | 21 | 34
 | 1.1 mm | 0.7 mm
Pitch angle | 16.5 deg | 16.5 deg
Transposition pitch | 85.0 mm | 85.0 mm
Cu/Sc ratio | 0.8 | 2
Insulation | 0.15 mm | 0.15 mm
Expected Dimensions (reacted & insulated) | 2.36 x 13.04 mm | 1.61 x 13.04 mm
Chart: B (T)
Conductor expected T1 2021  TBC
LF cable very similar to the 11-T cable
HF cable new, 1.1 mm strand
 risk of changes in dimensions, mitigated with dimensional margins
Jc and RRR extrapolated
 risks of impact on the design, mitigated with design margins

## Slide 3: Conceptual design RD 2.1 – R2D2 in F2D2
V 4.8.15 | Nominal @ 1.9 K
I | 15917 A
LL margin HF / LF | 22.4 % / 14.0 %
B @ (0,0) | 11.46 T
B peak HF / LF | 12.61 T / 9.77 T
Original idea: layer 3 only, same structure
IR2D2 ~ 160% IF2D2
 protection issues  margin to 20%
Steep load-line
 Stability issue  trade-off low Jc/high RRR
Grading not optimized
 need to redesign the coil
Chart: B (T)
LL HF F2D2 | 566.07 | 1373.07
LL LF F2D2 | 724.79 | 4951.02
HF WP | 1311.8832
LF WP | 3359.5445

## Slide 4: Conceptual design RD 2.1 – R2D2 in F2D2
Too much pre-load because of the thick shell
High peak stress
Need to redesign the structure
Different fillers and pads
 Marginal cost saving
0.10 mm Xinterf
0.05 mm Yinterf
+cool-down
208 MPa
Nominal:
13.38 kA, 11T
201 MPa
Short sample:
16.88 kA, 11T
205 MPa
v6.9.16

## Slide 5: Conceptual design RD 2.1 – Preliminary protection
Chart: JCu (A/mm²)
| 1335.6812688881546
F2D2 v4815 HF | 149
F2D2 4815 LF | 315
R2D2 4815 | 506
R2D2 4815 | 1215
R2D2 4816 | 967
R2D2 4816 | 1293
R2D2 6917 | 189
R2D2 6917 | 294
R2D2 6917 | 348
R2D2 6917 | 729
R2D2 611R1 | 199
R2D2 611R1 | 333
Hypothesis (Tiina’s spreadsheet):
  Adiabatic Regime
  Every coil has a quench heater
  No quenchback
  Rdump = 1000 V / I0
  No Differential inductance
  Magnetoresistivity
  Detection delay = 20 ms
  Heater activation delay = 20 ms
  Max. hotspot 350 K
Additional difficulty of R2D2 due to a high JCu
 Similar MIITS of F2D2 at 4.2 K
 Does not seems possible to operate at SS 1.9 K
Detailed simulations with COMSOL ongoing
Safe zone
Limit zone
Design iterations

## Slide 6: Conceptual design RD 2.1 – 2D Magnetic
Parameter | NOM 4.2 K | NOM 1.9 K | Ultimate | SS 4.2 K | SS 1.9 K | Unit
Current | 13772 | 15055 | 16500 | 17215 | 18819 | A
LL Margin HF LF | 20.0 20.5 | 20.9 20.0 | 4.2/1.9 K 4.2/12.9 4.5/11.3 | 0.0 0.7 | 0.9 0.0 | %
B (0,0) | 10.42 | 11.15 | 11.98 | 12.46 | 13.29 | T
B peak HF | 11.82 | 12.69 | 13.67 | 14.27 | 15.23 | T
B peak LF | 7.68 | 8.32 | 9.05 | 9.49 | 10.21 | T
Energy density | 474 | 553 | 649 | 725 | 818 | kJ/m
JCu HF JCu LF | 1472 1508 | 1627 1667 | 1827 1783 | 1853 1886 | 2034 2084 | A/mm²
Hotspot HF / LF | 104 / 141 | 135 / 203 | 210 / 350 | 260 K / 450 K | 580 / 1192 | K
11 T Nominal « guaranteed » (20 % margin, low Jc)
12 T Ultimate achievable (350 K conservative)
Possibility to explore high MIITS above Ultimate
Chart: B (T)
| 12.75
HF WP 1.9K | 1286.4664
LF WP 1.9K | 3294.4558
HF UWP | 1404.2863
LF UWP | 3606.4618
HF WP 4.2K | 1174.8088
LF WP 4.2K | 2974.5742

## Slide 7: Conceptual design RD 2.1 – 2D Mechanical
v6.14.R2
v6.9.16
Parametric analysis to select best Shell Vs yoke dimensions:
Energization at 18819 A
Pre-loading
Structure allows both:
Low preload for nominal
High preload up to SS 1.9K
Structural components below limits at all steps
Shell Thick. (mm) | 26 | 22 | 20 | 22 | 22 | 22
Yoke Ext. Rad. (mm) | 190 | 190 | 190 | 195 | 210 | 220
Overall Rad. (mm) | 216 | 212 | 210 | 217 | 232 | 242
Yoke OK? | No | No | No | No | No | Yes
Coil Contact OK? | Yes | No | No | Yes | Yes | Yes

## Slide 8: Conceptual design RD 2.1 – 2D Mechanical
Preload – 0.2 mm interf.
Cool-down to 4.2K
13772 A, 10.4 T
Preload – 0.6 mm interf.
Cool-down to 1.9 K
16500 A, 12.0 T
Preload – 0.7 mm interf.
Cool-down to 1.9 K
18819 A, 13.3 T
Nominal 4.2 K
Ultimate
Short sample 1.9 K
112 MPa
158 MPa
169 MPa
109 MPa
95 MPa
36 MPa
218 MPa
193 MPa
133 MPa
5 MPa
15 MPa
0 MPa

## Slide 9: Conceptual design RD 2.1 – 3D Magnetic
Return End
Criteria:
Bpeak spacer < Bpeak center
Bpeak center - Bpeak spacer > 0,5 T if possible
Guarantee a minimum ‘good field’ length
Max. coil length 1300 mm

## Slide 10: Conceptual design RD 2.1 – 3D Magnetic
Location | Bpeak [T] | ΔBpeak [T]
SS, HF | 11,85 | 0
LE, HF | 10,26 | 1,59
RE, HF | 11,22 | 0,63
Outer lead HF | 7,26 | 4,59
Inner lead HF | 11,12 | 0,73
SS, LF | 7,75 | 0
RE, LF | 7,50 | 0,25
LE, LF | 7,66 | 0,09
Inner Lead LF | 7,51 | 0,24
Additional complexity due to racetracks
Need for spacers to decrease peak field in the ends
Not possible to optimize further the critical LF areas given the length constraint
130 mm ‘good field’ length

## Slide 11: Mockups RD 2.1 – Layer jumps (F2D2)
Mock-up A
Mock-ups made with a SMC 11T cable
Goals : validate concepts of exit jumps and develop procedures
Mock-up B

## Slide 12: Mockups RD 2.1 – Bending tests
Hard-way: SMC 11T bare cable  Safe Radius 450 mm defined
EasyWay: FRESCA2 insulated cable  Safe Ratio defined
250 mm
OK
OK
OK
COLLAPSE
NO
OK
OK
OK
NO

## Slide 13: Mockups RD 2.1 – Splices
Goal: validate procedure with 3D printed components and tooling
Fast turnover to allow modifications in the design
Dimensions adapted to the 11-T cable
Engineering design almost complete
Fabrication foreseen December, tests in January

## Slide 14: Mockups – Structure
HPP
C&T
LBNL
Goals:
Qualify bladder manufacturers
Validate Assembly procedures
Train on strain gauge implementation
Tests at cryogenic temperatures
Full test with dummy Al done
Full test with dummy Nb3Sn foreseen

## Slide 15: Enginnering design RD 2.2 - Coils
Straight section 243 mm
Ext. straight section 474 mm
Detailed turn-by-turn model with inputs from models and mockups:
Minimum bending radius:
Magnetic design
Mechanical/geometrical constraint
Project spec.

## Slide 16: Enginnering design RD 2.2 – Coil Components
Preliminary design only, detailed design ongoing.
Titanium
Stainless steel (SS)
Iron
Insulation filler
Insulation

## Slide 17: Enginnering design RD 2.2 – Coil Components
External splice concept
Preliminary design of the splice area.
To be validated with mockups
Layer jump LF forerunner
Layer jump HF
forerunner
Exit jump HF
Straight exit LF
[2 coils represented here]

## Slide 18: Enginnering design RD 2.2 – Winding tooling
Preliminary design only, detailed design ongoing.
To be validated with mockups

## Slide 19: Enginnering design RD 2.2 – Reaction tooling
Split tooling to allow for coil contraction
Preliminary design only, detailed design ongoing.
To be validated with mockups

## Slide 20: Enginnering design RD 2.2 – Structure
Simplified design imported from 3D magnetic model to check compatibility with coil components
Detailed design to be done
Iron yoke
SS rails
SS endshoe
Fillers (iron + ins.)
Titanium post
& spacers

## Slide 21: SMC RD 2.2a
Goals:
validate coil manufacturing process on a small scale
Coil fabrication at CEA (1 coil foreseen, components for 2)
Assembly and tests at CERN
Status:
ULs and Components received at Saclay
Tooling ready for winding
Furnace calibration foreseen
CEA impregnation tooling
   New design, under procurement
Instrumentation procedure under definition
Start manufacturing in January 2021

## Slide 22: Conclusions
Rescoping from F2D2 to R2D2
  Reduced number and size of coils
  Fits cost and schedule
But: non-anticipated difficulties
  Peak field in the ends due to racetracks
   Coil end optimization
  Difficult stability + protection due to high current
   Additional Jc and operational margins
Planning and deliverables:
  Conceptual design almost complete (RD-2.1)
  Detailed design started (RD-2.2b)
  SMC fabrication ready to start (RD-2.2a)
Various Mockups to validate concepts (RD-2.1)
  Need for conductor

## Slide 23
Backup slides

## Slide 24
Courtesy H. Felice

## Slide 25: Ideas on an integrated strategy
SMC 11T
Conductors
Pre-stress
Materials (Insulations etc.)
R2D2
Demonstrate Grading ≥ 12 T
‘Reduced’ demo. (FD?)
Grading + Flared-ends ≥ 14 T
+Grading
ERMC
(= ‘reduced’ RMM)
Demonstrate 16 T
RMM
Demonstrate
aperture =16 T
+Aperture
+Flared ends
+Flared ends
FRESCA2 (but 100 mm aperture)
Flared-ends + aperture ≥ 14 T
"Demonstrator" (F2D2?)
Grading + Flared-ends + Aperture = 16 T
+Aperture
+Grading
+Field

## Slide 26: Ideas on an integrated strategy
Demonstrator1
Flared-ends
+ 50 mm aperture ≥ 14 T
*
SMC 11T
Conductors
Pre-stress
Materials (Insulations etc.)
R2D2
Demonstrate Grading ≥ 12 T
‘Reduced’ demo. (FD?)
Grading + Flared-ends ≥ 14 T
+Grading
ERMC
(= ‘reduced’ RMM)
Demonstrate 16 T
RMM
Demonstrate
aperture =16 T
+Aperture
+Flared ends
+Flared ends
"Demonstrator" (F2D2?)
Grading + Flared-ends + Aperture = 16 T
+Aperture
+Grading
+Field

## Slide 27: Development plan toward 16 T Dipoles for FCC
1. SMC 11T (=Short Model Coil) [10]
Racetrack coils
No grading  Demonstrate field ≥ 12 T
2. R2D2 (=Research Racetrack Dipole Demonstrator)
Racetrack + Grading ≥ 12 T
3. FD (=Flared Dipole)
Grading + Flared-end coils ≥ 14 T
4. F2D2 (=FCC Flared-ends Dipole Demonstrator)
Reuse FD coils + structure
Grading + Flared-end coils + Aperture = 16 T
+Flared ends
+Aperture
[10] J.C. Perez et al., “Performance of the Short Model Coils Wound With the CERN 11-T Nb3Sn Conductor”, IEEE TAS 2015
+Grading

## Slide 28: Development plan toward 16 T Dipole for FCC
1. SMC 11T (=Short Model Coil) [10]
Racetrack coils
No grading  Demonstrate field ≥ 12 T
2. R2D2 (=Research Racetrack Dipole Demonstrator)
Racetrack + Grading ≥ 12 T
3. FD (=Flared Dipole)
Grading + Flared-end coils ≥ 14 T
4. F2D2 (=FCC Flared-ends Dipole Demonstrator)
Reuse FD coils + structure
Grading + Flared-end coils + Aperture = 16 T
+Flared ends
+Aperture
Current collaboration agreement
+Grading

## Slide 29: Development plan toward 16 T Dipole for FCC
1. SMC 11T (=Short Model Coil) [10]
Racetrack coils
No grading  Demonstrate field ≥ 12 T
2. R2D2 (=Research Racetrack Dipole Demonstrator)
Racetrack + Grading ≥ 12 T
3. FD (=Flared Dipole)
Grading + Flared-end coils ≥ 14 T
4. F2D2 (=FCC Flared-ends Dipole Demonstrator)
Reuse FD coils + structure
Grading + Flared-end coils + Aperture = 16 T
+Flared ends
+Grading
+Aperture
Future agreement to be discussed

## Slide 30: New Organization
CEA Project leader
E. Rochepault
Conceptual Design
E. Rochepault
Magnet Assembly
E. Rochepault
Coil Manufacturing
F. Rondeaux
Instrumen-tation
S. Perraud
Magnet Test
E. Rochepault
Mechanics
E. Rochepault
Winding R&D
M. Durante
Engineering Design
P. Manil
R&D and tests
M. Durante
Protection
V. Calvelli
Magnetics
V. Calvelli
Quality control
F. Rondeaux
Procedures
F. Rondeaux
Procurement
F. Rondeaux
Manufacturing supervision
F. Rondeaux
CAD
G. Minier
Drawings
G. Minier
Quality control
S. Perraud
Procedures
S. Perraud
Procurement
S. Perraud
Assembly supervision
S. Perraud
Mechanical analysis
E. Rochepault
Quench analysis
V. Calvelli
Magnetic analysis
V. Calvelli
Splice R&D
M. Durante
Structure R&D
S. Perraud
Conductor tests
M. Durante
Mechanical
S. Perraud
Electrical
S. Perraud
Protection
S. Perraud
Reaction R&D
M. Durante
Impreg. R&D
M. Durante
Former:
H. Felice
SMC
G. Maître
Magnetic
S. Perraud
Former:
P. Mallon

## Slide 31: New Organization
Infrastructure
M. Durante
CEA Project leader
E. Rochepault
Conceptual Design
E. Rochepault
Magnet Assembly
E. Rochepault
Coil Manufacturing
F. Rondeaux
Instrumen-tation
S. Perraud
Magnet Test
E. Rochepault
Mechanics
E. Rochepault
Winding R&D
M. Durante
Engineering Design
P. Manil
R&D and tests
M. Durante
Protection
V. Calvelli
Magnetics
V. Calvelli
Quality control
F. Rondeaux
Procedures
F. Rondeaux
Procurement
F. Rondeaux
Manufacturing supervision
F. Rondeaux
CAD
G. Minier
Drawings
G. Minier
Quality control
S. Perraud
Procedures
S. Perraud
Procurement
S. Perraud
Assembly supervision
S. Perraud
Mechanical analysis
E. Rochepault
Quench analysis
V. Calvelli
Magnetic analysis
V. Calvelli
Splice R&D
M. Durante
Structure R&D
S. Perraud
Conductor tests
M. Durante
Mechanical
S. Perraud
Electrical
S. Perraud
Protection
S. Perraud
Reaction R&D
M. Durante
Impreg. R&D
M. Durante
SMC
G. Maître
Magnetic
S. Perraud
Procurement
LRI
Quality
control
S. Roux

## Slide 32: Simplified schedule
 | 2020 | 2021 |  |  |  | 2022 |  |  |  | 2023 |  |  |  | 
 | T4 | T1 | T2 | T3 | T4 | T1 | T2 | T3 | T4 | T1 | T2 | T3 | T4 | 
Conceptual Design | Méca+ quench |  |  |  |  |  |  |  |  |  |  |  |  | 
Engineering Design |  |  |  |  |  |  |  |  |  |  |  |  |  | 
R&D and tests |  | Tests Splices | Tests conducteur | Tests bobinage | Tests imprégnation | Cu coil |  |  |  |  |  |  |  | 
Coil Manufacturing | Fabrication SMC |  |  |  |  | Cu coil | Nb3Sn coils |  |  |  |  |  |  | 
Magnet Assembly |  |  | R&D structure |  |  |  | Test à froid |  |  | Assemblage |  |  |  | 
Instrumentation |  | Design QH |  |  | Implementation QH | Implementation SG |  |  |  |  | Instrum tests |  |  | 
Magnet Test |  |  |  |  |  |  |  |  |  | Analyse méca | Analyse méca+magn +quench |  |  | 
RD-2.1 Conceptual design report F2D2/R2D2
Internal review conceptual design R2D2
Engineering design Review R2D2
RD-2.2b
Engineering design report R2D2
Conceptual Design Review R2D2
Coil fabrication readiness review
RD-3.1
R2D2 Cu coil
RD-4.1
R2D2 Magnet
Assembly readiness review
RD-3.2
R2D2 Nb3Sn coils
RD-4.2b
Test reports
RD-4.2a
Manufacturing folder
RD-2.2a
SMC coil

## Slide 33: Budget following rescoping
Following rescoping: Re-estimate of costs components/tooling
Is conductor envelope still the same ?
  Transferable to tooling?
  additional conductor?
 |  |  |  | CERN |  |  | 
R2D2 components | CERN | 301 500 € |  | material total | Material budget | diff | 
R2D2 large tooling | CERN | 126 000 € |  | 877 500 € | 900 000 € | - 22 500 € | should cover SMC
F2D2 conductor | CERN | 450 000 € |  |  |  |  | 
R2D2 conductor | CERN | 150 000 € |  |  |  |  | 
R2D2 small tooling | CEA | 116 800 € |  | CEA |  |  | 
 |  |  |  | material total | contingency | TOTAL | 
Consumables | CEA | 8 000 € |  | 144 400 € | 50 000 € | 194 400 € | 
mock ups | CEA | 19 600 € |  |  |  |  |