## Slide 1: Measuring conductivity of coated surfaces at high frequency
Andrea Passarelli

## Slide 2: Coatings at high frequency
EM characterization of “coating materials” is fundamental to evaluate accelerator performance limitations and build up a machine impedance model.
Surface impedance of the beam pipe depends on electromagnetic properties of coatings.
Layers of coating materials can significantly increase the resistive wall impedance at high frequency
Low conductvity, thin layer coatings (NEG, a‐C)
Rough surfaces (not taken into account so far)

## Slide 3: Outline
Coating characterization for RW
From Zs to Zwall
Conclusion

## Slide 4: Outline
Coating characterization for RW
  Proposed method
  The DUT
  Analytical evaluations
  Measurement results
  Outlook
From Zs to Zwall
Conclusion

## Slide 5: The goal of the study
To develop a reliable, handy and inexpensive system for the electromagnetic characterization
of Coating material in Sub-THz range.
NEG
Non-Evaporable Getter
TERA K15
Time-Domain THz Spectrometer

## Slide 6: The proposed method
Evaluation of the signal attenuation inside a DUT with coating deposited.
Electromagnetic characterization
of coating material.

## Slide 7: The DUT
Material | Iron
Waveguide | Circular
Length | 42
Radius | 0.9
Horns | Pyramidal
Length | 39
External side | 6
Total Length | 120
Dimension in mm
Pyramidal Horns
Circular waveguide

## Slide 8: The DUT
Reference
Measure
Advantages of this setup
Homogeneous deposition
Reusability of the system
Large area coating.

## Slide 9: Analytical evaluations
Power attenuation per length unit α is defined by:
The attenuation α due to the losses in the walls is:
N.Markuvitz – Waveguide Handbook
Zs : surf. char.imp.
Z : mode char.imp.
Htan : tang. mag. field
Ht : trans. mag. field

## Slide 10: Analytical evaluations
Waveguide radius a [mm] | Frequency range [GHz]
0.9 | 100-280
Single-mode regime analysis
The frequency range goes from fTE1,1 to fTE1,2

## Slide 11: Analytical evaluations
Along the foil of length lg :
The attenuation for TE1,1 mode:

## Slide 12: Analytical evaluations
Cu
NEG
d

## Slide 13: Analytical evaluations
Waveguide length: 42mm
Waveguide radius: 0.9mm
Copper conductivity: σcu = 6∙107 S/m NEG conductivity: σNEG = 3.5∙105 S/m*
Good agreement between FD CST simulations and analytical evaluations.
*E. Koukovini Platia et al.
Phys. Rev. Accel.Beams 20, 011002 (2017)

## Slide 14: Analytical evaluations
Along the foil in the transitions of length lt:
The attenuation for the sum of TE1,0 and TE 0,1 modes:
Pyramidal transitions to enhance the signal collection.

## Slide 15: Analytical evaluations
Transition length: 39mm
Transition side: 6mm → 0.9mm
Good agreement between FD CST simulations and analytical evaluations.
Copper conductivity: σcu = 6∙107 S/m NEG conductivity: σNEG = 3.5∙105 S/m*
*E. Koukovini Platia et al.
Phys. Rev. Accel.Beams 20, 011002 (2017)

## Slide 16: Analytical evaluations
Cylindrical waveguide +
Pyramidal transition
Reliable analytical tool
Copper conductivity: σcu = 6∙107 S/m NEG conductivity: σNEG = 3.5∙105 S/m*
*E. Koukovini Platia et al.
Phys. Rev. Accel.Beams 20, 011002 (2017)

## Slide 17: Measurement results
XRF in ATELIER DE TRAITEMENTS DE SURFACE
3.96 μm
3.68 μm

## Slide 18: Measurement results
Average of 5 repeated measurements

## Slide 19: Measurement results

## Slide 20: Measurement system upgrade
System specifications:
Spectral Range: > 3 THz
Dynamic Range > 70 dB
Scanning Range ~ 300 ps
Spectral Resolution < 3.5 GHz
Upgrade:
> 5 THz
> 90 dB
~ 850 ps
< 1.5 GHz
More accurate guiding system manufacturing

## Slide 21: Measurement results on a-C
Two samples with 3 μm of Amorphous carbon on copper bulk
Mechanical stress with 3 μm of a-C on cu slab

## Slide 22: Measurement results on a-C
Shown for the first time → CERN note will be published soon

## Slide 23: Outlook
New collaboration agreement
between CERN & INFN Naples in the framework of INFN ARYA project:
Realization of different laser surface treatments focusing on reduced nanoparticle formation (collaboration with Unina) and their EM characterization
Improving the sensitivity for the characterization of very thin structures resorting on resonant structure methodology
Dielectric resonator

## Slide 24: Outline
Coating characterization for RW
From Zs to Zwall
  Tools and methods
  Transmission line theory
  Comparison IW2D and TL for FCC e+e-
Conclusion

## Slide 25: Tools and methods
Two main tools with two different approach:
Transmission line theory
  To calculate the resistive wall impedance of a multilayer round chamber
  Can be applied recursively to take into account whatever number of layers
  Leontovich boundary condition required
  Ref: PhD thesis Carlo Zannini (EPFL 2013)
ImpedanceWake2D
  Solves Maxwell’s equation in frequency domain for a multilayer vacuum chamber made of arbitrary materials
  Field matching at all material boundaries
  Outputs the impedance contributions as a function of frequency
  Ref: PhD thesis Nicolas Mounet (EPFL 2012)

## Slide 26: From experimental 𝜎 to Zwall
Leontovich boundary condition
EM fields ⇒ planewave orthogonal to separation surfaces.
The condition imposed only for 1st layer: for field continuity, propagation direction is orthogonal through all the media.
b
for
(in case of high energy (β=1) and relatively not too high frequency)
info on : L. Vos: CERN-AB-2003-005 ABP
The transmission line approach

## Slide 27: IW2D vs. TL
TL
TL
IW2D
IW2D
M. Migliorati, Phys. Rev. Accel. Beams, vol. 21, p. 041001, Apr 2018.
FCC e+e-

## Slide 28: IW2D vs. TL
TL
TL
IW2D
IW2D
M. Migliorati, Phys. Rev. Accel. Beams, vol. 21, p. 041001, Apr 2018.
FCC e+e-

## Slide 29: Outline
Coating characterization for RW
From Zs to Zwall
Conclusion

## Slide 30: Conclusion
Sub-THz electromagnetic characterization of coating materials
  Reliable analytical model for the conductivity retrieval. Good agreement with CST Frequency Domain solver.
  Successful measurement campaign: reliable, handy and inexpensive method to evaluate the electromagnetic properties of samples under test.
  Published results on NEG and novel ones on a-C coatings.
  Outlook: characterization of different coating material (i.e. LESS) and extension of the frequency range.
From surface impedance Zs(conductivity 𝜎) to resistive wall impedance Zwall
  Transmission line theory is a flexible, stable and fast tool for resistive wall impedance evaluation (metallic boundary condition required at 1st layer)
Thank you!

## Slide 31
Backup slides

## Slide 32: Skin depth

## Slide 33: a-C Coatings
One side coating
Good thickness 5μm No Peel off
Sample under stress.
Two sides coating
Good thickness ~5μm
Peel off
No stress on foil

## Slide 34: NEG Coatings
Two sides coating
No peel-off
No stress on foil
Thickness of 3.1μm
ROTATING FRAME

## Slide 35: Approximation
The two transitions between the pyramidal horns and the cylindrical waveguide is neglected in the analytical evaluation.
0.9 mm
1.2728 mm
Square
waveguide
Circular
waveguide

## Slide 36: Measurement system
0
1
100
T-Light/
FS-Laser
ODU
PortA
PortB
Input fiber port
Output fiber port
Tx
Tera15-SL25-FC
Rx
Tera15-DP25-FC
Attenuator
Lens1
Lens2
Lens3
Lens4
2F
DDS Out1
PA310
Supply
Out
±15V
Vin
System specifications:
Spectral Range: > 3 THz
Dynamic Range > 70 dB
Scanning Range ~400ps
Spectral Resolution < 3GHz
N

## Slide 37: Previous work
Electromagnetic characterization of NEG Coatings in waveguides at high frequency
The operating principle we are going to present
overcomes two main inconveniences of this work:
Non-homogeneous deposition
Impossibility to reuse the same
waveguide for further measurements
E. Koukovini Platia et al.
Phys. Rev. Accel.Beams 20, 011002 (2017)

## Slide 38: Analytical evaluations
Boundary conditions
Polarization of planar wave

## Slide 39: Analytical evaluations
Waveguide side a [mm] | Frequency range [GHz]
 | 118-263
Waveguide side a [mm] | Frequency range [GHz]
 | 118-263
a
The frequency range goes from fTE1,0= fTE1,0 to fTE2,1 = fTE1,2
Boundary conditions
Polarization of planar wave