## Slide 1: Total and Double Differential Scattering Cross-Section Measurements of Isotropic Graphite
Atsushi Kimura, Shunsuke Endo, Shoji Nakamura
Japan Atomic Energy Agency

## Slide 2: Contents
Introduction
Samples
J-PARC Facilities
Double differential Scattering Cross-Section Measurement
Total Cross-Section Measurement
Summary

## Slide 3: Introduction
low atomic mass number
small neutron capture cross-section,
high neutron scattering cross-section, ⇒Sufficient neutron moderation capability
Nuclear-grade graphite has been considered as an efficient neutron moderator and reflector for the following reasons:
easy availability, and
comparatively low cost. ⇒Engineering Advantages
Notes: First, I’ll show you the introduction of this presentation.
As you know, graphite has been considered as an efficient neutron moderator and reflector.
This is because,
Graphite has ……
These mean graphite has sufficient neutron moderation capability.
Overmore, graphite is easy availability and low cost.
They are big advantages for engineering.

## Slide 4: Introduction②
Graphite has been used in many reactors. For example, in the case of High Temperature Engineering Test Reactor (HTTR)…
Schematic view of components and reactor core vessel of HTTR[1]
[1] T. Nishihara, et al., Excellent Features of Japanese HTGR Technologies, JAEA-Technology 2018-004, 2018.
HTTR is the high-temperature gas-cooled reactor in JAEA.
The first criticality of the HTTR was achieved in 1998. The reactor outlet coolant temperature was 950℃ under full thermal power of 30MW.
Fuel assembly
Notes: Therefore, Graphite has been used in many reactors.
For example in the case of High temperature engineering test reactor, HTTR,
Graphite is used in these reflector block, fuel assembly and upper and lower plenum.
This photo shows the fuel assembly of HTTR.
This is made by fine graphite.

## Slide 5: Introduction③
Graphite is widely used in many reactors as a moderator and reflector.
To obtain low energy (E < 1 eV) neutron spectrum accurate neutron total and DDSCS are required.
The total cross-section and DDSCS of graphite samples with different properties have been measured in the Materials and Life Science Experimental Facility (MLF) in the J-PARC.
Unfortunately, in this energy region, the cross sections are affected by the thermal neutron scattering law.
The results in large differences between samples in the case of graphite.
Notes: As you seen, graphite widely used in many reactors as moderator and reflector.
Accurate cross section of the graphite in the low energy region is very important to deduce neutron spectrum.
However, in this energy region, the cross sections are affected by the thermal neutron scattering law due to the crystal structure.
The reported results have large discrepancies.
Therefore, we have measured total C.S. and DDSCS of graphite in the Materials and Life Science Experimental Facility (MLF) in the J-PARC.

## Slide 6: Samples

## Slide 7: Samples①~What is Isotropic Graphite?~
Five isotropic graphite samples with different porosities, densities and grain sizes were selected as samples.
~What is Isotropic Graphite?~
Isotropic graphite is a graphite that is isotropically formed by cold isostatic pressing (CIP) method.
Isotopic graphite has:
high density, high strength,
uniform characteristics in three dimensions.
[1]Jun Tojo, TANSO, Vol.2008, pp.234, (2008).
Isotropic graphite is widely used for general industrial components such as semiconductor manufacturing equipment.
Many suppliers sell many types of isotropic graphite. (Easy to choice)
The raw material is filled into a rubber mold, placed in a pressure vessel filled with water or oil, and pressurized to form the product.
Notes: In the measurements, we have used Five isotropic graphite samples with different porosities, densities and grain sizes.
First, I’ll show you “What is isotropic graphite?”.
Isotropic graphite is a graphite that is isotropically formed with cold isostatic pressing (CIP).
In cold isostatic pressing, as shown here,
the raw material is filled into a rubber mold,
placed in a pressure vessel filled with water or oil, and pressurized to form the product.
As a result, Isotopic graphite has high density, high strength, and uniform characteristics in three dimensions.
Using these excellent properties, Isotropic graphite widely used for general industrial components.
Furtermore, Many suppliers sell many types of isotropic graphite.
We can choice several properties.

## Slide 8: Samples ~Properties~
Difference of typical properties between isotropic graphite and nuclear grade graphite and carbon
[1]M. Ishihara et al. / Nuclear Engineering and Design 233 (2004) 251–260
 | ET-34 (Isotropic graphite) | PGX graphite (WG)[1] | ASR-0RB carbon[1]
Bulk density (g/cm) | 1.86 | 1.73 | 1.69
Tensile strength (MPa) | 50 | 8.1 | 6.8
Compressive strength (MPa) | 120 | 30.6 | 50.4
Young’s modulus (GPa) | 11 | 6.5 | 8.7
Thermal expansion coefficient | 3.9 | 2.3 | 4.4
Thermal conductivity (W/(mK)) | 150 | 75 | 10
Ash (ppm) | Max. 100 | Max. 7000 | Max. 5000
Grain size (μm) | Mean 15 | Max 800 | Max 2000
Notes: This table shows difference of typical properties between isotropic graphite and nuclear grade graphite and carbon.
As you can see, Isotropic graphite has higher density, strength thermal conductivity, and high purity and low grain size.

## Slide 9: Samples ~X-ray photo~
https://www.toyotanso.com/Products/Special_graphite/
Four Japanese companies, Toyo Tanso, Ibiden, Tokai Carbon, and Shin Nippon Techno Carbon, hold approximately 65% of the world's isotropic graphite market share.
Isotropic graphite has a high density and a micro particle structure comparison to anisotropic graphite.
Photo of typical isotropic and anisotropic graphite
Demerit: Cost and Size (Largest size is typically 1m x 50cm x 50cm)
Notes: These pictures are X-ray photo of typical isotropic carbon and traditional carbon.
The pictures are taken from this HP.
This is not a picture of our samples.
However, as you can see, isotropic graphite has a high density and a micro particle structure comparison to anisotropic graphite.
Of course, Isotropic graphite has disadvantage.
One is cost and the other one is size.

## Slide 10: Samples ~Isotropic graphite in reactors~
Schematic view of HTTR[1]
Fuel assembly made of isotropic graphite
[1] T. Nishihara, et al., Excellent Features of Japanese HTGR Technologies, JAEA-Technology 2018-004, 2018.
Isotropic graphite used in Chinese HTRs, HTR-10 and HTR-PM, and first wall of fusion reactors.
Thanks to its excellent properties:
Easy to Machine
Ultra Heat Resistance,
Sufficient strength and
Highly consistent quality,
Isotropic graphite was used as moderators in the HTTR.
Notes: Using these excellent properties, isotpropic graphite is used in HTTR.
IN this fugure, these parts are made of isotropic graphite.
This Fuel assembly made of isotropic graphite
Isotropic graphite used in Chinese HTRs, HTR-10 and HTR-PM, and first wall of fusion reactors.

## Slide 11: Samples
 | Density (g/cm3) | Porosity※ （％） | Grain size※ (μm) | Purpose ※Typical (nominal) value
ET-10 | 1.75(1.75)※ | 15 | 15 | Graphite for general purposes: Industrial furnaces, and reactors (Made with similar process)
ET-11 | 1.76(1.77)※ | 14 | 13 | 
ET-34 | 1.84(1.86)※ | 11 | 15 | 
ED4 | 1.90(1.90)※ | 9 | 1 | Graphite for EDM （Electrical Discharge Machining）
T-8 | 1.88(1.85)※ | 9 | 5 | Graphite for ion implanters (High purity < 5ppm)
Five isotropic graphite samples were prepared for the experiments.
The samples have different densities, porosities and grain sizes.
Shape: cylindrical: 10mmφ, 10mmH
The samples were supplied by Ibiden Co. Ltd.
Impurities are less than 100 ppm.
Notes: Therefore, we have prepared Five isotropic graphite samples with different densities, porosities and grain sizes.
This picture shows the samples.
The samples are cylindrical shape and diameter of 10mm and height is 10mm
The table show a properties of the samples.
In the table, the values are typical value except for density without brackets.
These, ET-10, -11 and 34, are graphite for general industrial purposes.
These are made by similar process.
ED-4 is a very small grain size sample.
That is used for EDM.
T-8 is high purity sample.
Impurity is less than 5 ppm.
Impurities of the other samples are less than 100 ppm.
The samples were supplied by Ibiden Co. Ltd.

## Slide 12: Facilities

## Slide 13
Facility J-PARC : Japan Accelerator Research Complex
LINAC
180MeV
RCS
3GeV
MR
30GeV
Hadron physics
Neutrino experiment
MLF
(neutron exp.)
4
Notes: First I will show you a out line of J-PARC.
*There are three proton accelerators in J-PARC.
*One linear accelerator and two synchrotrons.
*180MeV protons from the linear accelerator are injected into RCS and accelerated up to 3 GeV.
*3GeV protons are transported to MLF or MR for high energy experiment such as hadron physics or neutrino experiment.
*This experiment was done in MLF.

## Slide 14: Facility ~MLF~
Entrance
Transmission experiment
BL04 ANNRI
Scattering C.S. experiment
BL14 AMATERAS
In the MLF, there are 23
neutron beam ports, and
21 beam lines are working.
Inelastic scattering 6 beam lines (BL14)
Diffraction 8 beam lines
Small angle scattering and reflection 3 beam lines
Capture gamma-ray 1 beam line (BL04)
Imaging and the other 3 beam lines
Pulsed neutron source
Muon beam lines
J-PARC MLF,
Taken from HP of J-PARC
Notes: This figure shows floor map of the MLF.
In the MLF, there 23 beam ports and 21 beam lines are working.
The transmission experiment were performed in BL04 ANNRI.
And the elastic C.S. measurements were performed in BL14 named AMATERAS.

## Slide 15: ANNRI (For transmission experiment)
NaI(Tl) Spectrometer
BL04: ANNRI (Accurate Neutron Nucleus Measurement Instrument)
Ge Spectrometer
6 and 7Li Glass detectors
A 6Li-glass scintillation detector for neutron
a 7Li-glass scintillation detector for γ-ray B.G
were installed at the flight length of 28.7m
Notes: First, I’ll show you the outline of ANNRI for transmission experiment
ANNRI is located on Beam Line NO.4 of MLF.
This figure shows a schematic view of ANNRI.
In ANNRI, we have two gamma-ray spectrometers for capture cross section measurements.
One is Ge detector array and the other one is NaI detectors.
Also, Li-Glass detectors for total cross section measurements are also equipped.

## Slide 16: AMATERAS (For scattering C.S. measurement)
BL14: AMATERAS, Cold-Neutron Disk-Chopper Spectrometer
Sample position
Disk choppers
Array of 3He tube detectors (Position sensitive)
AMATERAS is a disk-chopper type spectrometer.
The spectrometer is designed for inelastic neutron scattering experiments in the range from cold to sub-thermal neutron energy.
neutrons
Neutrons were monochromatized with disk choppers.
The neutrons are scattered by the sample.
The scattered neutrons were detected with arrays of He-3 tubes.
Derive the position and energy of the scattered neutrons.
Incident neutron energy 1 < Ei < 80 meV
Detection angle Horizontal: 3.4 deg. ~ 116 deg. Vertical: -16 deg. ~ 23 deg.
Resolution (ΔE/Ei) ~2% at Ei < 3 meV ~3-4% at Ei < 20 meV ~4-10% at Ei < 80 meV
Neutron intensity (@sample position) 6 ×104 n/s/cm2 (@ Ei = 20 meV)
Notes: For the elastic C.S. measurement, we used Cold-Neutron Disk-Chopper Spectrometer named AMATERAS.
AMATERAS is a disk-chopper type spectrometer.
Neutrons were monochromatized with disk choppers.
The neutrons are scattered by the sample
The scattered neutrons were detected with arrays of He-3 tubes.
Calculate the neutron energy of the scattered neutrons.
Using this spectrometer, we can obtain the scattered angle and energy of scattered neutrons.
Characteristics of the spectrometer are shown here.
Incident neutron energy 1 < Ei < 80 meV
Detection angle Horizontal: 3.4 deg. ~ 116 deg. Vertical: -16 deg. ~ 23 deg.

## Slide 17: DDSCS measurement

## Slide 18: Scattering C.S. measurements ~Experimental set-up~
Top of the refrigerator
Sample Holder cell
The graphite samples are placed in an aluminum cell and placed in a refrigerator. The refrigerator was installed at the sample position. The temperature was controlled at 300 K. (100 K and 485 K are measured for ET-34 only).
A blank cell was measured for B.G.
A Vanadium sample was measured for normalization. An incoherent cross section of 5.08b (NIST) was used.
Incident neutron energy: Filter ① :5.93，10.53，23.65，93.95 meV Filter ② :3.14，7.74，15.15，41.98 meV Filter ③ :1.17，1.48，1.94，2.64 meV
Measurement time: 2~3 hours for each sample and condition.
J-PARC MLF BL14: AMATERAS
Notes: For DDSCS experiments, the graphite samples are placed in an aluminum cell and placed in a refrigerator. Temperature was controlled at 300 K, 100K, and 485K.

## Slide 19: Scattering C.S. measurements ~Result1 (Ein =41.98meV)~
3°
116°
Vertical Angle
Height
-16°
23°
ET-34 (Ein =42meV)
Distribution of detected neutron Position. (Integral of all scattered neutron energies)
An array of 3He tube detectors
B.G. due to the Al cell
3°
116°
Vertical Angle
Height
-16°
23°
Vanadium (Ein =42meV)
3°
116°
Vertical Angle
Height
-16°
23°
Blank (Ein =42meV)
Vanadium has large incoherent C.S.
Neutrons are scattered isotropically.
->Relative efficiency was deduced.
Notes: These pictures show the Distribution of detected neutron Position.
That means Sum of all scattered neutron energies.
This ax shows the vertical angle from 3 to 116 degree.
This ax shows the horizontal angle from -16 to 23 degree.
This block shows an array of He-3 tubes.
Due to the support of the detector array, sum vertical angle is missing.
This is a result of graphite sample and this is a result of blank.
As you can see, these are paterns due to Bragg edge and these are B.G. due to the Al cell.
This is a result of vanadium sample.
Vanadium has large incoherent C.S. comparison to the coherent C.S.
Neutrons are scattered isotropically.
Detector efficiency was corrected using the result of the Vanadium measurements.

## Slide 20: Scattering C.S. measurements ~ Result1 (Ein =41.98meV)~
With considering dead time, neutron detection efficiency of each detector and solid angle, ΔE-Q distribution of each sample was obtained.
Blank
ET-34
|Q| (1/Å)
1.5
3
4.5
7.5
6
9
Ein-Eout（meV）
30
20
10
0
-10
-20
-30
|Q| (1/Å)
1.5
3
4.5
7.5
6
9
Ein-Eout（meV）
30
20
10
0
-10
-20
-30
Bragg Edges of graphite and Al are clearly observed.
Ein (wave number)
Q
2Θ
Eout
No detectors
Elastic Scattering
Notes: With considering dead time, neutron detection efficiency of each detector and solid angle, ΔE-Q distribution of each sample was obtained.
These graph shows the ΔE-Q distribution of ET-34 and Blank.
X ax shows Q value in other word difference between the wavenumber vector of incident neutrons and the wavenumber vector of scattered neutrons.
Y ax shows E-in minus E-out.
That means if Y ax is positive, neutron loss the energy and if Y ax is negative, neutrons gain energy.
As you can see, Bragg Edges of graphite and Al are clearly observed.

## Slide 21: Scattering C.S. measurements ~ Result1 DDSCS of E-34 (Ein =41.98meV)~
|Q| (1/Å)
1.5
3
4.5
7.5
6
9
Ein-Eout（meV）
30
20
10
0
-10
-20
-30
0.005
0.004
0.003
0.002
0.001
0.0
Cross Section (b/Sr/meV)
Subtract Blank from each sample,
Normalized by the vanadium result
-> DDSCS is derived.
ET-34
Preliminary
Notes: Subtract Blank from each sample,
Normalized by the vanadium result,
DDSCS of each sample was derived.
Elastic and inelastic cross section was obtained.

## Slide 22: Elastic C.S. measurements ~ Result1: DDSCS of E-34 (Ein =41.98meV)~
Chart: Energy Transfer (Ein-Eout:meV)
Preliminary
Detailed Analysis for multiple scattering correction and systematic uncertainties is ongoing.
Notes: To discuss easily, the DDSCS was re-bundled into 6 parts.
From 5 to 20 degree to 100 to 115 degree.
X-ax shows the scattered angle.
Y-ax shows the DDSCS.
The results is shown here.

## Slide 23
Elastic C.S. measurements ~ Result1: Temperature dependence (Ein =41.98meV)~
The inelastic scattering cross section decreases with decreasing temperature.
Energy increasing side > Energy loss side.
Chart: 
Chart: 
Cross Section (b/Sr/meV)
Energy Transfer (Ein-Eout:meV)
60°~80°
20°~40°
Notes: Temperature dependence was shown in these graph.
This side is form 20 to 40degree and this side shows from 60 to 80 degree.
With degreasing the temperature, the inelastic scattering cross section decreases.
Up scattering side is much degreasing comparison to the slowing down side.
This is a reasonable result.

## Slide 24: Elastic C.S. measurements ~ Result1: Sample dependence(Ein =41.98meV)~
60°~80°
20°~40°
Cross Section (b/Sr/meV)
There’s no clear differences (less than 10%) in inelastic C.S.
Energy Transfer (Ein-Eout:meV)
Sample dependence of the Inelastic C.S.
Chart: 
Chart: 
Preliminary
Notes: Sample dependence is shown in these graphs.
This side is form 20 to 40degree and this side shows from 60 to 80 degree.
As you can see, the result of each sample agrees very well.
There’s no clear difference between the samples.
The difference is less than 10 %.

## Slide 25: Elastic C.S. measurements ~ Result1: Elastic Cross Section (Ein =41.98meV)~
Chart: Scattering Angle 2Θ(degree)
002
004
112
110
103
101
006
100
114
002
101
In some Bragg edges, cross sections are different between the samples.
-> Discuss later
Preliminary
Notes: This graph shows the elastic scattering C.S.
This Ax shows scattered angle and this ax shows C.S.
As you can see, many Bragg edges are clearly observed and shape of the Bragg edges are different between the samples.

## Slide 26: Scattering C.S. measurements ~ Result2 (Ein =7.74meV)~
Ein-Eout（meV）
6
4
2
0
-2
-4
-6
Blank
Ein-Eout（meV）
6
4
2
0
-2
-4
-6
|Q| (1/Å)
0.5
1
1.5
2.5
3.5
2
3
|Q| (1/ Å)
0.5
1
1.5
2.5
3.5
2
3
Ein
Q
2Θ
Eout
Bragg Edge(0,0,2)
ET-34
Bragg Edges due to the Al cell
Dead time, neutron detection efficiency of each detector and solid angle are corrected
Notes: For neutron incident energy of 7.74 meV, we have done same steps.
These graph shows the ΔE-Q distribution of ET-34 and Blank.

## Slide 27
0.5
1.0
1.5
2.0
2.5
3.0
3.5
-6
-4
-2
0
2
4
6
2
0
1
0.5
1.5
Cross Section (mb/Sr/meV)
Ein-Eout（meV）
|Q| (1/Å)
Scattering C.S. measurements ~ Result2 DDSCS of ET-34 (Ein =7.74meV)~
(0,0,2) Brag edge is clearly observed.
Preliminary
Notes: This graph shows DDSCS of ET-34.
Strong (0,0,2) Bragg edge is clearly observed.

## Slide 28: Elastic C.S. measurements ~ Result2: Sample dependence(Ein =7.74meV)~
Chart: 
| -5.8000000000000007 | -5.6000000000000005 | -5.4 | -5.2 | -5 | -4.8 | -4.5999999999999996 | -4.3999999999999995 | -4.1999999999999993 | -3.9999999999999991 | -3.7999999999999989 | -3.5999999999999988 | -3.3999999999999986 | -3.1999999999999984 | -2.9999999999999982 | -2.799999999999998 | -2.5999999999999979 | -2.3999999999999977 | -2.1999999999999975 | -1.9999999999999976 | -1.7999999999999976 | -1.5999999999999976 | -1.3999999999999977 | -1.1999999999999977 | -0.99999999999999778 | -0.79999999999999782 | -0.59999999999999787 | -0.39999999999999786 | -0.19999999999999785 | 2.1649348980190553E-15 | 0.20000000000000218 | 0.40000000000000219 | 0.6000000000000022 | 0.80000000000000226 | 1.0000000000000022 | 1.2000000000000022 | 1.4000000000000021 | 1.6000000000000021 | 1.800000000000002 | 2.0000000000000022 | 2.2000000000000024 | 2.4000000000000026 | 2.6000000000000028 | 2.8000000000000029 | 3.0000000000000031 | 3.2000000000000033 | 3.4000000000000035 | 3.6000000000000036 | 3.8000000000000038 | 4.0000000000000036 | 4.2000000000000037 | 4.4000000000000039 | 4.6000000000000041 | 4.8000000000000043 | 5.0000000000000044 | 5.2000000000000046 | 5.4000000000000048 | 5.600000000000005 | 5.8000000000000052 | 6.0000000000000053
ET-10 | 0.00084909 | 0.00093023 | 0.00094831 | 0.001015 | 0.0010442 | 0.0011096 | 0.00114 | 0.0012007 | 0.0012288 | 0.0012934 | 0.0013644 | 0.001472 | 0.0015182 | 0.0015958 | 0.0016779 | 0.0017924 | 0.0018983 | 0.0020147 | 0.0022278 | 0.00234 | 0.002608 | 0.0027852 | 0.0030566 | 0.0034279 | 0.0039587 | 0.0047848 | 0.0060412 | 0.0098508 | 0.95999 | 2.4813 | 0.1556 | 0.017992 | 0.0068606 | 0.0037871 | 0.0025682 | 0.002098 | 0.0015063 | 0.001207 | 0.00099716 | 0.00081524 | 0.00075445 | 0.0006032 | 0.00059351 | 0.00046016 | 0.00046205 | 0.00041072 | 0.00034615 | 0.00037995 | 0.00031884 | 0.00031411 | 0.0003411 | 0.00034636 | 0.00029873 | 0.00033076 | 0.00034872 | 0.00038965 | 0.00037103 | 0.00030106 | 0.00046275 | 0.00030176
ET-11 | 0.00081943 | 0.00090351 | 0.00091929 | 0.00099172 | 0.0010166 | 0.0010776 | 0.0010983 | 0.0011969 | 0.0012354 | 0.0013257 | 0.0013376 | 0.0014231 | 0.0014783 | 0.0015801 | 0.00171 | 0.0017991 | 0.0019152 | 0.0020357 | 0.0022208 | 0.0023773 | 0.0026416 | 0.0028127 | 0.0031387 | 0.0035171 | 0.0040952 | 0.0049467 | 0.0062752 | 0.0099168 | 1.0066 | 2.5376 | 0.14765 | 0.016716 | 0.0068332 | 0.0040636 | 0.0027986 | 0.0022632 | 0.0016571 | 0.0013361 | 0.0011018 | 0.00090921 | 0.00083643 | 0.00064 | 0.00066014 | 0.00050499 | 0.00050466 | 0.00047168 | 0.000402 | 0.00041467 | 0.00037255 | 0.00036168 | 0.00037571 | 0.00037974 | 0.00034867 | 0.0003584 | 0.00040222 | 0.00042915 | 0.00046115 | 0.00037363 | 0.00051462 | 0.00039893
ET-34 | 0.00080079 | 0.00084808 | 0.00087673 | 0.00094771 | 0.00095311 | 0.0010409 | 0.0010382 | 0.0011233 | 0.001162 | 0.0012087 | 0.001265 | 0.0013159 | 0.0013887 | 0.0014817 | 0.0015164 | 0.0016246 | 0.00175 | 0.0018564 | 0.0020184 | 0.0021329 | 0.0023181 | 0.0024898 | 0.0027173 | 0.0030149 | 0.0034607 | 0.0041632 | 0.0052211 | 0.0087939 | 0.91752 | 2.2256 | 0.13211 | 0.016759 | 0.0059899 | 0.0031172 | 0.0020463 | 0.0016465 | 0.0012434 | 0.0010066 | 0.00081141 | 0.00068859 | 0.00063561 | 0.00047571 | 0.00050861 | 0.00037737 | 0.00038375 | 0.00034874 | 0.00030296 | 0.00032065 | 0.0002874 | 0.00025902 | 0.00029822 | 0.00028623 | 0.00025004 | 0.00028576 | 0.00031161 | 0.00034673 | 0.00035683 | 0.00029285 | 0.00042134 | 0.00028103
ED-4 | 0.00082326 | 0.00087878 | 0.00091275 | 0.0009853 | 0.0010004 | 0.0010721 | 0.0011094 | 0.0011892 | 0.0012228 | 0.0013133 | 0.0013597 | 0.001424 | 0.0014986 | 0.0016237 | 0.0016941 | 0.0017989 | 0.0019304 | 0.002064 | 0.0022647 | 0.0024134 | 0.0026677 | 0.0029203 | 0.0032282 | 0.0036628 | 0.004291 | 0.0051737 | 0.006553 | 0.010301 | 0.97808 | 2.4288 | 0.14185 | 0.017446 | 0.0072662 | 0.0043535 | 0.003003 | 0.0024681 | 0.0017498 | 0.001448 | 0.0011969 | 0.00097501 | 0.00087384 | 0.00067727 | 0.00067813 | 0.00054179 | 0.00053488 | 0.00049078 | 0.00043152 | 0.00045816 | 0.00038544 | 0.00039379 | 0.00041685 | 0.00039763 | 0.00035577 | 0.0003827 | 0.00040296 | 0.00042353 | 0.0004498 | 0.00036245 | 0.00048793 | 0.00034318
T-8 | 0.00081444 | 0.00085187 | 0.00091604 | 0.00097954 | 0.0009877 | 0.0010638 | 0.0010926 | 0.0011696 | 0.0012169 | 0.0012814 | 0.0013254 | 0.0014022 | 0.0014677 | 0.0015453 | 0.001647 | 0.0017443 | 0.0018966 | 0.0019983 | 0.0021858 | 0.0023082 | 0.0025776 | 0.0028347 | 0.0031329 | 0.0035134 | 0.0041246 | 0.005048 | 0.0062429 | 0.0096775 | 0.92768 | 2.3945 | 0.14728 | 0.017311 | 0.0070354 | 0.0041895 | 0.0029273 | 0.0023602 | 0.0017181 | 0.00138 | 0.001129 | 0.0009417 | 0.00084322 | 0.00066561 | 0.00068868 | 0.00053069 | 0.00053115 | 0.00049171 | 0.00043104 | 0.00042958 | 0.00038161 | 0.00034786 | 0.00039047 | 0.00036071 | 0.00033161 | 0.00036483 | 0.00038667 | 0.00041641 | 0.00040951 | 0.00034981 | 0.00049048 | 0.00031719
Chart: 
| -5.8000000000000007 | -5.6000000000000005 | -5.4 | -5.2 | -5 | -4.8 | -4.5999999999999996 | -4.3999999999999995 | -4.1999999999999993 | -3.9999999999999991 | -3.7999999999999989 | -3.5999999999999988 | -3.3999999999999986 | -3.1999999999999984 | -2.9999999999999982 | -2.799999999999998 | -2.5999999999999979 | -2.3999999999999977 | -2.1999999999999975 | -1.9999999999999976 | -1.7999999999999976 | -1.5999999999999976 | -1.3999999999999977 | -1.1999999999999977 | -0.99999999999999778 | -0.79999999999999782 | -0.59999999999999787 | -0.39999999999999786 | -0.19999999999999785 | 2.1649348980190553E-15 | 0.20000000000000218 | 0.40000000000000219 | 0.6000000000000022 | 0.80000000000000226 | 1.0000000000000022 | 1.2000000000000022 | 1.4000000000000021 | 1.6000000000000021 | 1.800000000000002 | 2.0000000000000022 | 2.2000000000000024 | 2.4000000000000026 | 2.6000000000000028 | 2.8000000000000029 | 3.0000000000000031 | 3.2000000000000033 | 3.4000000000000035 | 3.6000000000000036 | 3.8000000000000038 | 4.0000000000000036 | 4.2000000000000037 | 4.4000000000000039 | 4.6000000000000041 | 4.8000000000000043 | 5.0000000000000044 | 5.2000000000000046 | 5.4000000000000048 | 5.600000000000005 | 5.8000000000000052 | 6.0000000000000053
ET-10 | 0.00019735 | 0.00019722 | 0.00021246 | 0.00020938 | 0.00021272 | 0.00023045 | 0.00022306 | 0.0002392 | 0.00023881 | 0.00026195 | 0.00026265 | 0.0002826 | 0.00028828 | 0.0003087 | 0.00034001 | 0.00035351 | 0.00036746 | 0.00039987 | 0.0004373 | 0.00045336 | 0.00047419 | 0.0005344 | 0.00058944 | 0.00062688 | 0.00075763 | 0.00078612 | 0.00092013 | 0.00113 | 0.067958 | 0.23998 | 0.020734 | 0.001831 | 0.0015259 | 0.0015396 | 0.0022636 | 0.0021692 | 0.0023512 | 0.0022289 | 0.0022235 | 0.0022404 | 0.0021135 | 0.0020854 | 0.0020774 | 0.0020231 | 0.0020046 | 0.0019175 | 0.0019464 | 0.0018641 | 0.0018199 | 0.0017397 | 0.0017324 | 0.0017003 | 0.0016093 | 0.0015971 | 0.0014937 | 0.0013712 | 0.0011986 | 0.0010981 | 0.00097424 | -0.0023229
ET-11 | 0.00019535 | 0.00020633 | 0.00019856 | 0.00022166 | 0.00022236 | 0.00024279 | 0.00022449 | 0.00023637 | 0.00024956 | 0.00025823 | 0.00028403 | 0.0002833 | 0.00029163 | 0.00031858 | 0.00033197 | 0.00036726 | 0.00037328 | 0.0003964 | 0.0004399 | 0.00046581 | 0.00049818 | 0.00057117 | 0.00062381 | 0.00067242 | 0.0007984 | 0.00085895 | 0.0010238 | 0.0013139 | 0.076414 | 0.25424 | 0.020526 | 0.0019501 | 0.0016852 | 0.0016289 | 0.0022733 | 0.0021931 | 0.0023821 | 0.0023239 | 0.0023156 | 0.0022621 | 0.0021906 | 0.0022368 | 0.0021245 | 0.0021311 | 0.0020696 | 0.0020296 | 0.0020294 | 0.0019308 | 0.0019019 | 0.0018548 | 0.0018378 | 0.0017791 | 0.0017282 | 0.0017119 | 0.0016032 | 0.001504 | 0.0012893 | 0.0011673 | 0.0011226 | -0.0023291
ET-34 | 0.00021117 | 0.00021482 | 0.00021552 | 0.00021623 | 0.00022564 | 0.00022132 | 0.00023069 | 0.00024712 | 0.0002508 | 0.00025934 | 0.00026866 | 0.00027498 | 0.00029218 | 0.00030803 | 0.00032206 | 0.00033026 | 0.00034783 | 0.00037727 | 0.00040814 | 0.00043863 | 0.00045967 | 0.00049506 | 0.00053471 | 0.00058894 | 0.00069394 | 0.00065359 | 0.00075752 | 0.00092138 | 0.064913 | 0.22456 | 0.018242 | 0.0015617 | 0.0014001 | 0.0014459 | 0.0020812 | 0.0020167 | 0.0021444 | 0.0021109 | 0.0021005 | 0.002102 | 0.0019966 | 0.0020075 | 0.0019476 | 0.0019304 | 0.0018985 | 0.0018678 | 0.0018692 | 0.0017975 | 0.0017571 | 0.0016986 | 0.0016519 | 0.001617 | 0.0016001 | 0.0015531 | 0.0014719 | 0.0013109 | 0.0011442 | 0.0010606 | 0.001024 | -0.0021459
ED-4 | 0.00021417 | 0.00022754 | 0.00022654 | 0.00022666 | 0.00022435 | 0.00024217 | 0.00024617 | 0.00026034 | 0.00026816 | 0.00027695 | 0.00028157 | 0.00030346 | 0.00031458 | 0.00034762 | 0.00035495 | 0.00038742 | 0.00040207 | 0.00044304 | 0.0004801 | 0.00051831 | 0.00054036 | 0.00059987 | 0.00065896 | 0.00070481 | 0.00081893 | 0.00092318 | 0.0011137 | 0.0014049 | 0.077134 | 0.25786 | 0.020634 | 0.0020374 | 0.0016256 | 0.0015895 | 0.0022658 | 0.0022172 | 0.0023435 | 0.0022859 | 0.0022828 | 0.0022386 | 0.0021657 | 0.0021735 | 0.0020529 | 0.0020622 | 0.0020189 | 0.0019803 | 0.0019503 | 0.0018903 | 0.001886 | 0.0017586 | 0.001799 | 0.0017208 | 0.0017021 | 0.0016127 | 0.0015602 | 0.0014372 | 0.001228 | 0.0011264 | 0.0010468 | -0.002101
T-8 | 0.00022189 | 0.00020532 | 0.00022188 | 0.00022156 | 0.00022296 | 0.00023526 | 0.00024399 | 0.00024357 | 0.00025258 | 0.00027271 | 0.00028035 | 0.00028215 | 0.00029303 | 0.00033045 | 0.00034281 | 0.00036427 | 0.00039898 | 0.00041285 | 0.00043763 | 0.00049046 | 0.00052128 | 0.00057192 | 0.00061305 | 0.00068779 | 0.00081943 | 0.00086955 | 0.0010312 | 0.0012885 | 0.069671 | 0.25054 | 0.021985 | 0.0020312 | 0.0015841 | 0.0015123 | 0.0021831 | 0.0020876 | 0.0022501 | 0.0022378 | 0.0022 | 0.0021794 | 0.0020972 | 0.0020465 | 0.0019798 | 0.0019288 | 0.0019025 | 0.0019198 | 0.001879 | 0.001794 | 0.0017891 | 0.0017236 | 0.0016955 | 0.0016378 | 0.0016451 | 0.0015408 | 0.0014822 | 0.0013795 | 0.0011517 | 0.0010656 | 0.0010123 | -0.0020734
60°~80°
40°~60°
There’s no clear differences (less than 15%) in inelastic C.S.
Preliminary
Energy Transfer (Ein-Eout:meV)
Cross Section (b/Sr/meV)
Notes: Sample dependence is shown in these graphs.
This side is form 20 to 40degree and this side shows from 60 to 80 degree.
As same as the results of 41.98meV, the result of each sample agrees very well.
There’s no clear difference between the samples.
The difference is less than 10 %.

## Slide 29: Elastic C.S. measurements ~ Result2: Elastic Cross Section (Ein =7.74meV)~
Chart: Scattering Angle 2Θ(degree)
002
Preliminary
At some Bragg edges, cross sections are different between the samples.
002
101
101
Large small angle neutron scattering (SANS) is clearly
observed.
Notes: This graph shows the elastic scattering C.S.
This Ax shows scattered angle and this ax shows C.S.
As you can see, large small angle neutron scattering (SANS) is clearly observed.
At some Bragg edges, cross sections are different between the samples.

## Slide 30: Elastic C.S. measurements ~ Result: Bragg Edge~
Chart: 
Chart: 
(0,0,2)
Ein=7.74meV
Chart: 
(1,0,1)
Ein=7.74meV
(1,1,2)Ein=41.98meV
Chart: 
Scattering Angle 2Θ(degree)
Cross Section(b/Sr)
(1,1,4)Ein=41.98meV
 | Grain Size(μm) | Porosity (%)
ET-34 | 15 | 11
ET-10 | 15 | 14
ET-11 | 13 | 15
T-8 | 5 | 9
ED-4 | 1 | 9
Sharp(High)<------>(Low)Broad
ET-34<ET-10<ET11<T-8<ED-4
This trend seems to depend on the grain size.
Notes: These graphs show the sample dependence of the elastic C.S. at some Bragg Edges.
Bragg Edge is broadened from ET-34, ET-10<ET11<t-8<ED-4 become broader and broader in that order.
This trend seems to depend on the size of the grain size, but additional experiments and studies are required.

## Slide 31: Total C.S. measurement

## Slide 32: Total C.S. measurements ~Experimental set-up~
6Li glass detector
Sample position
Detector: 6Li and 7Li glass detectors
Sample thickness: 10mm
Measurement time: 12~16hours
Scattered neutrons with scattering angles of less than 0.25°are transmitted.
*
J-PARC MLF BL04 ANNRI
Delivered to MLF (126shot)
To Hadron Facility (4shot)
To MLF (126shot)
・・・・
・・・・
To Hadron (4shot)
Wide range TOF
Wide range TOF
In every 5.2 seconds (130 shot), the first 126 shots were delivered to the MLF, and the other 4 shots were supplied to the hadron facility.
This means that a wide range TOF experiment (200 ms) is possible in every 5.2 seconds.
Notes: Total cross section measurement was performed in ANNRI with Li-6 and Li-7 detectors.
Measurement time: 12~16hours.
In-J-PARC, In every 5.2 seconds (130 shot), the first 126 shots were delivered to the MLF, and the other 4 shots were supplied to the hadron facility.
This means that a wide range TOF experiment (200 ms) is possible in every 5.2 seconds.
We used this wide range TOF is used for C.S. measurement.

## Slide 33: Total C.S. measurements ~Raw TOF spectrum (dead time corrected)~
Chart: Time of Flight (ms)
0
40
80
120
160
200
10-5
10-6
10-7
10-8
10-9
10-10
Triger is created by delaying the previous pulse by 40 ms.
The first shot to MLF is observed here because there is no previous
~120 ms : Data after 40 ms is used as B.G.
160 ms~: Exp + Constant is used as B.G.
γ-ray B.G. was derived from the 7Li-glass spectrum.
Notes: This graph shows TOF spectra with dead time correction.
In ANNRI, Triger is produced from the previous neutron pulse with delaying 40 ms.
Therefore, The first shot to MLF is observed here because there is no previous
In the analysis,
In the TOF range before 120 ms, Data after 40 ms is used as B.G.
After 160 ms, Exp + Constant function is used as B.G.
The parameters were obtained by fitting the spectra from 120 ms to 160 ms.
γ-ray B.G. was derived from the 7Li-glass spectrum.

## Slide 34: Total C.S. measurements ~Transmission Ratio~
Chart: Neutron Energy (meV)
Notes: After subtracting B.G., Transmission ratio was calculated.
Black line shows the transmission ratio of ET-34 sample and red line shows its uncertainty.
From this ratio, C.S. is calculated.

## Slide 35: Total C.S. measurements ~Total C.S.~
Chart: Neutron Energy (meV)
Preliminary
Notes: This graph shows prerliminary C.S. of ET-34 sample with comparison to the deduced uncertainty.
As you can see some Bragg Edge is clearly observed.
However, in the energy range below 10 meV, deduced total C.S. is much higher than the previous measurement by Petriw.

## Slide 36: Total C.S. measurements ~Sample dependence~
In the epithermal range (over 40 meV), all samples tended to have same values. Close to the free atom cross-section of graphite.
Under 10 meV, the total cross sections of the samples separate from each other. ⇒Influence of SANS
* * *
Chart: Neutron Energy (meV)
Preliminary
Notes: This graph shows the difference of deduced total C.S.
In the epithermal range (over 40 meV), all samples tended to have values. Close to the free atom cross-section of graphite.
Under 10 meV, the total cross sections of the samples separate from each other.
It’s influence of small angle neutron scattering.

## Slide 37: Influence of SANS
Chart: Q (1/Å)
Q^-3.4
83°
7.6°
0.7°
Q^-3.6
Cross-section and Q have a linear relationship in Log-Log scale ⇒ Characteristics of SANS
Ein＝1.17meV
SANS of the samples are very large comparison to the reported experiments [1].
⇒ Caused by the uniformity of the grain size of the isotropic graphite.
[1] S. Petriw et al., Journal of Nuclear Materials 2010; 396: 181–188.
SANS has very little impact on criticality calculations!!
Scattered neutrons with angles of less than 0.25°are transmitted.
Additional correction is required.
Notes: This graph shows elastic C.S. with incident energy of 1.17meV.
As you can see, in Log-Log graph, elastic C.S. has a linear relation ship.
It is a characteristics of SANS.
The difference below 10 meV is considered to be the influence of SANS.
In this setting, Scattered neutrons with angles of less than 0.25°are transmitted.
Additional correction is required.
SANS of isoprtopic graphite samples are very large comparison to the traditional nuclear grade graphite reported by Petriw.
This is due to uniformity of the grain size in the isotropic graphite.
However, fortunately, SANS has very little impact on criticality calculations!!
This is because, neutron energy is not changed (SANS is elastic scattering) and only angle is slightly changed.

## Slide 38: Total C.S. measurements ~Around (0,0,2) edge~
Chart: Neutron Energy(meV)
Chart: 
(0,0,2)
Ein=7.74meV
Scattering Angle 2Θ(degree)
Shape of the (0,0,2) Bragg Edge varies with the samples.
The ET-34 sample has the sharpest slope, which is consistent with the smallest width in the elastic scattering.
Notes: This graph shows the total C.S. around (0,0,2) Bragg edge.
Shape of the (0,0,2) Bragg Edge varies with the samples.
As you can see, The ET-34 sample has the sharpest slope.
This graph shows the elastic C.S. around this Bragg Edge.
ET-34 is the smallest width.
These are consistent.

## Slide 39: Summary and Future Plans
Comparisons of our results to calculations will be presented by Dr. Nakayama on Friday.
The total C.S. and DDSCS of isotropic graphite have been performed in the MLF in the J-PARC.
The preliminary DDSCS were derived with nine incident neutron energies ranging from 1.2 to 94 meV.
Large small angle scattering and Bragg edges were observed.
The preliminary total C.S. was derived in the energy region from 1 to 1000 meV.
In the epithermal range, all samples agreed with the free atom cross-section of graphite. In the low-energy region, large SANS were observed.
Detailed analysis for uncertainties and some corrections are ongoing.

## Slide 40
The present study includes the result of ‘Development of Nuclear Data Evaluation Framework for Innovative Reactor’ founded by the Ministry of Education, Culture, Sports, Science and Technology of Japan.
The neutron experiments at the MLF of the J-PARC were performed under the user programs (Proposal No. 2022B0109, 2022P0301).
Thank you for your kind attention.

## Slide 42: Ge Spectrometer (FYI)
2 cluster-Ge detectors (7 Ge crystals are installed in the detector)
8 coaxial-Ge detectors
->Peak efficiency for 1.33MeV γ-rays: 3.64 ± 0.11 %
New DAQ System (CAEN 1724,1720) is installed in 2017.
Measurements of neutron capture cross sections of 241,243Am, 137,135Cs, 244,246Cm and stable isotopes have performed.
TOF spectra for 243Am Samples

## Slide 43: NaI detectors (FYI)
The NaI spectrometer consists of two NaI detectors.
Size: 330 mmϕ 203 mmL 90◦
203 mmϕ 203 mmL 125◦
Surrounded by plastic scintillator.
(The plastic scintillators were used to eliminate events triggered by cosmic rays. )
These scintillators were shielded from background rays and neutrons using the layers of lead, cadmium and borated polyethylene.

## Slide 44: Elastic C.S. measurements ~ Result1: Inelastic Cross Section (Ein =41.98meV)~
Chart: Energy Transfer (Ein-Eout:meV)
Ein=41.98 meV
60~80 degree

## Slide 45: Elastic C.S. measurements ~ Result1: Inelastic Cross Section (Ein =41.98meV)~
Chart: Energy Transfer (Ein-Eout:meV)
Ein=41.98 meV
60~80 degree

## Slide 46: Elastic C.S. measurements ~ Result2: DDSCS of ET-34 (Ein =7.74meV)~
Chart: Energy Transfer (Ein-Eout:meV)
| -5.8000000000000007 | -5.6000000000000005 | -5.4 | -5.2 | -5 | -4.8 | -4.5999999999999996 | -4.3999999999999995 | -4.1999999999999993 | -3.9999999999999991 | -3.7999999999999989 | -3.5999999999999988 | -3.3999999999999986 | -3.1999999999999984 | -2.9999999999999982 | -2.799999999999998 | -2.5999999999999979 | -2.3999999999999977 | -2.1999999999999975 | -1.9999999999999976 | -1.7999999999999976 | -1.5999999999999976 | -1.3999999999999977 | -1.1999999999999977 | -0.99999999999999778 | -0.79999999999999782 | -0.59999999999999787 | -0.39999999999999786 | -0.19999999999999785 | 2.1649348980190553E-15 | 0.20000000000000218 | 0.40000000000000219 | 0.6000000000000022 | 0.80000000000000226 | 1.0000000000000022 | 1.2000000000000022 | 1.4000000000000021 | 1.6000000000000021 | 1.800000000000002 | 2.0000000000000022 | 2.2000000000000024 | 2.4000000000000026 | 2.6000000000000028 | 2.8000000000000029 | 3.0000000000000031 | 3.2000000000000033 | 3.4000000000000035 | 3.6000000000000036 | 3.8000000000000038 | 4.0000000000000036 | 4.2000000000000037 | 4.4000000000000039 | 4.6000000000000041 | 4.8000000000000043 | 5.0000000000000044 | 5.2000000000000046 | 5.4000000000000048 | 5.600000000000005 | 5.8000000000000052 | 6.0000000000000053
5-20 | 0.00018055 | 0.00018703 | 0.00020305 | 0.00019249 | 0.00021246 | 0.00020827 | 0.0002223 | 0.00023617 | 0.00024388 | 0.00027443 | 0.00027803 | 0.00029887 | 0.00030535 | 0.00032218 | 0.00034497 | 0.00037747 | 0.00037779 | 0.00039737 | 0.00045784 | 0.00047895 | 0.00053156 | 0.00057676 | 0.00062973 | 0.00067545 | 0.00077327 | 0.00090137 | 0.00099056 | 0.0012092 | 0.20522 | 0.77039 | 0.058317 | 0.0023797 | 0.0010533 | 0.00086179 | 0.00067931 | 0.00058137 | 0.00053549 | 0.00047677 | 0.00042736 | 0.00041443 | 0.00039037 | 0.0003494 | 0.00033378 | 0.00032827 | 0.00029622 | 0.00028946 | 0.0002545 | 0.00021463 | 0.0001969 | 0.00017264 | 0.00015493 | 0.0001498 | 0.00012859 | 0.00012252 | 0.00012787 | 0.00011762 | 0.0001 | 0.00010992 | 0.00015357 | 0.00010562
20-40 | 0.00020363 | 0.00021351 | 0.00019519 | 0.0001924 | 0.00018668 | 0.00019472 | 0.00020671 | 0.00021246 | 0.00022265 | 0.00023372 | 0.00024744 | 0.00026155 | 0.00027423 | 0.00028091 | 0.00030972 | 0.00033138 | 0.00034168 | 0.00035647 | 0.00038866 | 0.0004182 | 0.00043905 | 0.00046942 | 0.00049934 | 0.00052906 | 0.00057737 | 0.00063861 | 0.00069427 | 0.00085014 | 0.056027 | 0.19471 | 0.016599 | 0.0013924 | 0.0007245 | 0.00060163 | 0.00049577 | 0.00039508 | 0.00034643 | 0.00029403 | 0.00027506 | 0.00024966 | 0.00022871 | 0.00022851 | 0.00021713 | 0.00021365 | 0.0002027 | 0.00020153 | 0.00018582 | 0.00019019 | 0.0002 | 0.00019238 | 0.00020119 | 0.00019846 | 0.00018385 | 0.0001729 | 0.00015873 | 0.00015491 | 0.00014184 | 0.00014114 | 0.0001442 | 8.3445e-05
40-60 | 0.00080079 | 0.00084808 | 0.00087673 | 0.00094771 | 0.00095311 | 0.0010409 | 0.0010382 | 0.0011233 | 0.001162 | 0.0012087 | 0.001265 | 0.0013159 | 0.0013887 | 0.0014817 | 0.0015164 | 0.0016246 | 0.00175 | 0.0018564 | 0.0020184 | 0.0021329 | 0.0023181 | 0.0024898 | 0.0027173 | 0.0030149 | 0.0034607 | 0.0041632 | 0.0052211 | 0.0087939 | 0.91752 | 2.2256 | 0.13211 | 0.016759 | 0.0059899 | 0.0031172 | 0.0020463 | 0.0016465 | 0.0012434 | 0.0010066 | 0.00081141 | 0.00068859 | 0.00063561 | 0.00047571 | 0.00050861 | 0.00037737 | 0.00038375 | 0.00034874 | 0.00030296 | 0.00032065 | 0.0002874 | 0.00025902 | 0.00029822 | 0.00028623 | 0.00025004 | 0.00028576 | 0.00031161 | 0.00034673 | 0.00035683 | 0.00029285 | 0.00042134 | 0.00028103
60-80 | 0.00021117 | 0.00021482 | 0.00021552 | 0.00021623 | 0.00022564 | 0.00022132 | 0.00023069 | 0.00024712 | 0.0002508 | 0.00025934 | 0.00026866 | 0.00027498 | 0.00029218 | 0.00030803 | 0.00032206 | 0.00033026 | 0.00034783 | 0.00037727 | 0.00040814 | 0.00043863 | 0.00045967 | 0.00049506 | 0.00053471 | 0.00058894 | 0.00069394 | 0.00065359 | 0.00075752 | 0.00092138 | 0.064913 | 0.22456 | 0.018242 | 0.0015617 | 0.0014001 | 0.0014459 | 0.0020812 | 0.0020167 | 0.0021444 | 0.0021109 | 0.0021005 | 0.002102 | 0.0019966 | 0.0020075 | 0.0019476 | 0.0019304 | 0.0018985 | 0.0018678 | 0.0018692 | 0.0017975 | 0.0017571 | 0.0016986 | 0.0016519 | 0.001617 | 0.0016001 | 0.0015531 | 0.0014719 | 0.0013109 | 0.0011442 | 0.0010606 | 0.001024 | -0.0021459
80-100 | 0.00044408 | 0.0004422 | 0.00046103 | 0.00044855 | 0.00045382 | 0.00047304 | 0.00049087 | 0.00050437 | 0.00050319 | 0.00051116 | 0.00052694 | 0.00052884 | 0.00056013 | 0.00059569 | 0.00057248 | 0.00060209 | 0.00064594 | 0.00067841 | 0.00066357 | 0.00068703 | 0.00072396 | 0.00074662 | 0.00077556 | 0.00082616 | 0.00083606 | 0.00089999 | 0.00096639 | 0.0011994 | 0.16697 | 0.48919 | 0.021773 | 0.0015378 | 0.00086163 | 0.00060479 | 0.00046983 | 0.00039576 | 0.00033393 | 0.00031141 | 0.00028035 | 0.0002676 | 0.00023411 | 0.00026422 | 0.00022837 | 0.00018654 | 0.00021125 | 0.00015944 | 0.00017938 | 0.0001806 | 0.00019542 | 0.00018251 | 0.00017204 | 0.00017543 | 0.00018839 | 0.00019296 | 0.00024014 | 0.00032977 | 0.00049806 | 0.00062678 | 0.0007238 | 0.00069597
100-115 | 0.0010366 | 0.0010583 | 0.0010775 | 0.0010609 | 0.0010825 | 0.0010755 | 0.0010399 | 0.0010367 | 0.00099381 | 0.0009562 | 0.00094707 | 0.00085719 | 0.00075368 | 0.00069482 | 0.00067007 | 0.00070496 | 0.00073194 | 0.00076104 | 0.00081217 | 0.00084215 | 0.00093542 | 0.0010106 | 0.001124 | 0.0012443 | 0.0014338 | 0.001746 | 0.0020465 | 0.0031083 | 0.93984 | 2.8217 | 0.18466 | 0.005708 | 0.0025727 | 0.0016221 | 0.0013343 | 0.0010973 | 0.00090568 | 0.000748 | 0.00064286 | 0.00053217 | 0.00046088 | 0.00039427 | 0.00036906 | 0.00029516 | 0.0002529 | 0.00023238 | 0.0002127 | 0.00018527 | 0.00017771 | 0.00017774 | 0.00020697 | 0.00016494 | 0.00017839 | 0.00017652 | 0.00016682 | 0.00016136 | 0.00017247 | 0.000182 | 0.00033926 | 0.0001677
Detailed Analysis for multiple scattering correction and systematic uncertainties was ongoing.
Preliminary

## Slide 47: BL14での測定 （Ein＝ 1.17 meV)
Blank
Ein
Q
Θ
Eout
ET-34
別のフレーム
が見えている

## Slide 48: 各測定におけるBragg Edge の形状
Chart: 散乱角(degree)
Chart: 散乱角(degree)
粒径の小さいED-4（1μm）が最小。
ET10≒ET34（15μm）＞ET11（13μm）
試料依存性
温度依存性（ET-34）
温度上昇とともに幅が太く、
散乱角は小さくなる。

## Slide 49: BL14での測定（Ein＝ 1.17 meV)
低エネルギーでは小角散乱の影響が大きくなる。
Chart: 散乱角(degree)

## Slide 50: Sample
Chart: Scattering Angle (degree)
We have measured 2 ED-4 samples. The results agree very well.
Elastic Scattering
Ein = 7.74 meV

## Slide 51: Facility ~Materials and Life Science Experimental Facility: MLF~
Experimental hall
3GeV,
proton beam
Building dimension :
Width : 70m
Length : 146m
Height : 30m
Exp. Hall Height : 22m
Proton beam line
1MW Spallation Target Station
(Mercury Target)
Target remote handling room
Spallation Mercury target
BL04: Nuclear
Data Beam Line
J-PARC MLF,
Taken from HP of J-PARC
Cooling systems (Basement)

## Slide 52: ANNRI (For transmission experiment)
NaI(Tl) Spectrometer
BL04: ANNRI (Accurate Neutron Nucleus Measurement Instrument)
Ge Spectrometer
6 and 7Li Glass detectors
Notes: First, I’ll show you the outline of ANNRI for transmission experiment
ANNRI is located on Beam Line NO.4 of MLF.
This figure shows a schematic view of ANNRI.
In ANNRI, we have two gamma-ray spectrometers for capture cross section measurements.
One is Ge detector array and the other one is NaI detectors.
Also, Li-Glass detectors for total cross section measurements are also equipped.

## Slide 53: Li Glass detectors for total cross section measurement
Li-glass detector
Sample
A 6Li-glass scintillation detector for neutron and a 7Li-glass scintillation detector for γ-ray B.G. were installed at the flight length of 28.7m
Measurements of neutron total cross sections of 241,243Am and 155,157Gd have been finished.
DAQ
( CAEN V1720)
TOF spectra for 241Am