## Slide 1
Improvements on the damage calculations using evaluated nuclear data and NJOY
Shengli Chen1, David Bernard2
1 Sino-French Institute of Nuclear Engineering & Technology, Sun Yat-sen University, China
2 CEA, IRESNE, DER/SPRC/LEPh, Cadarache, France
June 7, 2023
Aix-en-Provence, France

## Slide 2
Sun Yat-sen University
1 University, 3 Cities & 5 Campuses
广州
Guangzhou
深圳
Shenzhen
珠海
Zhuhai
IFCEN in Zhuhai
Sino-French Institute of Nuclear Engineering &Technology (IFCEN) (Zhuhai)
Institut franco-chinois de l'énergie nucléaire (IFCEN)

## Slide 3
2009：Witnessed by prime ministers of both China and France, SYSU and FINUCI Created IFCEN Jointly on SYSU Zhuhai Campus
  Grenoble INP-UGA
  CEA-ISTN
  Ecole de Chimie
  de Montpellier
  IMT Atlantique
  Ecole de Chimie
  de Paris
2015
Phase II agreement signed
2022
Phase III agreement signed

## Slide 4
卢鹤绂院士
中国“核能之父”
“第一个揭露原子弹秘密的人”
卢鹤绂教授坪石授课
3 years preparatory cycle
3 years engineering cycle
1 year undergraduate
Training in Guangzhou south campus
3 years undergraduate college training
Sino-French cooperation integration
3 years master
From other bachelor program
Improvement: A Fused System
Sino-French Cooperation
(French as the first foreign language)
3+3 4+2
2010-2020
Training in big academic subjects
Sino-French cooperation integration
（French as a second foreign language）
1+3+3 since 2021
Professional
Master
Two-year
system
Undergraduate
Four-year system
3 years
Preparatory cycle
Engineering cycle
3 years
Three years
In China
Undergraduate
Three years
In China
3 years of Sino-
French excellence
Preparatory
Professional
Master
3 years of Sino-
French excellence
Engineering
One year
Training in
big academic
subjects
(south campus
in Guangzhou)
French preparatory
& engineering education model
China undergraduate
& master
education model
SYSU
Characteristics
A Fused Sino-French System
CTI Accreditation Renewal in 2022:
A 6-Year accreditation received --- the longest possible!
The high-quality of the IFCEN program fully recognized!

## Slide 5: ND @ IFCEN: Summary and Prospect
IFCEN is prepared for nuclear data education and research (theory, experiment, structure and decay, fission and reaction), chance to construct the unique sub-major in China
Hope to obtain help from other collaborators
Education:
  Introduction to Nuclear Physics and Nuclear Data: 14 sessions for nuclear data part
  Introduction and Application of Nuclear Data: 36 sessions
  Nuclear Data Acquisition and Processing: 54 sessions
  Lectures to colleagues and students for general introduction to nuclear data
Research:
  Nuclear structure data evaluation system
  Machine learning based nuclear data evaluation and application
  Macroscopic validation
  Associate Professor (9): Cenxi YUAN, Jun SU, Long ZHU, Wei HUA, Bo MEI
  Assistant Professor (2): Shengli CHEN

## Slide 6: Outline
Introduction of damage cross section
Two-body reaction-induced
Neutron capture reaction-induced
N-body reaction-induced
Conclusions

## Slide 7: (Neutron) irradiation damage
@Knaster2016NatPhys
Incident particle
Light emitted particle
Target nucleus
Recoil nucleus (= PKA)
Atoms in lattice
(e.g., n, γ e-, e+, Xn+)
PKA: Primary Knock-on Atom
Atomic displacements
304 stainless steel irradiated in OSIRIS at 330 ℃ and tested at 330 ℃
@Averty1998Fontevraud4
Displacement per Atom (DPA)

## Slide 8
Incident neutron
channel 1
…
Chart: 
Recoil energy
Recoil energy
Chart: 
Chart: 
Recoil energy
…
Target nucleus
channel 2
channel n
Neutron flux
PKA spectra
Damage cross sections
Radiation damage
Radiation damage model
Radiation damage model
Two paths to compute neutron irradiation damage
Chen, Nucl. Instrum. Methods B, 508: 41-48, 2021
8
Flux independent

## Slide 9: Threshold displacement energy and Kinchin-Pease model
@King1983JNM
Ed
Probability of displacement
Exp. Data of Cu
Step function approach
2Ed Energy
Number of displacement
E - Ed < Ed
Boundary condition:
N(2Ed) = 1
, [2Ed, Ec]
E
E-Ed
PKA

## Slide 10: Currant DPA formulae and generalized damage energy
Norgett-Robinson-Torrens (NRT-DPA) (1975)
Damage energy:
PF: atomic displacement
(1 – PF): electronic excitation/ionization
Athermal Recombination-Corrected (ARC-DPA) (2015)
Use of generalized damage energy (GDE):
A unique form!

## Slide 11: Damage cross section based on GDE
Damage (energy) cross section:
Reaction XS
Normalized differential XS
DPA XS and damage XS for monatomic materials:
Vector including all free parameters
With reliable recoil spectra

## Slide 12
Discrete reactions:
m, v1
m', u1
M, v2
M’, u2
CM
vCM
u2
vR
u1
v'
Calculation of damage cross section:
Angular distribution
Two-body reaction-induced: theory
m, E
m’, E’
M, 0
M', ER
Continuum reactions:
Energy-angular distribution
(i.e., double differential cross section, = DDXS)
Chen et al., Nucl. Instrum. Methods B, 456: 120–132, 2019

## Slide 13: Two-body reaction-induced (1)
52Cr
55Mn
55Mn MT91
Incorrect recoil data!
Wrong frame
Chen and Bernard, J. Nucl. Mater., 562: 153610, 2022

## Slide 14: Two-body reaction-induced (2): 59Ni
Chen and Bernard, J. Nucl. Mater., 562: 153610, 2022
Further (experimental) investigation on the DDXS of the (n,α) reaction

## Slide 15: Two-body reaction-induced (3): W in ENDF/B-VIII.0
Chen et al., Fusion Eng. Des., 171: 112594, 2021
Chen and Bernard, J. Nucl. Mater., 562: 153610, 2022
184W(n,2n)
Wrong frame?
Spectrum | JEFF-3.3 | JENDL-4.0u | ENDF/B-VIII.0 | Modif. MF6 | Max. Diff.
First mirror unit | 1.009 | 1.072 | 0.647 | 0.958 | 66→11%
Inner vertical target | 1.022 | 1.085 | 0.640 | 0.964 | 70→13%
14 MeV
DPA rates / JEFF-3.1.1 calculation (NatW)

## Slide 16: Two-body reaction-induced (4): 56Fe in JEFF-3.3
Chen, Nucl. Mater. Energy, 33: 101284, 2022
665 keV max. recoil in ENDF
> kinematics limit 523 keV!
56Fe
EUROFER97
10 MeV

## Slide 17
Average recoil energy:
Neutron capture reaction-induced: theory
Chen, Nucl. Instrum. Methods B, 513: 1–8, 2022
NJOY for MF6:
!
NJOY for MF12-15:
184W(n,γ)185W

## Slide 18
Neutron capture reaction-induced (1): 56Fe and 58Ni
Discrepancy is significantly reduced
Chen, Nucl. Instrum. Methods B, 513: 1–8, 2022

## Slide 19
Neutron capture reaction-induced (2): 184W
!
GDE:
TALYS-1.9
More accurate photon data
Stochastic sampling of photon kicks
Chen, Nucl. Instrum. Methods B, 513: 1–8, 2022

## Slide 20: N-body reaction-induced
For N > 2 emission nuclear reaction：
Scalar variables: 3N
Scalar equations: conservation of momentum 3 (+ energy 1)
Degree of freedom (DOF): 3N-3 (or 3N-4)
DOF in evaluated files: ≤ 2N
without recoil spectra:
DOF ≤ 2N-1 < 3N-3
Approximation required!

## Slide 21: For (n,2n) reaction
Indistinguishable 2 neutrons
N = 3, DOF：33-3 = 6
Without recoil spectrum, DOF in ENDF ≤ 3 Approximation
Symbol | Method for computing recoil energy
R | Recoil energy directly retrieved from ENDF
INL | Treating (n,2n) reaction as continuum inelastic scattering
B1 | Binary approximation using a = 1
B2 | Binary approximation using a = 2
KCM2 | Kinematics using secondary data in the CM frame twice
KCM1 | Kinematics using secondary data in the CM frame once
KLab2 | Kinematics using secondary data in the Lab frame twice
KLab1 | Kinematics using secondary data in the Lab frame once
Chen, Nucl. Instrum. Methods B, 508: 41–48, 2021

## Slide 22: (n,2n) reaction-induced damage cross section
Reasonable agreement between different methods
Chen, Nucl. Instrum. Methods B, 508: 41–48, 2021

## Slide 23: Conclusions & outlook
NJOY prefers using (not well verified) recoil data in MF6
Verification using max. & min. recoil energies
(n, γ): more accurate photon data; sampling of photon emissions
(n,2n): agreement between different approaches
Adding verification option in NJOY HEATR
Implementing stochastic sampling for (n, γ) (e.g., TRIPOLI, PHITS)?
Evaluation: verifying recoil data & photon data

## Slide 24: References
S. Chen, D. Bernard, P. Tamagno et al., Calculation and verification of neutron irradiation damage with differential cross sections, Nucl. Instrum. Methods B, 456: 120–132, 2019
S. Chen, Methods for calculating the (n,2n) reaction-induced damage cross section with different approaches of kinematics, Nucl. Instrum. Methods B, 508: 41–48, 2021
S. Chen, D. Bernard, Y. Peneliau, Comparison of evaluated nuclear data for neutron irradiation damage calculation in fusion spectra, Fusion Eng. Des., 171: 112594, 2021
S. Chen, Study of neutron capture reaction-induced displacement damage cross section and KERMA factor, Nucl. Instrum. Methods B, 513: 1–8, 2022
S. Chen and D. Bernard, Recommendation for computing neutron irradiation damage from evaluated nuclear data, J. Nucl. Mater., 562: 153610, 2022
S. Chen, New evaluation of neutron-induced displacement damage cross section for EUROFER97, Nucl. Mater. Energy, 33: 101284, 2022

## Slide 25
Shengli Chen (陈胜利)
chenshli23@mail.sysu.edu.cn
Thank you!