## Slide 1: Overview of sigraflex
J. Maestre and C. Torregrosa
On behalf of EN-STI-TCD

## Slide 2: Agenda
Summary of previous meetings
Experimental characterization and numerical model of sigraflex
Introduction to the future HRMAT-HED: sigraflex target
Further discussions and Next steps

## Slide 3: Summary of previous meetings
Production of the sigraflex samples and set-up of the testing machine under controlled temp and speed rate.
Discussion on possible models for sigraflex and in particular about the EoS.
Series of meetings with SGL-NTNU-CERN in order to enhance the understanding of the sigraflex and how it is made. Additional meeting with UKAEA aiming for discussing about last findings on HRMAT-43
Summary of previous experimental tests and findings; new proposal tests and discussion about possible numerical models.
Review of the current status about:
Modeling
Experimental tests

## Slide 4: Summary of the last meeting 18th sept 2020
CERN side:
Summary of findings related to HRMAT-43:
Overall dynamic response of the TDE core for RUN2-3
Last findings on the operational dump related to the fracture of the HLM disc that constrains the sigraflex core of the TDE
Modeling: it is required to define a model for the analysis of the local behavior (level of the sheets) and macro behavior (stack of sheet) key parameters
Estimation of the conditions at which the sigraflex can be exposed in term of: energy deposition, temp, thermal strain-rate, etc. useful to define the model
Micro-physic
Macro-physics

## Slide 5: Summary of the last meeting 18th sept 2020
NTNU side:
Extensive review of the literature and summary of known properties/parameters related to sigraflex or expanded graphite
Experimental test:
  On going test:
  Proposal test:
Modeling concepts: continuous model based on porous media
Series of tensile tests at different conditions:
Strain-rate
Air-vacuum
Pre-compression
Micro-sheet foils seems to be relevant
CTE testing:
  Strain-rate
  Air-vacuum
Micro CT scan
Compression test:
  Air-Vacuum
  In-plane and out-plane

## Slide 6: HRMAT-HED (2021)
Sigraflex Target: main goals:
Proton Beam
Sample of 0.5 mm thickness tested in HRMT-43 saw 2450 J/g
Investigate further the response of Sigraflex under beam impact:
  - Gas/Vacuum
  - Constrained / unconstrained / compressed
  - Beam spot size
  - Intensity ramp-up to identify limit
0.2x0.2 mm

## Slide 7
Thank you for
your attention!

## Slide 8: New modeling proposal
Classical constitutive eq. can be very complex to define because of the complexity of the sigraflex itself:
Orthotropic
Non-symmetrical
Strain rate/temp dependency
Trapped air? Multiphase
Micro-physics??
Micro-FEM
Macro-Models
Multi-scale models:
Capture the micro-physic implicitly
No-need for complex constitutive eq.
…but computational expensive
DNS
MICRO-FEM
DMN Deep material network
ONLINE
MACRO FEM
Micro-physics is embedded
Extrapolation
CPU expensive