## Slide 1
Annealing R&D at FNAL
Daniel Bafia
LCWS’21
17th March 2021

## Slide 2: Outline
Introduction
High Temperature N-Doping (>800C)
Low Temperature in-situ bake (90-200C)
Mid Temperature in-situ bake (200-400C)
Conclusions & Future Work

## Slide 3: Outline
Introduction
High Temperature N-Doping (>800C)
Low Temperature in-situ bake (90-200C)
Mid Temperature in-situ bake (200-400C)
Conclusions & Future Work

## Slide 4: State-of-the-art in High Q0 and High G
Dramatic increase in performance of Nb SRF cavities in recent years
N-Doping: Q0>3e10 @ 38 MV/m
Mid-T Bake: Q0>4E11 @ T<1.5 K!
75/120C ‘Modified’ Low T bake: record quench >50 MV/m (213mT)
Lessons learned on drivers for high Q0 and High G
What limits quench in high Q0 cavities?
What ‘heals’ HFQS post LTB?
What enables ultra-high gradients?
T = 2 K
f0 = 1.3 GHz
Mid-T Bake
N-doped
LTB
75/120C Mod Bake
EP

## Slide 5: Outline
Introduction
High Temperature N-Doping (>800C)
Low Temperature in-situ bake (90-200C)
Mid Temperature in-situ bake (200-400C)
Conclusions & Future Work

## Slide 6: Our Current Stand in High T N-Doping Quench Fields
Achievable quench field has evolved: 17 – 20 MV/m [2013]
D. Bafia et al., SRF’19
Improvements enabled by tweaking the doping ‘recipes’ But what drives quench in N-doped cavities?
2013 N-Doping Performance, Single Cells
2021 N-Doping Performance, Single Cells
 30 – 38 MV/m [today]
T = 2 K
f0 =1.3 GHz
T = 2 K
f0 =1.3 GHz

## Slide 7: Key Knobs in Nitrogen Doping
N2
Nb
Slides adapted from M. Martinello
800C UHV, XX hours
800C UHV, XX minutes
UHV cooling
XX um EP
N
Final RF Surface
800C UHV, XX minutes
UHV cooling
XX um EP
800C N2
p = 25 mTorr XX minutes
800C N2
p = 25 mTorr XX minutes
N Interstitial
NbxNy
Depth Profile of Nitrogen Impurities
2/0
2/6
Different recipes =
different N concentrations =
different performance
A. Grassellino, SRF 2019
Y. Trenikhina et al, Proc. of SRF 2015

## Slide 8: Possible Cause for Quench in Doped Cavities: Surface Roughness
One possible origin of quench in N-doped cavities may stem from surface roughness present after the final EP
Typically optimize EP using clean, bulk Nb
However, cavities have a heavily nitrided surface after the N-doping furnace run  substantially altered chemical potential
   Shifts electropolishing to the etching/pitting regime
May create rough surface; preferential etching at some grains?
Rough, recessed grains
V. Palmieri, SRF’03
One possible fix: by lowering electrolyte temperature, may slow down removal, remain in polishing regime, and produce a smoother surface
I-V Curve for EP
SEM Images of FNAL N-Doped 9-Cell Cavity Cutout

## Slide 9: Investigating Quench Field Post Standard vs Cold EP
A 9-cell cavity was subjected to the 2/0 nitrogen doping surface treatment with different final EP temperatures at FNAL with a surface reset in between
Standard temperature EP:
Quench at 20 MV/m
Quench at 25 MV/m
T=2 K
f0 = 1.3 GHz

## Slide 10: Investigating Quench Field Post Standard vs Cold EP
A 9-cell cavity was subjected to the 2/0 nitrogen doping surface treatment with different final EP temperatures at FNAL with a surface reset in between
Standard temperature EP:
Quench at 20 MV/m
Quench at 25 MV/m
Cold EP:
Quench at 32 MV/m!
T=2 K
f0 = 1.3 GHz

## Slide 11: A Possible Path for Higher Fields in N-Doped Cavities: Cold EP
In the context of LCLS-II HE R&D, found that 9-cell cavities with lower final EP temperatures quenched at higher fields!
Cold final EP may slow down Nb etching, ensures a smoother surface
Qual. Threshold: 23 MV/m
The lower the EP temperature, the higher the max gradient
M. Checchin, TTC’2020, CERN

## Slide 12: Conclusions for High Temperature N-Doping
Although all steps of N-doping are important, optimization of electropolishing parameters is critical to unlock higher gradients
Performing the final electropolishing step post the N-doping furnace run at lower temperatures likely slows down the removal process and ensures a smoother surface

## Slide 13: Outline
Introduction
High Temperature N-Doping (>800C)
Low Temperature in-situ bake (90-200C)
Mid Temperature in-situ bake (200-400C)
Conclusions & Future Work

## Slide 14: Finding #1: Role of Oxygen in HFQS Mitigation/Mild Baking
Cut out TOF-SIMS studies revealed oxygen diffusion as a driver for the 120C baking effect
EP cavity: no O- signal beneath oxide
Mod bake: substantial O- below oxide
  O diffusion in Nb follows Fick’s law, Benvenuti, SRF’01
Implications: HFQS in SRF cavities is mitigated by O diffusing from oxide and trapping free H
A. Romanenko, TTC’20, CERN
Mod bake
EP
Any LTB should mitigate HFQS, not just 120C
T = 2 K
f0 =1.3 GHz

## Slide 15: Evolution of HFQS with Sequential in-situ Baking Treatments
A cavity was sequentially baked in-situ at 90C (x 12hr, x 24hr, etc.) without disassembly/ever losing vacuum
Observe gradual increase in HFQS onset after each step
HFQS absent up to quench after 90C x 384 hr (16 days)!
Calculated O concentration with depth after each step
  As oxygen diffuses deeper, HFQS moves up in field
Calculated O Profile
HFQS eliminated after 90 C x 16 days!
T = 2 K
f0 =1.3 GHz

## Slide 16: Recreating Performance by Tailoring Same O Profile
Baked two cavities with different treatments that produce the same oxygen profile with depth
160C x 12hr
200C x 1hr
Calculated O Profile
Identical oxygen profiles produce identical RF performance!
90 C x 384 hr, 160 C x 12 hr, 200 C x 1 hr all work just as well as 120 C!
O diffusion plays critical role in HFQS mitigation - supports Romanenko model of hydrides
T = 2 K
f0 =1.3 GHz

## Slide 17: Finding #2: Record Gradients via 75/120C Bake + Cold EP
FNAL developed 75/120C modified low T bake treatment + cold EP:
1) Record-breaking quench fields
2) Bifurcation phenomenon
75C x 4hrs
120C x 48hrs
- growth and dissipation of room
temperature Nb nano-hydrides
50 MV/m!
Cavity Post 75/120C Baking at FNAL Sent to Other Labs Around the World
AFM studies by Z. Sung et al., SRF’19
See talk by Sam Posen from Monday of this conference for application of this treatment in a prototype High Gradient Cryomodule for ILC!
Produces two phenomena
D. Bafia et al., SRF’19

## Slide 18: Conclusions for Low Temperature Baking
The diffusion of oxygen in low temperature (90C – 200C) in-situ baking is responsible for the mitigation of high field Q slope and enables higher quench fields in cavities
Record-breaking gradients achieved via 75/120C modified low temperature baking + cold EP

## Slide 19: Outline
Introduction
High Temperature N-Doping (>800C)
Low Temperature in-situ bake (90-200C)
Mid Temperature in-situ bake (200-400C)
Conclusions & Future Work

## Slide 20: New Mid-T Bake Developed at FNAL
Pioneered a new mid-T (300C – 400C) in-situ bake that produces Q0>5e10 @ 2 K and Q0>4e11 at T<1.5 K
Yields performance between N-doping and N-infusion
4e11!
5e10!

## Slide 21: Origins of Ultra-High Q Post Mid-T Baking: SIMS Studies
Originally developed for quantum applications to dissolve oxides
In-situ mid-T baking performed on EP samples in SIMS
Oxide removed by mid-T bake
Nb2O5- Signal
NbN- Signal
Creates infusion-like N profile
S. Posen et al., PRA 13, 014024 (2020)
Mid-T baking provides a simple way to effectively perform N-doping without final EP  yields ultra-high Q0!
However, quench is still limited to ~30 MV/m; is there an optimal temperature and duration that yields both high Q0 and quench field?

## Slide 22: Optimizing Mid-T Baking for High Q0/High G: Sequential Studies
A single 1.3 GHz SRF cavity is currently being subjected to sequential treatments of mid-T baking (200C) without disassembly/ever losing vacuum
Cavity was baselined with the 90 C x 384 hr in-situ bake to remove HFQS
f0 =1.3 GHz
T = 2 K

## Slide 23: Optimizing Mid-T Baking for High Q0/High G: Sequential Studies
A single 1.3 GHz SRF cavity is currently being subjected to sequential treatments of mid-T baking (200C) without disassembly/ever losing vacuum
Cavity was baselined with the 90 C x 384 hr in-situ bake to remove HFQS
200C x 1 hr mid-T bake decreased Q0 and reduced quench field, curve shape changed
Estimate that oxide reduced by 0.25 nm – 0.5 nm
Suggests that partial oxide dissolution leads to substantial degradation
Performance gets worse before it gets better? Study ongoing
f0 =1.3 GHz
T = 2 K

## Slide 24: Outline
Introduction
High Temperature N-Doping (>800C)
Low Temperature in-situ bake (90-200C)
Mid Temperature in-situ bake (200-400C)
Conclusions & Future Work

## Slide 25: Conclusions
Substantial progress made in the understanding of High Q and High G
High temperature N-doping: EP parameters are important in surface finish  difference in achieving 17 MV/m and 30 MV/m!
Oxygen is a key player in the mitigation of HFQS in low temperature baking
75/120 C modified low temperature bake + cold EP shows record-breaking gradients
Mid-T baking: ultra-high Q’s already systematically achieved, currently taking steps to optimize further

## Slide 26: Future Work: Investigating New Surface Treatments with CVD/ALD
Fermilab will soon commission a new CVD/ALD furnace that will enable previously difficult surface treatments:
  Doping with different gases/elements
  A15 thin film deposition
  Baking in different atmospheres
Lots of new knobs to turn!
Will further optimize new recipes!
Notes: Quantum – deposit oxide (S-I-S, S-S structures)

## Slide 27: Thank you for your attention

## Slide 28: Backup

## Slide 29: Correlating Quench Field with SIMS Studies – 9 - Cell
Samples cut from each cell and studied in TOF-SIMS to obtain depth profile
Quench area – cell #1
Spot #1 – cell #5
Spot #2 – cell #5
NbN/Nb
C/Nb
S/Nb
F/Nb
O/Nb
Grassellino et al., SRF 2019

## Slide 30: Low Temperature Bake

## Slide 31: Role of Oxygen in Trapping of Hydrogen
A. Romanenko et al., Proc. of SRF’19, THP014

## Slide 32: Model of Oxygen Diffusion
Diffusion of oxygen in Nb very well modelled by assuming oxide serves as an infinite source
Benvenuti et al. SRF’01:
A. Romanenko, TTC’20, CERN

## Slide 33: Bifurcation in Performance
Possible Causes for Branching | Likely Candidate?
Dewar | NO – observed in 2 separate dewars
Top Plate | NO
Cables | NO
Calibration | NO - Qext 2 does not explain branching in Q and G
Flux trapping | NO – MOST were cooled in zero compensated field
f=1.3GHz
T=2K
Btrapped = 5.88mG to account for branching; not possible with compensation coils in VTS
Observed branching behavior in cavities retested without disassembly in between (always under vacuum)
3 single-cell cavities post 75/120C baking were tested several times without disassembly
D. Bafia et al., SRF’19

## Slide 34: Likelihood of Trapped Flux Causing Bifurcation
Tc
Tc
Tc
≤1mG before Tc
≤0.2mG before Tc
No transverse field compensation/fluxgates for these tests – but transverse fields measured to be <1mG in the past
Estimate of field necessary to cause bifurcation @ 40MV/m:
Rlower =270nΩ/1E10 = 27nΩ
Rupper =270/1.56E10 = 17.3nΩ
Btrapped =10nΩ /1.7nΩ /mG = 5.88mG
05/08 – no coils – 49MV/m
5/31 – coils – 41MV/m!

## Slide 35
Cryogenic Atomic force microscopy studies by Sung et al. found presence of previously unobserved room temperature niobium nano-hydrides on LTB samples
Warming to 320K caused room temperature niobium nano-hydrides to shrink in size
Applied similar protocol to cavities
Z. Sung et al., SRF’19
Hydrides found near room temp for 120C baked cutout
Avg. No. of NbH Precipitates within 10 x 10 μm2 unit area during cooling
Cryo-AFM Studies on 120C Bake Cavity Cutouts by Sung et al.

## Slide 36: Comparison of 75/120 Bake Cavities Cooled From 295K vs 320K
Cooling cavities from 320K shows consistently higher quench field and Q0 at high fields for cavities post 75/120 bake when compared to cooling from 295K.
In-situ 320K may be dissociating non-superconducting niobium hydrides
Chart: Hydride Size Through Warm Up of 120C Baked Cavity Cutout
| -0.10565999999999999 | 0 | 0.10565999999999999 | 0.21132000000000006 | 0.31697999999999998 | 0.42264000000000002 | 0.5283000000000001 | 0.63396000000000008 | 0.73961999999999994 | 0.84528000000000003 | 0.95094000000000001
300K | 10.0272 | 12.1364 | 8.978 | 8.4522 | 18.869 | 45.913 | 59.8121 | 41.9346 | 16.5423 | 0 | 1.4022
320K | 6.7294 | 2.8077 | 4.4415 | 27.2424 | 38.8374 | 37.0574 | 0 | 0.8542
Courtesy of Zuhawn Sung
QvsE of Cavities Post 75/120 Bake
AFM finds minimum Nb-H size @ 320K
f=1.3GHz
T=2K

## Slide 37: Decomposition of 75/120 Bake Cavities Cooled from 295K vs 320K
Branching in both BCS and residual components – not due to trapped flux
Cooling down from 320K gives a BCS similar to that of infusion

## Slide 38: Mid – T Baking

## Slide 39: Decomposition – EP Baseline

## Slide 40: Q(E) curves at 2K and lowest temperature
T =2K
400 C x 3 hr – exhibited N-doping behavior
800C x 3 hr followed by 400C x 3 hr – exhibited standard EP behavior
500C x 1 hr – EP behavior at 2K

## Slide 41: Pressure Data From the in situ SIMS Runs – Nitrogen Origin
400C first ramp up
800C first, then 400C
Another 400C without re-exposure
Nitrogen seems to be coming from the outgassing
A. Romanenko, TTC’2020 - CERN
Performed same treatments in SIMS
400 C x 3 hr – strong spike in pressure
800C x 3 hr then 400C x 3 hr – smaller spike in pressure
400C without re-exposure – substantially smaller peak

## Slide 42: SIMS in-situ Results on EP Cutouts
After 400C 1 hr straight
NbN/Nb
before
+800C 4 hr + 400C 1 hr
+400C 1hr + air
A. Romanenko, TTC’2020 - CERN
Only the “400C x 1hr straight” treatment introduced a substantial level of N in the RF layer