## Slide 1: SANDA WP3 Task 3.3: Target production
Goedele Sibbens, EC-JRC Geel, Belgium
SANDA meeting 11-02-2021

## Slide 2: Content
Task 3.3: Target production
Target requests
Status pending target requests
Some examples of prepared targets

## Slide 3: Task 3.3: Target production
Task coordinator: JRC, partners: PSI
Target requests related to energy and non-energy applications are considered.
During the first 12 months of the project, target requests from collaborators were collected.

## Slide 4: Target requests

## Slide 5: Target requests

## Slide 6: Pending target requests

## Slide 7: Examples
Backing
0.635 µm thick polyethylene film
Deposit
Be(NO3)2 thickness: 0.36 µm
7Be activity: 24.5 GBq
7Be(NO3)2 layer by drop deposition
E.A. Maugeri et al., Preparation of 7Be targets for nuclear astrophysics
research, 2017 JINST, Published by IOP Publishing for Sissa Medialab
PSI

## Slide 8: Examples
Backing
50 × 50 × 0.018 mm Al foil
placed between two Al frames
with a 40 mm diameter central hole
Implantation
7Be activity: 1 GBq
Implantation of 7Be into aluminium foils
E.A. Maugeri et al., Preparation and characterization of three 7Be targets for the measurement
of the 7Be(n, p)7Li and 7Be(n, 𝛼)7Li reaction cross sections, Nuclear Inst. and Methods in Physics Research, A 889 (2018) 138–144
PSI

## Slide 9: Examples
Backing
34 µg/cm2 polyimide foil
on 1 mm thick Al ring Øout 90 mm Øin 70 mm
Deposit
238U diameter: 20 mm
238U areal density: 377 µg/cm2
238U mass:1.84 mg
JRC-Geel
238UF4 deposit by vacuum evaporation

## Slide 10: Examples
Backings for target request 4x 238U 350µg/cm2 Ø 30mm (SANDA T1.2.3)
+ 62 µg/cm2 PI foil (JRC-Geel)
1mm thick Al ring
Øout 60mm Øin 40 mm (JRC-Geel)
+ 87 nm Al deposit (CEA)

## Slide 11
SANDA target request form
Target request to be sent to
Dorothea Schumann
dorothea.schumann@psi.ch
Goedele Sibbens
goedele.sibbens@ec.europa.eu

## Slide 12: Thank you Goedele Sibbens EC-JRC Geel, Belgium goedele.sibbens@ec.europa.eu
© European Union 2020
Unless otherwise noted the reuse of this presentation is authorised under the CC BY 4.0 license. For any use or reproduction of elements that are not owned by the EU, permission may need to be sought directly from the respective right holders.
Notes: Update/add/delete parts of the copy right notice where appropriate.
More information: https://myintracomm.ec.europa.eu/corp/intellectual-property/Documents/2019_Reuse-guidelines%28CC-BY%29.pdf