## Slide 1: 4D tracking – sensors with internal gain
N. Cartiglia
INFN - Torino
23 April 2021

## Slide 2
Sensors for future trackers
Without avalanche gain
Hybrid
Monolithic
BiCMOS
(SiGe)
Passive
CMOS
CMOS
Planar
Si/Diamond
3D
Si/Diamond
With avalanche gain
Low-gain mode (LGADs)
High-gain and Geiger mode (APD, SPADs)
AC-coupled
BiCMOS
(SiGe)
Resistive readout
DC-coupled

## Slide 3
4D tracking – sensors with internal gain
With avalanche gain
Low-gain mode (LGADs)
DC-coupled
AC-coupled
BiCMOS
(SiGe)
Resistive readout
First design innovation: low gain avalanche diode (LGAD)
  ==> ~ 20 gain, thin sensors, large signals, large dV/dt
  Excellent timing resolution (~ 30 ps), not so good spatial resolution (pixel/sqrt(12))
Second design innovation: resistive read-out (joining RPC, GEM..)
  ==> Spread the signal over many pads while maintaining good efficiency (due to internal gain)
  Excellent position and timing resolutions (<5 um, ~ 30 ps)

## Slide 4
By “4D tracking” we mean the process of assigning a space and a time coordinate to a hit.
Timing can be available at different levels of the event reconstruction:
Timing in a single point (timing layer ATLAS,CMS)
Timing at some points along the track
Timing at each point along the track
We are just at the beginning of this path
4D tracking – options

## Slide 5: 4D tracking: Sensor – ASIC interaction
C Det
R in
Sensor
ASIC
Sensors produce a current pulse
In timing circuits ”things can go wrong very rapidly” (quote from a wise ASIC designer),
==> this is not a simple evolution of what we know how to do.
Optimization of 4D tracking can only happen with a very strong collaboration between the two community.
Future developments need to be done by desiging the sensors and the ASIC together
ASICs measure the time of arrival
==> Sensors and ASICs are two parts of a single object

## Slide 6
First design innovation: low gain avalanche diode
The LGAD sensors, as proposed and first manufactured by CNM
(National Center for Micro-electronics, Barcelona):
High field obtained by adding an extra doping layer
E ~ 300 kV/cm, closed to breakdown voltage
The low-gain mechanism, obtained with a moderately doped p-implant, is the defining feature of the design.
The gain layer:
a parallel plate capacitor with high field
zoom
Drift area with gain
0.5 – 2 mm long

## Slide 7
Summary of LGAD temporal resolution
Resolution without gain
There are now hundreds of measurements on 45-55 mm-thick UFSDs
 Current sensor choice for the ATLAS and CMS timing layers
Non-uniform ionization
Physical limit:
non uniform signal shape
Amplitude variation
Shape distortion
Simulation of signals in 50-um RSD

## Slide 8: LGAD radiation hardness
Evolution with radiation of the biasing working point for a 45-micron thick LGAD with a carbonated gain layer
Increase bias to compensate for gain implant doping deactivation.
Present LGAD designs provide large signals and low noise up to 2.5E15 n/cm2

## Slide 9
Second design innovation: resistive read-out
9
The signal discharges to ground
The AC pads offer the smallest impedance to ground for the fast signal
The signal is formed on the n+ electrode ==> no signal on the AC pads
-+
-+
-+
-+
-+
-+
Fast signal
long RC
Fast signal
long RC
In resistive readout the signal is naturally shared among pads (4-6) without the need of B field or floating pads
Thanks to the internal gain, full efficiency even with sharing

## Slide 10
10
The laser is shot at the position of the magenta dot: the signal is seen in 4 pads
Example of a signal in an RSD
Pad 1
Pad 3
0 2 4 6 8
Time [ns]
0 2 4 6 8 10
Time [ns]
0 2 4 6 8 10
0 2 4 6 8 10
60
40
20
0
-20
Amplitude [mV]
60
40
20
0
-20
60
40
20
0
-20
Amplitude [mV]
60
40
20
0
-20
1
2
4
3
P 1
Pad 1
Pad 2
50-mm thick RSD,
Gain ~ 20
Pad 4

## Slide 11: Summary of RSD position resolution
RSDs reach a spatial resolution that is about 5% of the inter-pad distance
 ~ 5 mm resolution with 150 mm pitch
RSDs have the “usual” LGAD temporal resolution of 30-40 ps

## Slide 12: ASIC for RSD
12
Very important point: in hybrid technology (sensor bump-bonded to the ASIC), the area available for each read-out channel is identical to the pixel area
ASIC channel area
150 x 150 um2
Assuming a goal of ~ 5 mm spatial resolution,
the RSD pitch can be 150-200 mm
At least a factor of 10-20 more space than using binary readout
Can concentrate the power available for that area into a single channel
The needed circuits for timing might actually fit
Sensor
ASIC

## Slide 13: Manufacturers: a pretty large pool
Producer | LGAD | RSD | Funding Source | Collab. Institute | Projects
CNM Barcelona (Spain) RD50 member | Doping Radiation Arrays Carbon, Gallium | Time Resolution | Spanish Ministr. RD50 (DoE R&D) AIDA, AIDAInnova | IFAE RD50 IFCA | ATLAS HGTD CMS-ETL
FBK Trento (Italy) RD50 | Radiation Carbon Isolation | Geometry Spatial & Time Resolution. | INFN, ERC, AIDA, AIDAInnova RD50 (DoE R&D) | INFN Torino RD50 | ATLAS HGTD CMS-ETL
Micron (UK) | Small Pixels |  | UK Science Council | Glasgow U. | X-ray Diamond
HPK (Japan) | Doping , Thickness Radiation, Arrays | Time Resolution | (DoE R&D) BNL ATLAS CMS | UCSC KEK | ATLAS HGTD & CMS-ETL Collaboration
BNL, (US) RD50 member |  | Time Resolution | DoE LDRD | BNL, FNAL UCSC | EIC
NDL (China) | 8” |  | Chinese Gov | IHEP | ATLAS HGTD
IME (China) | 8” |  | CAS | USTC | ATLAS HGTD
T-e2v | Time Resolution |  | STFC | Birmingham, Oxford, RAL | 
Red: Research Institutions
Blue: large commercial manufacturers

## Slide 14: Present results & short term evolutions - I
Physicist
Trench-isolated design
LGAD evolution: use trenches
Signal in a single pixel
Almost 100% fill factor
Temporal resolution (50 mm) : 35-40 ps
High Occupancy OK
Rate ~ 50-100 MHz
Rad hardness: to be studied
No gain area ~ 5 um
No gain area ~ 50 um
JTE/p-stop LGAD
CMS && ATLAS choice
Signal in a single pixel
Not 100% fill factor
Very well tested
High Occupancy OK
Rate ~ 50-100 MHz
Rad hardness ~ 1-2E15 n/cm2
HPK2
16x16 array
2.1 cm
JTE + p-stop design

## Slide 15: Present results & short term evolutions - II
RSD: resistive readout
Signal in many pixels
100% fill factor
Excellent position resolution:
  ~ 5 mm with large pixels
Temporal resolution (50 mm) : 35-40 ps
Rate ~ 10-50 MHz
Rad hardness: to be studied
i-LGAD
p-side segmentation
Signal in a single pixel
100% fill factor
Thin i-LGAD with single side processing under development (using trenches, spring 2021 @ CNM)
High Occupancy OK
Rate ~ 50-100 MHz
Rad hardness: to be studied

## Slide 16: Contacts and future projects
In the recent past, many experiments have expressed interests in pursuing R&D projects on fast timing
Existing experiments:
ALICE3
CMS LS3
NA62++
LHC-b
HADES
Future projects
FCC-ee,
CLIC,
FCC-hh,
m-m collider
Despite this large group of experiments, there is not a coordinated effort yet on 4D tracking. Each experiment does its own R&D
For the sensors: RD50 is the focal point

## Slide 17: 4D tracking in the far future - I
Dead area:
Now: 50-80 mm between pads
most likely it will become very small, <5 mm
Production yield:
Now: maximum sensor dimensions are ~ 3x3 cm2
it will increase with experience, maybe even to the full 10x10 cm2
Foundries might switch to 8” and dramatically increase productivity
Radiation hardeness :
Now: ~ 2E15 neq/cm2
Difficult to say, a possible hard limit on the safe bias voltage (10V/mm) might reduce possible improvements. Near goal: ~ 5E15 neq/cm2

## Slide 18: 4D tracking in the far future - II
Timing resolution:
Now: 30 ps for 50 mm thick sensor
Thinner LGAD do better, but the signal charge is less.
The improvements will depend on the ASIC more than on the sensor.
Spatial resolution:
Now: < 5 mm in RSD, ~ 100’ mm in LGADs
LGAD have a resolution of pixel/sqrt(12).
Very difficult to measure accurately time in very small pixels.
Resistive read-out has an extraordinary position resolution with large pixels ==> only for low occupancy experiments

## Slide 19
Another possible future: the BiCMOS way
Without avalanche gain
Monolithic
With avalanche gain
Low-gain mode (LGADs)
BiCMOS
(SiGe)
Monolithic BiCMOS, using the properties of SiGe transistors, obtains excellent timing performances.
Presently without internal gain, in the near future with internal gain

## Slide 20: Monolithic design for 4D tracking (FASER)
Isolated HBT for signal amplification.
Analogue electronics in pixel, digital electronics in a separate deep-nwell to improve noise robustness.
>95% fill factor.
Negative High Voltage applied to the heavily p-doped substrate.
Electronics inside the guard-ring, isolated from substrate using deep n-well.

## Slide 21: Prototype chip in SiGe BiCMOS
1
2
3
5
4
Time resolution [ps]
Pixel size: ~100×100 µm2
Pixel capacitance: 80 fF
MPV input charge: 0.25 fC
No cut on data
TOF test with Sr-90 source
Preliminary
Thr: 1050 e-
Thr: 920 e-
Thr: 600 e-
Thr: 570 e-

## Slide 22: R&D in progress at the University of Geneva
MONOLITH Project:
ERC advanced for the development of monolithic silicon pixel sensors in SiGe BiCMOS with picosecond time resolution. Sensor design based on PicoAD concept of the University of Geneva.
FASER :
SNSF project to build of a new pre-shower module for FASER experiment at LHC based on monolithic pixels in SiGe BiCMOS with very large dynamic range, 100 µm pixel size and 100ps time resolution.
100 µPET:
SNSF project to build a small animal PET scanner with 100 µm resolution based on monolithic silicon pixel sensors in SiGe BiCMOS.

## Slide 23: Conclusions
4D tracking based on internal gain is a very young development
Presently, the first 2 large timing layers are being built
Intense R&D in many aspects, many new experiments are planning to have a flavor of 4D tracking
Possible to achieve excellent position and time resolutions
Each experiment is different in term of requirements (material budget, fluence, resolutions, etc): there is not a fit-all design
Very difficult to improve from 30 ps to 10 ps per hit